Energy Education and Research Collaboration

Sixth Quarterly Report

April 14, 2008-Sep1, 2008

###### Prepared by

Prof. Nariman Farvardin, Provost

Principal Investigator and EERC Project Director

Prof. Avram Bar-Cohen, Chair

EERC Project Deputy Director

Dr. Azar Nazeri

EERC Research Manager

A.J. Clark School of Engineering

University of Maryland, College Park, MD 20742-3035

Prepared for

The Petroleum Institute

Abu Dhabi, United Arab Emirates

Sep 1, 2008

EERC Key Contributors

##### University of Maryland – College Park, MD, USA

Sami Ainane

Shapour Azarm

Balakumar Balachandran

Avram Bar-Cohen

John Cable

Serguei Dessiatoun

Nariman Farvardin

Ashwani K. Gupta

Ali Haghani

Yunho Hwang

Greg Jackson

PK Kannan

Ken Kiger

Mohammad Modarres

Reinhard Radermacher

Amir Riaz

##### Petroleum Institute – Abu Dhabi, UAE

Ali Almansoori

Ahmed Abdala

Tareq Al Ameri

Saleh Al Hashimi

Valerie Eveloy

Afshin Goharzadeh

Mansour Karkoub

Rocky Kubo

Michael Ohadi

Peter Rodgers

Mohamed Sassi

Abdennour Seibi

Table of Contents

List of EERC Key Contributors	ii

Table of Contents	iii

Executive Summary	1

Introduction	5

Individual Project Reports	11

A.	Educational/Research Activities	12

1-Visit to GASCO and ADGAS	13

S. Dessiatoun (UMD), M. Alshehhi (UMD), E. Al-Hajri (UMD)

B.	Research Thrusts	16

B-1 Energy Recovery and Conversion s

1-Force-Fed Cooling of Photovoltaic Arrays for High Efficiency Solar Energy Conversion Systems	17

S. Dessiatoun (UMD), A. Shooshtari (UMD), M. Ohadi (PI)

2-Sulfur Recovery from Gas Stream using Flameless and Flame Combustion Reactor	26

A.K. Gupta (UMD), M. Sassi (PI)

3-Solid Oxide Fuel Cells for CO2 Capture and Enhanced Oil Recovery	42

G. Jackson (UMD), V. Eveloy (PI), A Almansoori (PI)

4-Fundamental Immiscible Porous Media Studies for Improved Reservoir Models	53

K. Kiger (UMD), A. Riaz (UMD), A. Shooshtari (UMD)

5-Solar Cooling 	55

R. Radermacher (UMD), Y. Hwang (UMD) R. Kubo (PI), P. Rodgers (PI)

6-Waste Heat Utilization in the Petroleum Industry	67

R. Radermacher (UMD), Yunho Hwang (UMD), S. Al Hashimi (PI), P. Rodgers (PI)

B-2 Energy Efficient Transport Process 	75

1-Thermally Enhanced Polymer Heat Exchanger for Seawater Applications	76

A. Bar-Cohen (UMD), P. Rodgers (PI), A. Abdala (PI)

2-An EHD-Enhanced Gas/Liquid Separator	83

S. Dessiatoun (UMD), A. Shooshtari (UMD), M. Ohadi (PI), A. Goharzadeh (PI)

3-Study of Condensing Flows in a Micro-scale Channel with a Micro-element Array

and Visual Techniques	89

S. Dessiatoun (UMD), A. Shooshtari (UMD), M. Ohadi (UMD), A. Goharzadeh (PI)

B-3 Energy System Management 	98

1-Robust Optimization of Petrochemical Systems	99

S. Azarm (UMD), S. Al Hashimi (PI), T. Al Ameri (PI)

2-Dynamics and Control of Drill Strings on Fixed and Floating Platforms	109

B. Balachandran (UMD), M. Karkoub (PI), Y. Abdelmagid (PI)

3-Developing Corporate Dashboards for Multi-Unit Firms:  An Agent-Based Approach	120

P. K. Kannan (UMD), T. Al Ameri (PI)

4-Development of a Probabilistic Model for Degradation Effects

of Corrosion-Fatigue-Cracking in Oil and Gas Pipelines	125

M. Modarres (UMD), A. Seibi (PI)

Executive Summary

The following is a summary of the major project activities that have taken place over the completed quarter.  For more details, see the individual reports in the last section of this report.

A.	Educational/Research Activities

1-Visit to GASCO and ADGAS

The major purpose of this visit was to identify research opportunities for future EERC projects. Two ADNOC companies, GACSO and ADGAS, were supportive of our purpose and have shown interest in future research.

2- Future Faculty program

In this quarter, UM embarked on a new activity and started a pilot project to improve the preparation of ADNOC scholars for their future academic positions at PI. This program called Future Faculty Program (FFP) was delivered in June and July of 2008 to four UAE nationals (1 Ph.D. and 3 Ph.D. candidates).

3- Student Exchange

# Five PI seniors from four different departments spent six weeks as interns at UM in July and August 2008, in partial fulfillment of their curriculum requirements.

B.	Research Projects

Energy Recovery and Conversion Projects

1-Force-Fed Cooling of Photovoltaic Arrays for High-Efficiency Solar Energy Conversion Systems

S. Dessiatoun (UMD), M. Ohadi (PI)

Objective: To create a database on the available cooling techniques for high heat flux solar concentrator arrays necessary for efficient conversion of solar energy to electric power, and to design and fabricate an experimental prototype and associated setup to verify the feasibility of this concept and the capacity for force-fed cooling.

Progress:

- Constructed and packaged three complete samples consisting of bonded microchannels and a manifold with heater.

- WIrebonded heaters on three samples with the wirebonding machine at the Center for Nanophysics and Advanced Materials (CNAM) at the University of Maryland.

- Constructed an open loop experimental setup, consisting of the test section, a DC power supply, measurement devices, and a data acquisition system, to test the performance of the samples with water as a refrigerant.

- Tested the performances of the samples under different input power levels in an open loop system.

2-Sulfur Recovery from Gas Stream using Flameless and Flame Combustion Reactor

Prof. A.K. Gupta (UMD), M. Sassi (PI)

Objective: To obtain fundamental information on the thermal process for sulfur recovery from sour gas by conventional flame combustion and flameless combustion using numerical and experimental studies. The ultimate goal is to determine optimal operating conditions for sulfur conversion.

Progress:

- Reduced further the 20-reaction pathway mechanism to 17 reactions and tested it against two detailed mechanisms at different sets of operating conditions.

- Designed and fabricated an updated experimental facility capable of replicating Claus-process conditions in both the flame and flameless modes with minimized heat losses.

- Conducted preliminary tests of the updated facility to verify the homogeneity of the high-temperature environment needed for flameless combustion mode of sulfur recovery.

3-Solid Oxide Fuel Cells for CO2 Capture and Enhanced Oil Recovery

G. Jackson (UMD), S. Dessiatoun (UMD), V. Eveloy (PI), A. Almansoori (PI)

Objective: To investigate the feasibility of implementing advanced solid oxide fuel cell (SOFC) technology for producing power from oil well off-gases while providing a source of concentrated CO2 for sequestration and enhanced oil recovery.

Progress:

- Continued testing of membrane electrode assemblies (MEA’s) with Ni/YSZ/CeO2 anodes for performance on syngas (hydrocarbon reformate) and n-butane for a range of temperatures and fuel conversions.

- Refined heat transfer models in SOFC models for predicting temperature distribution in down-the-channel fuel cell models.

- Implemented first-generation down-the-channel fuel cell model for analysis of fuel cell performance on syngas streams.

- Began system-level analysis of integration of SOFC into petroleum processing.

4-Fundamental Immiscible Porous Media Studies for Improved Reservoir Models

K. Kiger (UMD), A. Riaz (UMD), A. Shooshtari (UMD)

Objective:  To study experimentally and numerically the detailed mechanics of immiscible two-phase flow in porous media, with the intent to explore the nonequilibrium mechanisms responsible for the breakdown of traditional continuum equations used for reservoir simulation. The outcomes of this research will enable the rational modeling extension of the traditional equilibrium relative permeabilties to account for the non-equilibrium conditions which occur for unstable displacement conditions.

Progress:

- The current funding represents an initiation seed program in anticipation of a fully funded project during Phase II. As such, current efforts have been directed towards developing the computational tools, techniques, and test facility that will be needed for the successful completion of the project.

5-Solar Cooling

R. Radermacher (UMD), Yunho Hwang (UMD), R. Kubo (PI), P. Rodgers (PI)

Objective:  To design, fabricate, and test a solar cooling system with the highest possible cooling COP measured to date.

Progress:

- Finished the literature review and published a review paper on solar cooling technologies.

- Modeled the solar sub-system in TRNSYS.

- Modeled the best combination between the solar technologies and the thermal cooling technologies in TRNSYS.

6-Waste Heat Utilization in the Petroleum Industry

R. Radermacher (UM), Yunho Hwang (UM), S. Al Hashimi (PI), P. Rodgers (PI)

Objective: To utilize waste heat in petroleum processing plants to minimize overall energy consumption.

Progress:

•	The following were modeled in ASPEN:

- GE MS6001 gas turbine

- Natural gas liquefaction and fractionation process

- Double effect water/LiBr absorption chiller

Energy Efficient Transport Processes

1-Thermally Enhanced Polymer Heat Exchanger for Seawater Applications

A. Bar-Cohen (UM), Dr. Peter Rodgers (PI), Dr. Ahmed Abdala (PI)

Objective: To address the fundamental thermal performance issues associated with the use of thermal high-conductivity polymer materials in heat exchangers.

Progress:

- Built crossflow heat exchanger and manifolds. Calibrated apparatus and began data collection.

- Submitted draft paper to 2009 Tunisia conference on Convective Heat and Mass Transfer in Sustainable Energy.

- Patrick Luckow visited the PI to assist in reviewing ADGAS heat exchanger data for designing a prototype polymeric heat exchanger.

- Began draft of review paper on polymer heat exchangers.

- Began Moldflow filling parametric analysis and creation of response surface models.

- Completed experimental verification of Moldflow filling simulation.

- Measured thermal conductivity of the thermally enhanced Nylon 12 to measure actual in-plane and out-of-plane conductivities.

2-An EHD-Enhanced Gas/Liquid Separator

S. Dessiatoun (UM), M. Ohadi (PI), A. Goharzadeh (PI)

Objective: To study hybrid inertia-EHD gas-liquid separation phenomena for electrically conductive and nonconductive liquid particles suspended in a moving gaseous medium.

Progress:

- Modified air-oil separator to enable safe operation and environmental conditions for the Aerodynamic Particle Seizer (APS).

- Ran experiments to test the behavior of droplets under voltage variations.

- Preparing journal paper for submission to the journal Aerosol Science and Technology.

- Visited ADNOC companies to develop research opportunities.

3-Study of Condensing Flows in a Micro-scale Channel with a Micro-element Array and Visual Techniques

S. Dessiatoun (UM), A. Shooshtari (UM), A. Goharzadeh (PI)

Objective: To investigate the fundamentals of the two-phase condensing flow phenomenon in a sub-millimeter microchannels.

Progress:

- Completed constant-quality pressure drop testing of condensation in microchannels with R-134a and R245fa.

- Designed a visualization microchannel condenser and ordered a high-speed camera.

Energy System Management

1-Robust Optimization of Petrochemical Systems

S. Azarm (UM), S. Al Hashimi (PI), T. Al Ameri (PI)

Objective: The objective of this study is to develop a framework for robust optimization the design of a distillation column, while considering the net profit effect at the plant level.

Progress:

- Developing a preliminary decomposed bi-subsystem multi-objective optimization model for a petrochemical system.

- Set up and tested the convergence of a multi-objective, multi-disciplinary optimization problem for the reactor-distillation model.

- Obtained some preliminary Pareto solutions to the reactor-distillation system optimization problem in the deterministic case.

- UM proposed a new and more efficient single-objective, single-level robust optimization method that considers feasibility robustness.

- Testing the proposed single-level robust optimization method using a single-objective distillation column optimization problem. Preliminary results indicate that the computational efficiency of this new robust optimization is significantly better than our previous method.

- PI submitted an abstract for a conference paper to the International Conference on Modeling, Simulation, and Applied Optimization (ICMSAO) in Sharjah 2009. The abstract was accepted.

- Developing two PI-UM joint papers: one in the area of combining robust optimization and sensitivity analysis, and the other on the new single-level robust optimization approach for single-objective optimization problems.

2-Dynamics and Control of Drill Strings on Fixed and Floating Platforms

B. Balachandran (UM), M. Karkoub (PI), Y. Abdelmagid (PI)

Objective: To develop and analytically and numerically study control-oriented models for drill strings; to investigate control of an under-actuated nonlinear system (drill string) with complex interactions with the environment; and to build a drill-string testbed at the PI/UM to test the theoretical findings.

Progress:

- Conducted fixed-point analysis and calibration of reduced-order models.

- Ran numerical investigations to determine how the motions are organized around the equilibrium position.

- Performed preliminary experiments to visualize rolling and bumping motions for different torque inputs.

- Presented a conference paper entitled “Drill-String Dynamics” authored by C. M. Liao, B. Balachandran, M. Karkoub, and Y. Abdelmagid at the Twelfth Nonlinear Vibrations, Dynamics, and Multibody Systems on June 1st in Blacksburg, VA.

- Preparing a journal article for submission to the ASME Journal of Vibration and Acoustics.

3-Developing Corporate Dashboards for Multi-Unit Firms:  An Agent-Based Approach

P. K. Kannan (UM), T. Al Ameri (PI)

Objective: To develop measurement systems that will incorporate the interconnectedness among the units and provide clear guidelines at the multi-unit level through dashboards that will enable the management of such complex systems and improve the understanding of such systems. The project will also enable managers to understand the implications of their various policies and decisions at the multi-unit level through the use of agent-based models.

Progress:

- Modified the research problem to one multi-plant problem within a firm to make the scope manageable.

- UM hired engineering student Phillipe Herve Kamaha to work on the project for the summer as well as for Fall 2008 and a high-school student, Wendell Shirley, for the summer 2008.

- Began initial research activities focused on the first objective of the project as follows: determining key performance indicators (KPIs) across firms and understanding how they are impacted by market forces and interactions.

- Modeling simple setups of the problem with 4 plants and a closed market of customers, and examining the impact of various control variables on meeting customer demand and on stock-outs.

4-Development of a Probabilistic Model for Degradation Effects of Corrosion-Fatigue-Cracking in Oil and Gas Pipelines

M. Modarres (UM), A. Seibi (PI)

Objective: To propose and validate a probabilistic model for health management of oil pipelines in process plants.

Progress:

- Modified models to account for stress, frequency, and temperature.

- Gathered data on a failed pipeline at the Ruwais Refinery in Abu Dhabi; applied it to model.

- Submitted purchase order to Cortest.  Equipment completion is expected August 25, 2008.

- Submitted papers to conferences and journals.

Introduction

In line with its mission to provide world-class education to the citizens of the United Arab Emirates in engineering and the applied sciences, the Petroleum Institute (PI) of Abu Dhabi, UAE, has entered into a long-term collaborative effort with the University of Maryland (UM) to enhance its own undergraduate, graduate studies/research, and continuing education practices. The PI was founded by Emiri decree in 2001 under the direction of H.H. Sheikh Khalifa bin Zayed Al-Nahyanand.  It is sponsored by a consortium of Abu Dhabi National Oil Company (ADNOC) and its international partners (Shell, BP, Total, and Japan Oil Development Company.

The PI and UM recognize the many potential benefits for both institutions that could result specifically from collaborative educational and research activities in the field of Energy Sciences and Engineering.  The Energy Education and Research Collaboration (EERC) has been created within the A.J. Clark School of Engineering at the University of Maryland to provide the administrative structure and academic oversight for these collaborative efforts.

During this sixth quarter of the EERC’s funded effort, partnerships between UM and PI faculty have been further solidified, and significant progress has been made on the collaborative research projects.

# Collaborative Activities

I.  	Collaborative research projects

At the  first EERC workshop, in January 2008, the PI expressed interest in consolidating the existing EERC projects into smaller groups of "Theme Teams" or “Research Thrust Areas.” The objectives of these research groups are to provide more coherency and closer collaboration between PI and UM faculty, to aid in identifying research areas of joint interest, and to set the stage for a smooth transition to the Phase II proposal and efforts.  As a result of discussions which ensued during and after the workshop between PI and UM faculty, three major areas of research were identified which does encompass all existing and possibly future Phase II projects. The listing of the projects in this quarterly report follows this categorization and consolidation and we will continue to format the reports in the same fashion for the next two reports of Q7 & Q8. Please note that the consolidation of the projects as presented and discussed below are meant as a guiding format and are by no means absolute or final. Further discussion between UM and PI faculty and administrators is needed and will hopefully lead us to a mutually cogent and productive, areas of research.

The three Thrust Areas are as follows:

- Energy Recovery & Conversion

This research area is focused on effective energy recovery and utilization in the oil and gas industry. The aim is to study and develop technologies and processes that efficiently recover energy from low-energy sources, or that convert energy at high efficiencies with low emissions, therefore safeguarding the environment. Such focus is demonstrated in projects such as the fuel cell project, which uses efficient petroleum extraction and production of CO2 streams for enhanced oil production; the waste heat project, which efficiently uses low grade waste heat using advanced cycles and process as well as photovoltaic solar energy collection and utilization; and the sulfur recovery project, which promotes clean energy recovery without the emission of trace acid gases and sulfur recovery from sulfur and acid-rich gas streams.

2.	Energy Efficient Transport Processes

The objective of this area of research is to study and develop energy efficient transport processes.  Projects in this area include modeling, fabrication and testing efforts on the development of polymer heat exchanger technology; development of micro-channel technologies for oil and gas processing as well as separation of the contaminants from the gas stream; and a systematic understanding of the role of turbulence and multi-component turbulent flow on the oil flow for oil recovery. UM offers expertise in understanding the complex turbulence phenomena for enhanced oil recovery by bringing unique research in two-phase multi-component turbulent flow. Understanding of this flow will assist in increased oil production.

- Energy System Management

This area of research concentrates on development of models and methods for condition-based monitoring, health prognostics, and decision support for managing energy systems that are used in oil, gas and petrochemical installations. The impact of the research in this project is expected to be in both engineering and business and across all stages of the energy production process: from exploration to production, transmission, storage, processing, and transportation. The proposed research has two interrelated and synergistic research threads: 1) Condition Based Monitoring and Prognostics (CBMP), and 2) Decision Support Systems (DSS). The objective of the CBMP thread is to develop models and methods for online monitoring, dynamics and control, and health prognostics and maintenance for energy systems. The DSS thread will focus on models and methods for infrastructure planning, estimating key performance indicators for multi-firm enterprises, and developing tools that can be used for multi-subsystem optimization and sensitivity analysis of oil, gas and petrochemical systems under risky conditions.

Progress on each research project is provided in detail in the body of the report.

# II. Additional Activities

Future Faculty Program (FFP)

In this quarter, UM embarked on a new activity and started a pilot project to improve the preparation of ADNOC scholars for their future academic positions at PI. This program called Future Facult Program (FFP) was delivered in June and July of 2008 to four UAE nationals (1 Ph.D. and 3 Ph.D. candidates). The participants were Dr. Hamad Karki, Mohamed Al Shehhi, Ebrahim Al Hijri, and Mohamed Chooka. This pilot workshop started June 2, 2008 for six weeks and included a series of seminars on teaching taught by Professor Sami Ainane. The research component of the program was taught by Professor Ashwani Gupta.  All four participants also enrolled in a class to fulfill the teaching practicum of the program, in which they actively participated in all aspects of teaching the course.

This program which is modeled after a similar program at UM, is to prepare PhD Candidates for academic careers and increase their competetiveness for acquiring academic positions at top universitie. The participants will be ADNOC scholars who are close to completing their Ph.D.s at UM or other institutions in the U.S. or elsewhere. The FFP consists of a sequence of training seminars, a teaching practicum, and a leadership component.

The seminars are provided by UM faculty with a proven record in the above areas, and participants will be asked to prepare the documents discussed, submit their material for review by the instructor, and revise their material in accordance with the review comments.

The leadership component of the program will be delivered in the Fall semester.

Among the topics to be covered in the FFP seminars are:

- Giving effective oral presentations

- Writing technical papers and reports

- Creating course content

- Managing a class

- Interacting effectively with students

- Accommodating various student learning styles

- Identifying research areas

- Writing grant proposals

# In the teaching practicum each ADNOC scholar will be teamed with a senior faculty member and provided with the opportunity to co-teach a course. The ADNOC scholar is expected to be involved in all aspects of the course: he will help in the development of the syllabus, teach some of the lectures, write and grade exams, and evaluate the students.  In all these activities, there will be close supervision by the faculty mentor. Typically, the teaching practicum will be completed in one semester for ADNOC scholars at UM and in a six-week concentrated format for outside participants.

For the leadership component to the FFP, participants are envisioned to take a leadership workshop or short-course (based on the current certificate programs taught at the R. Smith School of Business and MTECH of the Clark School of Engineering) and have a chance to shadow a prominent University or industry executive.

# Student Exchange

# Five PI seniors from four different departments spent six weeks as interns at UM in July and August 2008, in partial fulfillment of their curriculum requirements.

Following is a list of the students and the professors they worked for. The students had a productive six weeks at UM working on their projects, visiting UM labs such as the nuclear reactor facility at UM, the capital’s museums such as the famous Air & Space Museum, and the campuses of MIT and Harvard in   Cambridge, Massachusetts. All students will be submitting a report on their internships and expect to receive a grade from their PI advisors. All of the UM professors have invited their interns for a longer stay to continue working on their research topics.

| Student | UM Professor | Professor’s Email |
| --- | --- | --- |
| Mamoud Adi, MEEG | Dr. S. K. Gupta | skgupta@UM.edu |
| Mohamed Al Hebsi, PEEG | Dr. Amir Shooshtari | amir@UM.edu |
| Mohamad Tamer Chaklab, ELEG | Dr. Mia Yu | mmyu@UM.edu |
| Amro El-hag, CHEG | Dr. Serguei Dessiatoun | ser@UM.edu |
| Bakeer Bakeer, MEEG | Dr. Greg Jackson | gsjackso@UM.edu |

II.  	EERC faculty telephone conferences

Many projects continued to have regular weekly (Thermally Enhanced Polymer Heat Exchanger for Seawater Applications) or biweekly phone conferences (Robust Optimization of Petrochemical Systems and Waste) between the collaborators at UM and PI.

III.	Joint monthly meetings via video-conference

Joint monthly meetings have continued as an effective means for faculty members to present their research to the entire group. The last video-conference (VC) was conducted on April 30, 2008. The agenda of the meeting was as follows:

| Agenda EERC Video Conference Call – April 30, 2008 |
| --- |
| Time | Presentation |
| 9:00 | Welcome – UM Dr. Bar Cohen |
| 9:03 | Welcome – PI Dr. Ohadi |
| 9:06 | Welcome & announcements—Dr. Azar Nazeri |
| 9:15 | “Progress on Experimental Testing of Solid Oxide Fuel Cell for EERC Project," Greg Jackson, Paul Jawlik |
| 9:35 | High Efficiency Solar Cooling Technology, R. Radermacher, Ali Alalili |
| 9:55 | Wrap Up – Nazeri |

IV.	PI Distance Learning Students

The table below shows a list of students currently working on EERC projects, their advisors at UM, and the PI collaborating faculty.  The table also includes the degrees sought and the students’ funding sources.

| UM Professor | PI Professor | Student | Degree | Funding Source |
| --- | --- | --- | --- | --- |
| Modarres | Seibi (TCM) | Mohamed Chooka | Ph.D. | ADNOC |
| Balachandran | Karkoub (TCM)*, Abdelmagid | Chien-Min Liao | Ph.D. | EERC |
| Dessiatoun | Ohadi, Goharzadeh, Kubo | Mohamed Alshehhi | Ph.D. | ADNOC |
|  |  | Ebrahim Al-Hajri | Ph.D. | ADNOC |
|  |  | Elnaz Kermani | M.S. | EERC |
| Azarm | Al Hashimi, Al Ameri | Genzi Li | Ph.D. (graduated 8/2007) |  |
|  |  | Wei Wei Hu | Ph.D. | EERC |
| Gupta | Sassi | Hatem Selim | Ph.D. | EERC |
| Bar-Cohen | Rodgers, Abdala | Juan Cevallos | M.S. | EERC |
|  |  | Patrick Luckow | M.S. | EERC |
| Radermacher | Al Hashimi, Rogers, | Ali Alalili | Ph.D. | ADNOC |
|  |  | Amir Mortazavi Chris Somers Paul Kalinowski | M.S. M.S. M.S. (graduated 9/2007) | EERC EERC Mannheim |
| Jackson | Eveloy (TCM), Almansoori (TCM)* | Paul Jawlik | M.S. | EERC |
|  |  | Siddharth Patel | M.S. | EERC |

* = To be assigned

TCM = Thesis Committee Member

CA = Co-advisor

# At this point we have seven Ph.D. students and seven M.S. students at UM.

# Collaborative Publications

Invention Disclosure:

Professor Radermacher has recently filed for an “Invention Disclosure” called "Advanced Solar Cooling Technology.” Mr. Ali Alalili, a UAE national and a current Ph.D. student at UM is the co-inventor.

# Journal Articles

1.	Mohamed Sassi and Ashwani K. Gupta, “Sulfur Recovery from Acid….” accepted, American Journal of Environmental Sciences.

2.	Yunho Hwang, Reinhard Radermacher, Ali Al Alili Isoroku Kubo, “Review of Solar Cooling Technology,” accepted, International Journal of HVAC&R.

3.	Serguei Dessiatoun, Sourav Chowdhury, Edvin Cetegen, Ebrahim Al-Hajri, Michael Ohadi, “Studies of Condensation of Refrigerants …” Submitted to Journal of Heat and Mass Transfer, September 2007.

4.	Li, G., M. Li, S. Azarm, N. Al Qasas, T. Al Ameri, and S. Al Hashimi, “Improving Multi-Objective Genetic Algorithms…” submitted to Structural and Multidisciplinary Optimization.

5.	M. Chookah, M. Nuhi, M. Modarres, and A. Sebi, “Development of a Probabilistic Physics of Failure Model of Compressed Natural Gas Bus Cylinder” submited to Reliability Engineering & Systems Safety Journal.

# Conference Presentations

- Sassi, M., BenRejab, S., and Gupta, A. K., “CFD Simulation of Combustion…” 5th Mediterranean Combustion Symposium (MCS-5), Monastir, Tunisia, September, 2007.

- Serguei Dessiatoun, Sourav Chowdhury, Edvin Cetegen, Ebrahim Al-Hajri, Michael Ohadi, “Studies On Condensation Of Refrigerants…” presented at the 5th International Conference on Nano, Micro and Minichannels, June 2007, Puebla, Mexico.

- A. K. Gupta and M. Sassi, “Simulations of Claus Furnace…” Invited Keynote International Workshop on Advances in Combustion Science and Technology, India, Jan 2008.

- Bar-Cohen, A., Rodgers, P., Cevallos, J.G., "Application of Thermally Conductive Thermoplastics to…Heat Exchangers," accepted, 5th European Thermal-Sciences Conference, May 2008, Eindhoven, the Netherlands.

- M. Chookah, M. Nuhi, M. Modarres, and A. Sebi, “Development of a Probabilistic Model for ….Oil Pipelines…” submitted to Probabilistic Safety Assessment (PSA'08) conference.

- .P. Luckow, Bar-Cohen, P. Rodgers, J. Cevalles, "Energy Efficient Polymers for Gas-Liquid Heat Exchangers” to be presented at Energy Sustainability 2008 Conference, Jacksonville, Fl, August 2008.

- P. Kalinowski, Y.  Hwang, R. Radermacher, S. Al Hashemi, P. Rogers, “Waste Heat Powered Absorption Refrigertion Sytem the LNG Recovery Process” accepted for publication in Sorption heat Pump Conference, September 23-26 2008, Seoul.

# Quarterly Report Schedule

The following are the revised dates for the submission of future reports.

| Quarter 2 | June 30, 2007 |
| --- | --- |
| Quarter 3 | September 30, 2007 |
| Quarter 4 | February 14, 2007 |
| Quarter 5 | April 15, 2008 |
| Quarter 6 | June 30, 2008 |
| Quarter 7 | August 30, 2008 |
| Quarter 8 | October 31, 2008 |

Individual Progress Reports

A. Educational/Research Activities

Visit to GASCO and ADGAS May 4 – May 8, 2008 Dr. Serguei Dessiatoun Mohamed Alshehhi Ebrahim Al-Hajri

Agenda

- Sunday (May 4)

  - 8:00 am -10:00 am

    - Meeting with ADGAS company for possible research opportunity

  - 11:00 am - 2:00 pm

    - Meeting with GASCO company for possible research opportunity

- Monday (May 5)

  - 10:00 am - 5:00 pm

    - Visit GASCO oil field (HABSHAN Plant) to become familiar with new projects in gas process

- Tuesday (May 6)

  - 9:00 am - 10:00 pm

    - Meeting with ADNOC

  - 11:00 am - 1:00 pm

    - Visit Petroleum Institute to follow up with EERC projects

  - 1:30 pm - 3:00 pm

    - Follow up with security passes to visit ADGAS oil field (DAS Island)

- Wednesday (May 7)

  - 8:00 am - 3:30 pm

    - Visit ADGAS oil field (DAS Island) become familiar with new projects in cryogenic applications on gas process

- Thursday (May 8)

  - 10:00 am - 1:00 pm

    - Meeting with MASDAR to become familiar with their projects in renewable energy

Objective

The objective of the visit was to explore research opportunities in the oil and gas industry in the UAE and to define application problems that can be solved with innovative and creative existing technologies.

Introduction

For decades, the oil and gas industry has been using conventional processes and process equipment. As a result, only minor efficiency improvements have been reported on the processes and components. Little has been done to introduce new and innovative research and technologies to this industry where substantial room for improvements exists.

The major purpose of this visit was to identify research opportunities for future EERC projects. Two ADNOC companies, GACSO and ADGAS, were supportive of our purpose and have shown interest in future research.

Identified Applications in the Oil/Gas Industry

ADGAS

Our team met with processing and mechanical engineers from ADGAS in both the main office in Abu Dhabi and at Das Island. The two teams discussed the possibilities of research in separation of solid and liquid particles from natural gas flows coming from oil wells. These solid and liquid particles cause damage to the compressors if they are allowed to enter the ADGAS plant. Currently, ADGAS returns the flow to the neighboring plant (ADMA) to filter the gas flow. The process is costly because as the gas flow is returned back to ADMA, the ADGAS plant has to keep operating at reduced loads until the filtered gas flow is returned to ADGAS again. The technology developed in Mohamed Al-Shehhi’s EHD separation project will solve many separation problems, particularly separation of fine liquid and solid particles.

Another possible research opportunity that we have identified with ADGAS is to improve the performance of the cryogenic column and minimize its size by using microchannel heat exchangers. The existing cryogenic column is used to liquefy natural gas to be stored and then shipped to customers around the world. However, the unit is the largest and most complicated column in ADGAS. The unit is so complicated that ADGAS has to call the manufacturer to perform all scheduled maintenance on the unit. Current research in this field indicates that the cryogenic column could be reduced in size, improved in performance. An easy-to-maintain cryogenic unit could also be designed.

GASCO

In our visit to GASCO, we were granted a visit to Habshan field. We discussed with several engineers issues facing GASCO in terms of processing natural gas. We learned from these discussions that GASCO is concerned about sulfur removal from natural gas. We also learned that GASCO is expanding its current capabilities by four times due to the high demand from the Abu Dhabi government for natural gas to be used in power generation. This high demand for natural gas has driven GASCO to explore more gas wells, which has led GASCO to natural gas wells with high sulfur concentrations, up to 23%.

The current sulfur removal process is to mix natural gas with Amine solution in a bulky vertical column. Multiple stages are used for natural gas with high sulfur concentration due to the inefficient chemical reaction in a single column. The equipment used for sulfur removal is very expensive, and adding multiple stages adds to the capital cost. Therefore, our team has proposed to use microchannel reactors to remove sulfur from natural gas. Recent studies in the literature show that micro-reactors are highly efficient due to the large area-per-volume of microchannels, which enhances the resident reaction time. In addition, the mixing ratio in microchannels can be precisely controlled, and the reaction temperature can be easily controlled too.

Summary

Our visit to both ADGAS and GASCO provided our team with inside information on gas processing and allowed us to explore possible areas of research. We have seen substantial research opportunities, which have generated several research proposals. These proposals will be soon submitted to PI through the EERC research program as future possible research in the oil and gas industry.

B. Research Projects Energy Recovery and Conversion Projects

Force-Fed Cooling of Photovoltaic Arrays for High-Efficiency Solar Energy Conversion Systems UM Investigators: Dr. S. Dessaitoun, Dr. A. Shooshtari GRA’s: E. Kermani, PI Investigator(s): Dr. M. Ohadi Start Date: March 2007 Report Date: 30 June 2008

1.	Objective/Abstract

The proposed project will create, based on a survey of available literature, a database on the available cooling techniques for high heat flux solar concentrator arrays necessary for efficient conversion of solar energy to electric power. The typical cooling load necessary for optimum radiation concentration and optimum photovoltaic conversion efficiency will be identified, and a novel force-fed cooling technique that has been developed at UM will be applied to contain this cooling load. An experimental prototype and associated setup will be designed and fabricated to verify the feasibility of this concept and the capacity for cooling by this technique. Based on these experimental results, the radiation concentration levels acceptable to this cooling capacity will be redefined. The type of fluid and its flow rate, the temperature of the surface where solar radiation is incident, and the uniformity of temperature on this active area are the main issues that will be addressed in this proposed project. The scalability of this technique for uniform cooling of industry-scale extended area panels will be a guiding parameter for the design and development of the heat exchanger prototype proposed here.

2.	Deliverables for the Completed Quarter

- Packaging

Three complete samples consisting of bonded microchannels and a manifold with heater have been constructed and packaged in the packaging setup with inlet and outlet pipes and a power supply pad.

- Wirebonding

Heaters have been wirebonded on three samples with the wirebonding machine at the Center for Nanophysics and Advanced Materials (CNAM) at the University of Maryland. As a result, gold can be connected to the power supply to act as a resistance and heat up.

- Experimental Setup

An open loop experimental setup consisting of the test section, a DC power supply, measurement devices, and a data acquisition system has been made to test the performance of the samples with water as a refrigerant. Pressure for the system is supplied from a nitrogen tank to circulate water in the system at different pressure levels.

- Experimental Procedure and Preliminary Test Results

The performances of the samples have been tested under different input power levels in an open loop system.

3.	Summary of Project Activities for the Completed Quarter

- Packaging

Epoxy glue was used around the perimeter of the sample to fix it in the packaging test section, and two springs were used to keep the sample in place. Two thin rubber sheets used under and above the sample provide a smooth contact between the sample and the G10 package. The samples were then ready for wirebonding. Two pipes connected to inlet and outlet holes for refrigerant to pass through the sample. Three K-type thermocouples were used to find the temperature on the heater surface, at the inlet, and at the outlet. Figure 1 shows the packaged sample.

Figure 1.  Packaged sample with thermocouples and electrical connections

- Wirebonding

The wirebonding machine at the Center for Nanophysics and Advanced Materials (CNAM) was used to make interconnections between the heater and the solder leads. In the samples aluminum wire was attached to the gold heater at ambient temperature, and a wedge bond was formed by pressure and vibration energy. On each sample, a minimum 10 wirebond was formed on each side to prevent wire burnout at high-current tests. Figure 2 demonstrates a sample with wirebond on both sides and surface thermocouples.

Figure 2. Sample with wirebond and surface thermocouples

- Experimental Setup:

The test section consists of the packaged sample with three K-type surface thermocouples: one thermocouple each at the inlet and outlet, and one thermocouple to find the zero temperature. The inlet was connected to a reservoir of distilled water and the outlet was connected to another reservoir to find the flow rate. Flow rate was measured by the division of weight of water by specific time. A nitrogen tank was connected to U type pressure gage device to measure the pressure applied to the system.

A programmable DC power supply (Sorenson, Inc., model #DLM150-4) provided power to the heater.  The power supply was controlled by a data acquisition system (BenchLink Data Logger System) programmed on a personal computer through a general programming interface bus DAS card. Data was acquired through six thermocouples, a programmable power supply and BenchLink Data Logger System. The experimental setup is shown in Figure 3, and a closer view of the test sample is shown in Figure 4.

Figure 3.  Experimental setup

Figure 4. Experimental sample

- Experimental Procedure and Preliminary Test Results

The first step in running the experiment was to calibrate the thermocouples. All six K-type thermocouples were calibrated with the RTD thermocouple in a chiller with a temperature range between 10 0C and 50 0C. One sample curve for one surface thermocouple is presented in Figure 5. The next step was to calibrate the heater resistance at different temperatures. For that, heated distilled water was run through the system, and with real time data acquisition card surface temperatures, inlet and outlet temperature and resistance were measured. Two calibration curves were plotted: the first, heater resistance versus average inlet and outlet water temperature, and the second, resistance versus average surface temperature. Both curves are plotted in Figure 6.

Figure 5. Calibration curve for one of the surface thermocouples

Figure 6. Calibration curve of the heater resistance with two methods

In the experiments the DC power supply was started at about 8 W and was increased every 10 W to about 58 W. At each power level, tests at six different pressure drops were performed. All the data from thermocouples and supplied power were recorded with the BenchLink Data Logger System and were exported to Microsoft Excel.

Figure 7 demonstrates the results for pressure drop versus flow rate for a sample whose channel width was 40 µm and the refrigerant was distilled water. As can be seen, the graph is linear. In Figure 8 heat transfer coefficient versus flow rate is plotted. The maximum heat transfer coefficient at 1.22 gr/s flow rate was 57500 W/m2K. In Figure 7 surface temperature of the heater versus power level at different pressure drops is plotted. The maximum temperature of the surface was about 48 0C.

Figure 7. Pressure drop versus flow rate

Figure 8. Heat transfer coefficient versus flow rate

Figure 9. Surface temperature versus input power at different pressure drops

4.	Difficulties Encountered/Overcome

- There were some difficulties in wirebonding.

- During the experiment, the flow rate decreased, which could be due to blockage; therefore, a filter was used.

5.	Planned Project Activities for the Next Quarter

- Continue packaging more samples.

- Run the experiment and produce data.

Appendix

Justification and Background

The abundance of solar energy in Middle Eastern countries provides significant opportunity for development of eco-friendly power generation technologies essential in the modern world. Several decades of research have produced significant knowledge and innovations in design of economically viable, silicon-based photovoltaic (PV) panels and mirrors for concentration of solar radiation and its conversion to electric power. One of the outstanding challenges in this field is the active and uniform cooling of these large-area, high heat flux solar concentrator arrays, because the conversion efficiency is heavily dependent on device temperatures and drops significantly with an increase in temperature. If an appropriate cooling technique is possible, these solar panels will become more effective and commercially viable, which could pave the way for a rapid transition of the current power generation industry towards eco-friendly alternatives for local use, increasing currently available export resources and also creating a base for future energy export technologies.

Among several techniques enabling the use of solar energy, solar photovoltaics exhibit significant potential for economic and eco-friendly process for power generation industry. After five decades of research and development, photovoltaic energy production is growing exponentially across global markets. Northern Europe and Japan currently lead in the research and commercialization of PV technology. Solar panels on the facades and roofs of commercial and residential buildings are common pictures in these countries, where solar energy is used in every aspect of utilities, including heating, cooling and lighting needs. Most of those countries have climates with high cloudiness and low intensity direct sunlight, limiting the energy conversion effect. The static PV arrays that work well with dispersed sun light have already been developed. These cells are used in the static arrays and are simple silicon-based cells with poor conversion efficiency.

Progress has been made on decreasing the cost and consumption of solar array material by using thin film PV cells. Daytime tracking of the sun by sensor-enabled drives offers significant benefit in increasing solar array effectiveness. Also, in the recent decade, works have been published on the concentration of solar radiation by parabolic mirrors and lens structures onto smaller sized solar panels, which greatly reduce the cost and increase conversion efficiency by increasing specific power. The US Department of Energy has recently reported exceeding 40% efficiency level with concentrated arrays compared to 8.5% for static arrays. The efficiency of the array increases with the level of concentration if array temperature is kept at a low constant value. The same low array cost compared to the total system cost will allow updating to current technology. The radiation concentration up to 80,000 times is theoretically possible but currently just 400 to 500 times is feasible due to high heat dissipation requirement on the PV concentrator arrays.

Approach

UM-side participation

- Conduct extensive literature survey on PV radiation concentrators. Summarize available cooling technologies for these arrays with notes on their cost, size and other scalability issues.

- Evaluate cooling loads, taking into account recent advances in radiation concentration technologies and conversion efficiencies.

- Develop a force-fed heat exchanger prototype capable of rejection of this expected heat flux. Explore the possibility of MEMS fabrication techniques for creating micro-grooves integrated with solar panels. Also identify possible fluid choices and pumps to meet the demand.

- Conduct experimental study on force-fed-based single- phase processes to determine cooling capacity.

- Based on outcome of experiments, design, fabricate, and test a complete PV converter and cooler package in the field.

- Make recommendations for a radiation concentration that is commensurate with this thermal management technique.

PI-side participation

- Provide information and symbiotic assistance to the UM team regarding current concentrator designs, available cooling techniques and expected heat loads.

- Prepare a solar concentrator to be packaged with UM-made heat exchanger for final testing.

- Corroborate UM testing of the concentrator and cooling element in UAE desert conditions

- Provide contributions to the preparation of final project report and recommendations.

Two-Year Schedule

UM-side participation

Year 1

- Literature review and summary

- Design of force-fed cooler for PV array

- Fabrication of experimental prototype and experimental loop

Year 2

- Finalized experimental setup

- Experimental results

- Recommendations for optimized PV converters with respect to developed cooling capacity

- Final report

PI-side participation

Year 1

- Input on literature review and summary

- Discussion and assistance in design of test prototype

- Concentrator design

Year 2

- Discussion and assistance in experimentation

- Concentrator fabrication or participation in fabrication

- Testing of concentrator and cooling system in UAE conditions

- Input on final report and recommendation

Key References

- Muresan, C., Menezo, C., Bennacer, R., Vaillon, R., ”Numerical Simulation of a Vertical Solar Collector Integrated in a Building Frame : Radiation and Turbulent Natural Convection Coupling,” Heat Transfer Engineering, vol. 27(2), pp. 29-42, 2006.

- Konnttinen, P., Lund, P.D., “Thermal Stability and Moisture Resistance of C/Al2O3/Al solar absorber surfaces,” Solar Energy Materials and Solar Cells, vol. 82, pp. 361-383, 2004.

- Ramanathan, K., Keane, J., Koufi, R., “Properties of High-Efficiency CIGS Thin-Film Solar Cells,” Proceedings of 31st IEEE Photovoltaics Specialists Conference and Exhibition, Lake Buena Vista, FL, January, 2005.

- Han, D., “Microscopic Mechanism of Staebler-Wronski Effect in a-Si Films and High Efficiency Solar Cells,” Final Subcontract Report prepared under subcontract no. ADJ-1-30630-09, National Renewable Energy Laboratory, 2004.

- Bakirov, M., “Photoelectric and Radiation Characteristics of Silicon Solar Cells at High Illumination Levels and Elevated Temperatures,” Semiconductors, vol. 31(5), pp. 439-440, 1997.

Sulfur Recovery from Gas Stream using Flameless and Flame Combustion Reactor UM Investigators: Prof. Ashwani K. Gupta UM GRA’s: Hatem Selim PI Investigator(s): Prof. Mohamed Sassi Student: Sami Ben Rejeb Start Date: October 2006 Report Date: 15 July 2008

1.	Objectives/Abstract

The main objective is to obtain fundamental information on thermal process of sulfur recovery from sour gas by conventional flame combustion as well as flameless combustion, using numerical and experimental studies. Our ultimate goal is to determine optimal operating conditions for sulfur conversion. Therefore, an experimental study of the flameless versus flame combustion processes of the Claus furnace is proposed. In the study we will explore the operating conditions and perform exhaust gas analyses of both flame and flameless modes of reactor operation in sought of attaining enhanced sulfur recovery.

Specific objectives are to provide:

- A comprehensive literature review of the existing flame combustion process for sulfur removal with special reference to sulfur chemistry.

- Near isothermal reactor conditions and how such conditions assist in the enhanced sulfur recovery process.

- CFD simulation of the flame and flameless combustion in the furnace.

- Design of a flameless combustion furnace for experimental verification of the numerical results.

- Measurements and characterization in the flameless combustion furnace that utilizes high temperature air combustion principles.

- Experiments with different sulfur content gas streams using the flame and flameless combustion furnace modes of operation.

- Determination of the product gas stream for evaluation of sulfur recovery in the process

2.	Deliverables for the Completed Quarter

- Further reduction of our previously introduced 20-reaction pathway mechanism. Three reactions have been eliminated, and rational assumptions of pre-exponential factors, activation energies, and temperature exponents were made for the remaining reactions. The resulting 17-reaction mechanism has been tested against two detailed mechanisms at different sets of operating conditions.

- Design and fabrication of an updated experimental facility capable of replicating Claus-process conditions in both the flame and flameless modes with minimized heat losses. Sophisticated controls were implemented for accurate and safe operation of the facility. The test rig also comprises means for temperature measurement, capture of recovered sulfur, and gas sampling for validation of our numerical calculations of chemical kinetics

- Preliminary tests of the updated facility to verify the homogeneity of high-temperature environment needed for the flameless combustion mode of sulfur recovery.

3.	Summary of Project Activities for the Completed Quarter

Executive Summary

During the reported quarter, progress continued in the areas of experimental facility design and modification, experimental tests, and chemical-kinetics calculations. In this report we describe an updated experimental facility designed and fabricated to study both flame and flameless modes of sulfur recovery. The high-temperature conditions of the Claus process were easily achieved with minimum losses and adequate homogeneity. The H2S injection mechanism utilized was the one recommended in our previous report. Sophisticated controls were implemented to ensure accurate and safe operation. The facility is also equipped with a means of temperature scanning and gas sampling and analysis. Moreover, temperature scanning along the hydrogen sulfide reactor centerline has been performed under different conditions of fuel/oxygen injection while keeping the ratio stoichiometric in order to ensure that we could achieve the required temperature homogeneity and to assure that the required temperature levels were achievable.  Finally, a simplification for the reduced mechanism, introduced in a previous report, has been done based on extensive literature review and elimination for the reactions with marginal effects. We ended up with a 17-reaction mechanism, which has been compared with two detailed mechanisms and has shown good agreement with them.

Progress

4.1	Experimental Facility

Our experimental facility at the UM Combustion Laboratory has been designed and fabricated to allow for the investigation of both flame and flameless modes of sulfur recovery. The test rig comprises two reactors, a CH4/O2 reactor followed by an H2S/O2 reactor, as shown schematically in Figure 1. In the flameless mode of operation, CH4 and O2 are injected into the methane reactor in chemically correct proportions through a coaxial injector. The combustion of methane and oxygen yields hot products that provide the necessary high-temperature environment for flameless reaction of hydrogen sulfide in H2S reactor. The amount of oxygen needed to satisfy the Claus-process stoichiometry is accounted for and injected along with oxygen needed for methane combustion.

Figure 1. A schematic diagram of the test rig

The two reactors of the test rig are connected through a 4-legged cross-connection. While two legs connect the reactors, the other two legs are utilized for H2S injection. Following the recommendations of our last report, the injection tubes of H2S extend up to few injection-diameters from the test-rig centerline to allow for traverse injection at centerline. Based on the findings of the last report, this injection geometry is expected to have the advantages of good mixing and minimum radical quenching and heat loss, as compared to the previously studied injection geometries.

To minimize heat loss from test rig, the interior of entire rig was coated with zirconia (ZrO2) insulation. Zirconia has a very low thermal conductivity of 0.2 W/m.K and withstands temperatures as high as 2500 K. Using considerable zirconia thickness, the 1600-K optimum temperature of sulfur recovery at peak efficiencies was easily achieved at half the maximum flow rates of reactants the facility can safely endure. The 3-inch methane reactor was coated by a ½-inch thick zirconia layer over its entire length of 9 inches, allowing for an enclosed volume of 2 inches diameter. The reactor diameter and insulation thickness have been carefully chosen to simultaneously increase the resistances to convective heat transfer from hot gases to zirconia and from the reactor exterior to ambient surroundings. The hydrogen-sulfide reactor, on the other hand, is 12 inches long, has an inner diameter of 1 inch, and comprises a zirconia tube of 1-inch OD and ½-inch ID. The dimensions of the  H2S reactor and its zirconia tube have been chosen to (a) match geometries of previous experimental research from the literature and (b) decrease heat losses to ambient surroundings.

The operation of test rig is controlled through a sophisticated control board; see Figure 2. The flow rates of CH4, O2, and H2S are controlled by means of digital, normally-closed flow meters/controllers. Independent of upstream pressure, the controllers are capable of achieving their set points with an accuracy of 0.15% of full-scale within a 5-second response time. The full-scale flow rates of reactants are 10, 20, and 1 lit/min for CH4, O2, and H2S, respectively. The individual set points are set remotely through digital DC power sources, which provide the necessary electromotive forces across the set-point terminals of the controllers. The sensitivity of each power source is 0.1 V, which divides the 5-V set-point range of each controller into 50 increments. When no set point is provided, the controllers shut off the flows completely to prevent leakage of any non-combusted gas into the test rig.

Ignition of the reactants is attained safely inside the test rig by means of a stun gun. The gun (hidden behind the control board in Figure 2) creates a 100-kV electrical potential, enough to generate a spark across a 1.5-inch air gap. This potential is harnessed and channeled through electrical wiring to two ceramic-coated electrodes inserted into the upstream section of the methane reactor, as seen in Figures 1 and 3. The tips of the electrodes approach each other at the reactor centerline, leaving a gap of 0.25 inches. The generated spark is approximately 0.5 inches above the exit of CH4/O2 coaxial burner. This choice of spark length and location ensures that the spark strikes a locally ignitable mixture of CH4 and O2, so that the reactants ignite shortly after leaving the injector without any accumulation of unburned combustible mixture within methane reactor. The initiation of sparking is managed through the ignition switch within the facility control board. The switch closes the power-input circuitry of the stun gun, which results in spark generation; see Figure 4.

Figure 2. Photograph of test rig

Figure 3. CH4/O2 burner and ignition system

Figure 4. Facility control board

Temperature measurement can be performed along the centerline of the H2S reactor by means of an 18-inch-long type-K Omega® thermocouple; see Figures 1, 2, and 5. The thermocouple is connected to a temperature display unit calibrated to give temperature value directly for K-type thermocouples and to internally simulate zero-junction. The thermocouple wiring is protected inside a 1/8-inch metal tube filled with isolative material. The entire thermocouple assembly is movable along the H2S-reactor centerline inside a bored-through Swagelok® fitting to ensure concentricity while scanning the axial temperature distribution.

At the end of H2S reactor the gases leave through a ½-inch-diameter, 18-inch-long flexible connection that connects the test rig to the gas-conditioning and sampling system. This system starts with a 3-inch-diameter, 12-inch-long tank for capture of recovered sulfur. The dimensions of the flexible connection and sulfur-capture tank were chosen to ensure that the gases leaving test rig are cooled down to about 500 K, which is an adequate temperature for sulfur capture, where it is in liquid form and has the lowest viscosity. The sulfur-capture tank is internally equipped with multiple baffles to reduce the velocity of incoming flow and facilitate better capture efficiency of sulfur from gas stream, as sulfur deposits on baffles and tank inner walls. As the gases leave the tank sulfur-free, they are forwarded to another tank filled with an aqueous alkaline solution, where the acid-forming gases, like SO2, CO2, and any residual H2S, get neutralized. The effluent gas, if any, exiting the alkaline-solution tank contains primarily hydrogen and is discharged into the lab exhaust system. A small portion of the gas stream is sampled between the sulfur-capture and alkaline-solution tanks for analysis in an Agilent® gas chromatograph. A water trap at the beginning of sample line captures most of the sample moisture, before the sample passes through an ice-cooled condenser that removes the remaining moisture. The dry sample is then fed to the gas chromatograph for analysis.

Figure 5. Gas conditioning and sampling system

4.2 Experimental results of temperature scanning along H2S reactor center line

In this section we will focus on the temperature distribution along the hydrogen sulfide reactor where the facility was tested at different reactor temperatures to allow us to study the homogeneity of the temperature inside the reactor. The test was performed under stoichiometric conditions, and the reactor temperature was changed by increasing the air and fuel accordingly to reach the required temperature. The test was performed without any H2S injection; it was only for the CH4 and O2 in order to test how homogeneous the temperature was, and if it could afford the required temperatures or not. The temperature was measured along the reactor centerline by a step of 0.5 inch (1 flow-diameter). It was found that the maximum length required to reach a constant temperature along the reactor was less than 5 inches (10 flow-diameters), so the figures will be 5 inches along the reactor length.

The temperature is homogeneous along the reactor centerline up to a certain extent; however, the higher the fuel flow rate and reactor temperature, the higher the temperature loss along the reactor centerline. Despite this fact, the temperature variation at the high flow rates is still acceptable. For instance, at the 4.6 lit/min (2.45 kW) methane flow rate, the asymptotic temperature was 1573K and the maximum temperature in the reactor was 1608K (2.2% deviation).

Figure 6. Axial temperature distribution along the hydrogen sulfide reactor centerline

4.3 The reduction mechanism for hydrogen sulfide oxidation

Previously, we have shown the importance of obtaining a reduced mechanism for the hydrogen sulfide/oxygen reactions, as it will enable us to use the commercial simulation software packages in simulating the reactive cases more efficiently, and it will reduce the divergence chances to a higher extent. Moreover, we provided a 20-reaction mechanism that contains the main reactions of the H2S/O2 reaction.  In this report we will work on the reduction of the mechanism introduced before, based on what has been mentioned in the literature and some rational assumptions for the activation energy, pre-exponential factor, and temperature exponent. It has been proven that the following reactions are insignificant in the H2S/O2 reaction compared to other reactions, so they have been excluded from the reduced mechanism.

SO2+ OH (HOSO+O

SO+SO ( SO2+S

S2+O(SO+O

These reactions are not significant in the reaction mechanism; therefore, we end up with the following pathway mechanism:

Figure 7. The 17-reaction reduced mechanism (left), the 20-reaction

reduced mechanism (right).

Next, we worked on defining the parameters of the reaction rate constants (activation energy, pre-exponential factor, and temperature exponent) to rationalize this reduced mechanism and compensate the effect of the reduced reactions. Table (1) lists the reduced mechanism parameters. Recall that the reaction rate constant (K) is calculated from the following equation:

Table 1. The reduced mechanism for H2S/O2 reaction

| # | Elementary Reactions |
| --- | --- |
| 1 | H2S+M (S+H2+M |
| 2 | H2S+H(SH+H2 |
| 3 | H2S+O(SH+OH |
| 4 | H2S+S(HS2+H |
| 5 | SH+O(H+SO |
| 6 | SH+OH(S+H2O |
| 7 | SH+HO2(HSO+OH |
| 8 | S+O2(SO+O |
| 9 | SH+O(S+OH |
| 10 | H+SO2+M(HOSO+M |
| 11 | HS2+H(S2+H2 |
| 12 | HS2+O(S2+OH |
| 13 | HS2+S(S2+SH |
| 14 | SH+S(S2+H |
| 15 | SO+O2(SO2+O |
| 16 | HSO+H(SH+OH |
| 17 | HOSO+O2(HO2+SO2 |

Figure 8 shows the Arrhenius plot for the 17 reactions separately at different temperatures from 800K up to 2000K.  The plot is a semi-log plot, which provides as much detail as possible for the reaction rate constant change with temperature. We can notice that some reactions are very sensitive to the temperature variation, such as reaction 1, which is reasonable where this reaction is responsible for the dissociation of hydrogen sulfide. On the other hand, some reactions are not sensitive to the temperature change, such as reaction 16, and this is because of the high reactive tendency of the reactants (HSO and H), which are both radicals.

In order to verify the success of this reduced mechanism we will compare it with two detailed mechanisms and see whether it agrees with them.

Leeds University mechanism

The mechanism by Leeds University1 contains 116 elementary reactions.  The comparison will be held at different temperatures 1400-1800 K with steps of 100K. The stoichiometry of inlet reactants is that of the Claus process. This comparison will be applied on the main species only, i.e., H2S, S2, SO2, and O2

Figure 8. Arrhenius plot for the 17 reactions used in the reduced mechanism.

Figure 9 shows that the behavior of oxygen obtained by the reduced mechanism is in good agreement with the detailed one, especially at high temperatures.

Figure 9. Oxygen mole fraction at different temperatures with reduced mechanism (left), and Leeds mechanism1 (right)

Figure 10 presents the behavior of H2S at different temperatures. Both mechanisms give almost the same asymptotic value; however, the beginning of the combustion is different.

Figure 10. Hydrogen sulfide mole fraction at different temperatures with reduced mechanism (left), and Leeds mechanism1 (right)

Figure 11 gives the behavior of SO2 at different temperatures. It is obvious that the asymptotic values are pretty coherent at the high temperatures. One the other hand, the low temperatures, especially 1400K, required more time to reach the asymptotic value.

Figure 11. SO2 mole fraction at different temperatures with reduced mechanism (left), and Leeds mechanism1 (right)

Figure 12 shows the effect of changing the reactor temperature on S2 mole fraction. The agreement between the reduced and Leeds mechanism is still much better at the high temperatures.

Figure 12. S2 mole fraction at different temperatures with reduced mechanism (left), and Leeds mechanism1 (right)

Tsuchiya et al. mechanism

Tsuchiya et al. [2] have suggested a detailed 31-reaction mechanism for the hydrogen sulfide oxidation reaction. A comparison was made between some of their results and our 17-reaction reduced mechanism.

The comparison between these two mechanisms was executed under the following inlet conditions:

4% H2S

6% O2

90% Ar

Reactor temperature 1800K

The following figure shows that under these conditions (lean) the agreement between the two mechanisms is much higher than the previous case. Most of the species got the same value at nearly the same residence time; however, some radicals do not follow this rule like OH. This will need further detailed study.

Figure 13. Comparison between Tsuchiya et al. [2] mechanism (right), and the reduced mechanism (left)

The last step in this reduction mechanism strategy is to make some last, fine manipulations to get all the results coherent with the detailed mechanisms at different conditions. Afterwards, assuming steady state conditions for some radicals like HOSO, SO, and O, we would end up with a reduced mechanism on the order of single digit equations and would be able to represent the necessary detailed mechanism in the hydrogen sulfide oxidation reaction.

5.	Summary

An updated experimental facility has been designed and fabricated to study both flame and flameless modes of sulfur recovery. The high-temperature conditions of the Claus process have been easily achieved with minimum losses and adequate temperature homogeneity. The H2S-injection mechanism recommended in our previous report was used. Sophisticated controls were implemented to ensure accurate and safe operation. The facility was also equipped with the means of temperature scanning and gas sampling and analysis. In preliminary tests of the updated facility, temperature scanning was performed along the hydrogen sulfide reactor centerline under different conditions of methane/oxygen injection while keeping their ratio stoichiometric, in order to make sure that we could achieve the required temperature homogeneity and to assure that the required temperature levels are achievable.  A temperature of 1600 K was achieved easily at half the maximum heat load the test rig can endure. Finally, a simplification for the reduced mechanism, introduced in our previous report, has been done based on extensive literature review and elimination of the reactions with marginal effects. We ended up with a 17-reaction mechanism, which has been compared with two detailed mechanisms, and good agreement was observed.

6.	Difficulties Encountered/Overcome

None.

7.	Planned Project Activities for the Next Quarter

- Reduce the reduction mechanism further by applying the steady state assumption on some intermediate species.

- Study experimentally the effect of the reactor temperature on the H2S injected and the sulfur recovery efficiency.

- Study experimentally the effect of changing the reactor temperature on the asymptotic values of different species.

References

1.	http://www.chem.leeds.ac.uk/combustion/sox.htm

2.	Tsuchiya, K., Kamiya, K., Matsui, H., “Mechanism of H2S Based on Direct Examination of the Key eactions,” International Journal of Chemical Kinetics, Vol. 29, Issue 1, pp. 57-66, 1997.

Appendix

Justification and Background

Hydrogen sulfide is present in numerous gaseous waste streams from natural gas plants, oil refineries, and wastewater treatment plants, among other processes. These streams usually also contain carbon dioxide, water vapor, trace quantities of hydrocarbons, sulfur, and ammonia. Waste gases with ammonia are called sour gases, while those without ammonia are called acid gases. Sulfur must be recovered from these waste streams before flaring them. Sulfur recovery from sour or acid gas typically involves application of the well-known Claus process, using the reaction between hydrogen sulfide and sulfur dioxide (produced at the Claus process furnace from the combustion of H2S with air and/or oxygen), yielding elemental sulfur and water vapor: 2H2S(g) + SO2(g) = (3/n) Sn(g) + 2H2O(g) with ΔHr= -108 kJ/mol. Therefore, higher conversions for this exothermic, equilibrium-limited reaction call for low temperatures, which lead to low reaction rates that dictate the use of a catalyst. The catalytic conversion is usually carried out in a multistage, fixed-bed, adsorptive reactor process, which counteracts the severe equilibrium limitations at high conversions. This technology process can convert about 96% to 97% of the influent sulfur in H2S to S. However, higher removal requires critical examination of the process and use of a near isothermal reactor, since the conversion is critically dependent upon the exothermic and endothermic conditions of the reactions.

Flameless combustion has been shown to provide uniform thermal field in the reactor so that the reactor temperature is near uniform. Reactor size can also be reduced, and combustion-generated pollutants emissions can be reduced by up to 50%.  Energy efficiency can be increased by up to 30%. The application of this technology appears to offer great advantages for the processes under consideration. The UAE, which pumps about 2.4 million bpd of crude oil, is also home to the world’s fifth biggest gas reserves at about 200 trillion cubic feet. Abu Dhabi Gas Industries (GASCO), an operating company of the Abu Dhabi National Oil Company (ADNOC), is leading a drive to boost gas production in the UAE from five to seven billion cubic feet per day. This calls for sulfur recovery capacity of over 3,000 metric tons per day with the associated SOx and NOx emissions. Therefore, the adoption and further development of flameless combustion technology for sulfur recovery among other commercial and industrial heating processes is expected to be crucial and beneficial, both economically and environmentally.

The conventional sulfur recovery process is based upon the withdrawal of sulfur by in situ condensation within the reactor. The selective removal of water should, however, be a far more effective technique, as its effect on the equilibrium composition in the mass action equation is much greater. The in situ combination of the heterogeneously catalyzed Claus reaction and an adsorptive water separation seems especially promising, as both reaction and adsorption exhibit similar kinetics, and pressure can be adapted to the needs of the adsorptive separation. Such an adsorptive reactor will lead to almost complete conversion as long as the adsorption capacity is not exhausted. There are numerous possibilities for implementing these two functions, ranging from fixed-beds with homogeneous catalyst/adsorbent mixtures to spatially structured distributions or even fluidized beds. Most of the previous studies have concentrated on the Claus catalytic conversion reactors and the TGTU. However, some previous studies have identified the Claus furnace as one of the most important yet least understood parts of the modified Claus process. The furnace is where the combustion reaction and the initial sulfur conversion (through an endothermic gaseous reaction) take place.  It is also where the SO2 required by the downstream catalytic stages is produced and the contaminants (such as ammonia and BTX (benzene, toluene, xylene) are supposedly destroyed. The main two reactions in the Claus furnace are: H2S + 3/2 O2 = SO2 + H2O, with ΔHr= -518 kJ/mol, and 2H2S + SO2 = 3/2 S2 + 2H2O, with ΔHr= +47 kJ/mol. This last endothermic reaction is responsible for up to 67% conversion of the sulfur at about 1200 °C. Moreover, many side reactions take place in the furnace; these side reactions reduce sulfur recovery and/or produce unwanted components that end up as ambient pollutant emissions. Therefore, it would be useful to combine the endothermic and exothermic process using an isothermal reactor offered by flameless oxidation combustion.

Approach

Critical review

We propose to conduct a critical review of the various approaches used for sulfur removal from the sour gas. The emphasis here will be on sulfur chemistry with due consideration to the fate of ammonia. Following the review, an experimental and a CFD numerical study of the flameless oxidation of the fuel will be conducted as follows:

CFD simulation

A numerical simulation study of the flame under normal and flameless oxidation of fuels in the furnace will be conducted using the available codes. Global features of the flow and thermal behavior will be obtained using the Fluent CFD and Chemkin computer codes. These codes provide detailed simulation of the flow, thermal and chemical behaviors (i.e., detailed chemistry) in the reactor flow using gas-phase reactants. The sulfur in the fuel is in gas phase, so we will be able to simulate and monitor the fate of sulfur during various stages of endothermic and exothermic reactions and over a range of temperature regimes, including those covered in the Claus furnace process. The simulation results will also guide the final design of the flameless furnace. The simulations will also help assist in the experimental program for data validation with the eventual goal of implementing the process for sulfur removal.

Experimental study

An experimental study of the flameless vs. normal flame combustion process for the conditions examined in the theoretical study, including that of Claus furnace, will be conducted. We will explore the operating conditions and the exhaust gas analysis under conditions of both flame and flameless modes to determine the extent of sulfur conversion under the two conditions over the temperatures that can simulate endothermic and exothermic conditions in the Claus furnace. The goal is to seek conditions that yield the highest sulfur recovery from a process. To some extent, these conditions will be based on the composition of the acid/sour gas, from sulfur-rich (> 50% H2S) to lean (< 20% H2S). It is expected that our fundamental information will contribute to the eventual design guidelines of an advanced sulfur recovery process furnace operating under flameless combustion mode.

Solid Oxide Fuel Cells for CO2 Capture and Enhanced Oil Recovery UM Investigators: Prof. Greg Jackson UM GRA’s: Paul Jawlik and Siddharth Patel PI Investigator(s): Prof. Valerie Eveloy, Prof. Ali Almansoori Start Date: October 2006 Report Date: 15 July 2008

1.	Objective/Abstract

This multi-faceted project will investigate the feasibility of implementing advanced solid oxide fuel cell (SOFC) technology for producing power from oil well off-gases while providing a source of concentrated CO2 for sequestration and enhanced oil recovery.  This project will explore fundamental issues in identifying preferred material combinations for durable SOFC anode operation with typical oil well off-gas composition. Along with these fundamental issues, multi-scale modeling will include detailed models for assessing SOFC membrane electrode assembly architectures for optimal operation with hydrocarbons, and higher-level system models for evaluating integrated systems with all accessory equipment within the context of oil well operation.  System models will assess the economic viability of such a system and thereby determine technology performance requirements for successful implementation of SOFC-based systems for enhanced oil recovery with CO2 injection.

2.	Deliverables for the Completed Quarter

Task 1:  Experimental study of SOFC MEA’s for hydrocarbons

- Continue testing of membrane electrode assemblies (MEA’s) with Ni/YSZ/CeO2 anodes for performance on syngas (hydrocarbon reformate) and n-butane for a range of temperatures and fuel conversions.

- Develop methodology for removing cathode overpotentials for isolating anode performance in various tests.

Task 2: Numerical modeling for design of SOFC architectures

- Refine heat transfer models in SOFC models for predicting temperature distribution in down-the-channel fuel cell models.

- Implement first-generation down-the-channel fuel cell model for analysis of fuel cell performance on syngas streams.

Task 3: System-level analysis of integrated SOFC plants

- Begin system level analysis of integration of SOFC into petroleum processing

Task 4: Identification of multi-university research team for SOFC’s in the petroleum industry.

- No activities are planned for this task at this time.

3.	Summary of UM Project Activities for the Completed Quarter

The UM team has continued to explore a range of SOFC micro-architectures based on Ni/CeO2/YSZ anodes (for Task 1).  This quarter did not show any further progress in terms of improved MEA power densities over Q5 testing.  Thus, maximum MEA power densities (Vcell*i) of 0.6 W/cm2 on syngas and 0.35 W/cm2 on n-butane (with steam) at 800 °C remained the standard performance.  This data is presented again in Figure 1 to provide a basis for assessing current MEA performance for both syngas at (different fuel conversions) and n-butane with steam at an H2O/C ratio of 1.5.  Butane has not been tested for different conversions in the same way that syngas has been tested because it is expected that substantial internal reforming inside an SOFC channel flow path will cause a large fraction of the butane to be transformed into syngas [1].  Thus, for such hydrocarbon feeds, down the channel conversion will consist of substantial syngas formation and hopefully minimal carbon deposits with properly designed anode microarchitectures and materials.

Figure 1. Voltage and power density vs. current density curves for co-fired Ni/CeO2/YSZ anode-supported MEA’s operating at Tcell = 800 °C on n-butane with steam and on a range of syngas compositions at various locations along an SOFC channel (representing different total fuel conversions.

This past quarter did not see significant improvements in the results from the previous quarter as represented by Figure 1. Alternative means of incorporating CeO2 into the anode did not provide significant improvements to date and in some cases compromised MEA performance and electrolyte stability.

The modeling efforts were extended with improved heat transfer models developed to account for heat release due to non-electrochemical and electrochemical reactions in the 1-D through-the-MEA model.  This model was then expanded and used in a down-the-channel model with results initially obtained on syngas performance with axial heat conduction for a tubular SOFC geometry.  This model will be implemented fully in a planar system for the upcoming quarter.   Task 3 efforts for system-level analysis have begun, and this has included an investigation on the impact of expected impurities on SOFC performance.  In addition to the formal tasks, a PI intern has been successfully working this summer with the UM team on experimental testing and some analysis.

Task 1:  Experimental study of SOFC MEA’s for hydrocarbons

The Ni/CeO2/YSZ anode-supported, thin-electrolyte MEA’s with various microstructures have been tested for temperatures Tcell ranging from 700 to 800 °C on various fuels including 1) humidified H2 at a variety of H2O partial pressures, 2) syngas for a variety of fuel conversions, and 3) n-butane with H2O added at a 1.5-to-1 steam-to-carbon (S/C) ratio.  MEA architectures were fabricated with minor modifications to the fabrication protocol, which is retained in Appendix A in this report.  Additional cells with alternative anodes with ceria impregnated in the support and/or functional layers and also with ceria co-fired with Ni/YSZ in the anode support and/or functional layer.  Ceria has been added because of its ability to minimize coking [2, 3] and because ceria nanoparticles have been identified as a way to improve anode tolerance to H2S [4], which is expected to be one of the main contaminants for off-gases in petroleum processing.  Unfortunately, the tests in this quarter did not show further improvement in power density over the past quarter.  As explained below, MEA stability issues arose during this quarter, which slowed down progress on the testing.

Beyond just testing for the desired fuels, the MEA’s are also were also done with nearly pure H2 in the anode feed.  These tests with very high H2 content were performed to characterize the MEA cathode because nearly pure H2 feeds provides minimal anode overpotentials and allows for the evaluation of cathode overpotentials.  Equation 1, which relates overall measured cell voltage Vcell to the thermodynamically reversible cell voltage Vrev and the various overpotentials, provides a basis for understanding the value of this experimental procedure.

(1)

The pure H2 fuel testing allows for  and  to be minimized and if necessary well approximated by models.  Since is readily found from high-frequency impedance measurements, this allows for the pure H2 fuel MEA measurements to provide a basis for isolating the two cathode overpotentials   and , which can then be removed from voltage measurements along with .  This then allows for the anode overpotentials  and  to be evaluated during tests with syngas and hydrocarbons without relying on reference electrodes and their difficulties in implementing in SOFC testing as reported in the literature [5].  The anode overpotentials for the various measurements over Q5 and Q6 full cell measurements will be reported in the next quarterly report.

Task 2: Numerical modeling for design of SOFC architectures

Two accomplishments were achieved on this task in Q6.  Firstly, corrections were made for the energy balance for the non-isothermal, through-the-MEA model, and more analysis was performed on 1-D temperature variations for both syngas feeds and for methane feeds with internal reforming.  The second accomplishment involved an initial version with heat transfer, which was tested on syngas created from n-butane partial oxidation products.

For the non-isothermal, through-the-MEA model, the implementation of detailed methane oxidation chemistry adopted from previous references and UM work [6, 7]  allowed for several tests of the energy equation to determine expected thermal gradients perpendicular to the electrolyte.  The internal (endothermic) reforming of methane in the anode support layer causes some temperature losses in the MEA, and the drops in internal temperatures (from the flow channel temperature) increase with power density.  Figure 2a shows the predicted Vcell-i curve for an Ni/YSZ-anode supported MEA operating at 800 °C feed streams, including an anode stream of methane and steam at a steam-to-carbon ratio of 3:1.  The results show the relatively low power densities due to the slow reforming kinetics at 800 °C and due to the loss in temperature and therefore electrocatalytic activity in both the anode functional layer and the cathode.  The temperatures through the MEA at various current densities are shown in Figure 2b.  The overall temperature drop at the highest current density of 0.58 A/cm2 is less than 25 °C in the functional layer, but this can decrease cell performance due to increases in , and with the lower temperature.  All the same, this is still a relatively small temperature drop and suggests, as indicated in recent 2-D SOFC models, that most temperature variation in SOFC’s is along the channel flow [7].

Figure 2. a) Predicted Vcell vs. current density curve for an Ni/YSZ anode-supported MEA with 1020 µm thick anodes, 10 µm thick YSZ electrolytes, and 50 µm-thick LSM/YSZ cathodes operating at 800 °C flow temperatures with an CH4/H2O feed with a steam-to-carbon ratio of 3:1. b) Predicted temperature profiles for various current densities across the MEA for the case run in a).

An initial version of the down-the-channel model with heat transfer has been created for further studies.  This model, which is still in preliminary form, was used to predict current, species, and temperature profiles in a tubular fuel cell running on syngas created from catalytic partial oxidation of butane.  The model, which predicts heat transfer along the channel and across the MEA, shows that current densities vary strongly with distance along the channel.  Figure 3 illustrates this for three different Vcell, which was assumed fixed due to good current collection along the length of the tube.  The results also show that heat generation at higher current densities can be important for heating the cell and thus providing higher power.  This model will be described fully in the Q7 report.

Figure 3. Predicted current density as a function of Vcell and distance down the channel for a Ni/YSZ anode –supported tubular fuel cell.

Task 3: System-level analysis of integrated SOFC plants

The UM group began some system level analysis work by furthering its study on the impact of possible impurities from petroleum off-gases on SOFC anode performance and on assessing various designs for mitigating such impacts.  This work was an extension of a recent review paper by UM researchers and coauthors [8]. Expected fuel impurities such as H2S and perhaps some chlorinated species (likely converted to HCl) can significantly affect SOFC anode performance.  For Ni/YSZ anodes, this is particularly true for species that can react with the Ni to form new phases with poor electrochemical activity [9].  Other trace impurities can also appear but are not expected to be as significant.  The importance of gas clean-up for the system level studies will be increasingly important for designs that seek high fuel utilization for efficient operation and ease of downstream CO2 sequestration for enhanced oil recovery.

Recent reports on HCl impacts on SOFC anodes show that it can cause rapid degradation in Ni/YSZ anodes [10, 11].  Efforts to develop anode materials and architectures that can minimize degradation due to such halide impurities will be dependent upon how clean-up processes for the petroleum are integrated with the SOFC.  As such, this will be an important part of the system level modeling to be completed in Q7.

Significant work has been pursued to understand the effects of H2S on various anode materials.  These include efforts to develop new anode materials with higher sulfur tolerance [12, 13].  Sulfur concentrations as low as a few parts per million can deactivate Ni catalysts, which significantly reduces conventional Ni/YSZ anode performance.  This has led to considering alternative electrolyte-phase materials, notably GDC, which decreases the rate of Ni degradation [14].   The effects of CeO2 nanoparticle addition to Ni/YSZ anodes has been shown to dramatically improve sulfur tolerance, and this remains a promising approach for syngas applications with low H2S concentrations [4].  Alternative electronically conducting perovskite materials can replace Ni/YSZ-cermets altogether, and surprisingly good performance has been achieved with perovskite anode electrocatalysts such as strontium-doped lanthanum vanadate [15] and yttrium-doped strontium titanate [16] when using syngas with relatively high concentrations of H2S.  However, because questions remain as to the long-term durability of these anodes for SOFC applications, this project is preferring to take the approach of CeO2 addition as a preliminary approach for handling this project.  More work has been proposed in a follow-on program to address this issue.

System-level modeling using simplified versions of the Matlab SOFC models and Excel-based macro models will be implemented in Q7 for an example SOFC system integrated with a petroleum processing facility.  An initial design is being set up by the UM team, and the current PI intern is participating in this effort during his summer stay. This modeling approach will hopefully be complemented by Aspen/Hisys modeling, which will be discussed in September, when the PI faculty are expected to visit UM.

4.	Difficulties Encountered/Overcome

The experimental test program was not as successful this quarter due to inconsistent MEA durability.  This problem has been identified as material degradation, and so new materials have been bought and performance of recent cells is getting back to Q5 results.

The development of the down-the-channel SOFC model is progressing nicely with the only outstanding challenge being the development of CeO2 surface chemistry and ionic conduction models as well as the higher hydrocarbon surface chemistry models.  Progress is being made on this by the UM team on another project, and the detailed CeO2 surface chemistry mechanism and thermodynamics will be available.

5.	Planned Project Activities for the Next Quarter

In the upcoming quarter, the following activities are expected for Tasks 1-3, and some discussions will begin concerning Task 4 as the next phase of this collaboration is being discussed.

Task 1:  Experimental study of SOFC MEA’s for hydrocarbons

- Test more Ni/CeO2/YSZ anode-supported MEA’s for stability and higher power densities, particularly for butane feeds as well as for methane feeds.

- Use experimental results to validate models for Ni/CeO2 anode models for Task 2 at UM.

Task 2: Numerical modeling for design of SOFC architectures

- Continue development of hydrocarbon electrochemical models for CeO2 and study optimal anode architectures for hydrocarbons with 1-D through-the-MEA models

- Test the down-the-channel model at UM and provide a wide array of results for the next report and the upcoming visit by PI faculty.

Task 3: System-level analysis of integrated SOFC plants

- Initiate discussions with interested PI representatives and relevant industry representatives to begin the development of the steam reformer, carbon capture, and balance of plant models in Aspen or Hisys either at PI or UM.

Task 4: Identification of multi-university research team for SOFC’s in the petroleum industry.

- Nothing will be planned on this task until after high-level discussions are held to indicate PI interest in expanding this effort. This may occur to some extent during the PI faculty visit in September.

Appendix A

Fabrication Protocol for Ni/CeO2/YSZ-Anode Supported Cells

After substantial testing of various architectures and fabrication approaches for Ni/CeO2/YSZ anode-supported MEA’s, the following fabrication protocol has been identified for producing cells with the highest power densities that operate well on syngas at a variety of conversions and light hydrocarbons with steam addition.  These cells are what are referred to as co-fired with ceria.  The protocol here is different from impregnated ceria, where the CeO2 is added after the firing of a Ni/YSZ anode via a Ce(NO3)3·6H2O solution diluted with isopropanol.  The impregnated ceria adds CeO2 as very small particles in both the anode support and functional layers.  These cells were not as stable as the co-fired ceria likely due to ceria seeping into small pinholes in the electrolyte and compromising the electrolyte stability.

Fabrication of Ni/CeO2/YSZ Porous Anode Support with Ni/YSZ Functional Layer and Thin Electrolyte

The Ni/CeO2/YSZ anode supports are fabricated using NiO, CeO2, YSZ, and graphite powders.  NiO, CeO2. and YSZ powders are mixed with ethanol and ball milled for ~24 hrs.  Graphite pore former is then added, followed by further ball milling for a minimum of 4 hrs.  The slurry is then dried and passed through a sieve.  The dried powder is then pressed for 5-10 min. at a pressure of 10 metric tons for a 3 cm diameter cell.  The cells are then placed in a furnace and heated to 900°C over the course of 500 min. to burn out the graphite.

To create the interlayer, NiO and YSZ powders are mixed in isopropanol and sonicated for 5 to 10 min. (without pore former).  Polyvinyl butyral (PVB) is then added to the suspension, followed by further sonication lasting a minimum of 30 min.  The requisite amount of the suspension is drop-coated onto the surface of the cell and allowed to air dry.  The cell is then heated to 900°C in a similar manner as was previously mentioned.  This heating is performed to increase the strength of the cell and to ensure adhesion between the interlayer and the bulk of the cell.

For the thin electrolyte, YSZ is mixed in isopropanol and sonicated for 5 to 10 min.  PVB is then added to the suspension followed by further sonication lasting a half an hour.  The appropriate volume of the YSZ suspension is drop-coated onto the surface of the NiO/YSZ anode supports and allowed to dry in air.  The anode/dense electrolyte structure is then heated to 1450 ºC over a well-defined schedule (lasting 1.5 days) to densify the electrolyte.

Fabrication of LSM/YSZ Cathode Functional Layer with LSM Current Collecting Layer

LSM/YSZ paste purchased from Fuel Cell Materials (Lewis Center, OH) is used for the cathode functional layer.  A strip of Kapton tape with a half-inch diameter hole in the center is used as a mask.  The tape is placed on the electrolyte side of the cell and LSM-YSZ paste with some graphite powder pore former is spread evenly over the mask.  The paste is heat-dried.  This cathode functional layer behind is approximately 25-30 µm thick.  An optional current collecting layer of LSM paste with graphite powder pore former also from Fuel Cell Materials is similarly pasted over the functional layer to assist in current collection   The cell is then heated slowly to 1300ºC to burn out the graphite pore former and to solidify the interfaces between the electrolyte and the functional layer and between the functional layer and the current collecting layer.

Current Collection and Miscellaneous Preparation

A 0.5-mm silver wire is spot welded to a silver mesh and attached to the cathode using silver paste.  For the anode side, a 0.5-mm silver wire is spot-welded to a nickel mesh and attached to the anode using nickel paste.  The cell is mounted to an alumina tube using ceramic paste.  A thermocouple is then attached to the cathode side of the cell also using a ceramic paste.  The tube assembly is placed inside a furnace and heated to temperature without exposure to hydrogen.  Once at the desired temperature (usually 800°C or 850°C), the anode is exposed to hydrogen gas for several hours to reduce the NiO.

MEA Architecture:

Anode – 1 mm thick Ni/YSZ cermet with a dense ~20-30 micron Ni/YSZ interlayer

Electrolyte – ~10-15 micron thick dense YSZ electrolyte

Cathode – ~20 micron thick LSM/YSZ composite

Anode Current Collector – 50 mesh nickel gauze with nickel paste attached to the outer

anode surface

Cathode Current Collector – 50 mesh platinum gauze with platinum paste attached to

the outer surface of the cathode

Appendix B

Justification and Background

SOFC power plants provide a unique opportunity to provide ultra-high efficiencies (> 64% electrical) while simultaneously separating CO2 emissions from N2 dilution for efficient CO2 sequestration (17).  While SOFC architectures/MEA’s have been developed for operating with small molecule fuels (H2, CO, and CH4), challenges remain to develop SOFC assemblies for higher hydrocarbon fuels although recent progress in SOFC design and materials has indicated the feasibility of such systems.  The UM Team has been evaluating SOFC anodes for small hydrocarbon fuels, and their recent unpublished work on alternative ceria-based anodes show promise for stable operation with hydrocarbons.

This work, combined with the development of detailed microstructure models and higher-level system models, will provide the basis for pursuing a combined experimental and multi-scale modeling effort that will explore the possibility of implementing new high-temperature solid oxide fuel cells in petroleum extraction. These models will aid in both high-efficiency power production and production of concentrated CO2 streams for enhancing oil recovery while sequestering CO2 emissions.  This collaborative work will allow the Petroleum Institute and UM to become leaders in promoting SOFC technology to improve the operation of and reduce the environmental impact of oil recovery.

Approach

Four tasks identified for this project are presented here.

Task 1:  Experimental study of SOFC MEA’s for hydrocarbons

UM has high-temperature single-cell rigs with electrochemical characterization tools, electronic flow controls, and data acquisition for studying SOFC MEA’s.  This project will expand these capabilities to study porous MEA architectures of ceria-based anodes for stable operation on C3-C5 gases.  Experiments will explore the role of metal doping of the ceria for improved electronic conductivity and activity for fuel breakdown to avoid carbon build-up. The experiments will include V-I measurements as well as impedance spectroscopy to validate models developed in Task 2, as well as post-testing microscopy and surface characterization to evaluate the durability of the SOFC anodes for the different fuels. After being established at UM, these capabilities will be duplicated at the Petroleum Institute (PI) with the aid of UM researchers such that faculty at the PI will also participate in this effort while providing PI students a chance to explore SOFC technology.  A UM Graduate Student/Research Associate (RA) jointly supervised by the UM and PI Teams will assemble the experimental facilities at PI by the end of the first year of the project.  This will permit, in the second year of this project, the PI Team to commence assessing the reproducibility of experimental measurements performed at UM.  This will also provide PI students an opportunity to explore SOFC technology.

Task 2: Numerical modeling for design of SOFC architectures

Modeling of membrane electrode assemblies will explore optimal design of SOFC’s for hydrocarbon operation and high fuel conversion efficiency to provide optimal CO2 capturing by eliminating downstream combustion of unburned fuel.  This work will build on 1-D and 2-D detailed Matlab/Cantera-based models developed at UM for SOFC MEA analysis.  New efforts will involve the development and validation of hydrocarbon kinetic models on preferred anode materials identified in Task 1. Depending upon the availability of a RA/Graduate Student which PI plans to recruit for the project (see Key Personnel), and computational hardware/software resources at PI, the PI Team may i) expand the parametric analysis space explored at UM using Matlab/Cantera-based models provided by the UM Team, and/or ii) investigate numerical modeling methodologies and software to explore the feasibility of implementing multi-physics models used in the UM Team’s Matlab/Cantera models, into commercially-available computational fluid dynamics (CFD)-based software to improve the simulation of SOFC MEA’s having complex geometries.

Task 3: System level analysis of integrated SOFC plants

The economic and engineering viability of an integrated SOFC plant for CO2 sequestration and efficient power production will be investigated numerically by the UM Team, and possibly the PI Team - if compatible with man-power, and computational hardware and software resources available at PI - within the context of petroleum production, using Matlab-based system level modeling tools developed at UM and possibly other process analysis software to be identified for use at PI.  These tools will be used to explore overall balance of plant, adequacy of fuel supplies, and power requirements for CO2 capture.  If possible, this work will be done in consultation with ADNOC experts.

Task 4: Identification of multi-university research team for SOFC’s in the petroleum industry.

The UM/PI team will spend a portion of his time developing a broader-base team for pushing this project further toward implementation. Potential partners may include the Colorado School of Mines and the Norwegian University of Science and Technology, with whom UM has established collaborations in other research areas.  Industrial partners may also be considered.

Two-Year Schedule

Year 1:

- Begin experiments for identifying preferred material systems using ceria-based anodes for hydrocarbon SOFC operation.

- Perform post-testing material characterization for evaluation.

- Acquire equipment for assembly rig at the PI.

- Adopt Matlab SOFC models at UM for hydrocarbon studies.

- Undertake CFD modeling at PI.

Year 2:

- Perform experiments with preferred material systems for typical off-gas compositions (with varying team loadings).

- Validate models and perform SOFC design for both MEA microstructure and overall all fuel cell size.

- Establish system level models at both institutions, and Identify preferred system configurations for overall balance of plant.

References

- Gupta GK, Dean AM, Ahn K, Gorte RJ. 2006. Journal Of Power Sources 158: 497-503

- Gross MD, Vohs JM, Gorte RJ. 2007. Journal Of Materials Chemistry 17: 3071-7

- Costa-Nunes O, Gorte RJ, Vohs JM. 2005. Journal Of Power Sources 141: 241-9

- Kurokawa H, Sholklapper TZ, Jacobson CP, De Jonghe LC, Visco SJ. 2007. Electrochemical And Solid State Letters 10: B135-B8

- Adler SB. 2002. Journal of the Electrochemical Society 149: E166-E72

- Habibzadeh B. 2007. Understanding CO Electrochemical Oxidation Using Ni Patterned Anodes. Ph.D. Dissertation thesis. University of Maryland, College Park, MD

- Janardhanan VM, Heuveline V, Deutschmann O. 2007. Journal Of Power Sources 172: 296-307

- Kee RJ, Zhu HY, Sukeshini AM, Jackson GS. 2008. Combustion Science And Technology 180: 1207-44

- Trembly JP, Gemmen RS, Bayless DJ. 2007. Journal Of Power Sources 171: 818-25

- Trembly JP, Gemmen RS, Bayless DJ. 2007. Journal Of Power Sources 169: 347-54

- Buchinger G, Hinterreiter P, Raab T, Griesser S, Claassen R, et al. 2006. Journal Of Fuel Cell Science And Technology 3: 280-3

- Aguilar L, Zha SW, Li SW, Winnick J, Liu M. 2004. Electrochemical and Solid-State Letters 7: A324-A6

- Cheng Z, Zha SW, Liu ML. 2006. Journal Of The Electrochemical Society 153: A1302-A9

- Ouweltjes JP, Aravind PV, Woudstra N, Rietveld G. 2006. Journal of Fuel Cell Science and Technology 3: 495-8

- Cheng Z, Zha SW, Aguilar L, Wang D, Winnick J, Liu ML. 2006. Electrochemical And Solid State Letters 9: A31-A3

- Kurokawa H, Yang LM, Jacobson CP, De Jonghe LC, Visco SJ. 2007. Journal Of Power Sources 164: 510-8

- Moller BF, Arriagada J, Assadi M, Potts I. 2004. Journal of Power Sources 131: 320-6

Fundamental Immiscible Porous Media Studies for Improved Reservoir Models UM Investigators: K. Kiger, A. Riaz, A. Shooshtari GRA’s: M. Al Hebsi PI Investigators: Start Date: Current Quarter Report Date: 15 July 2008

1.	Objective/Abstract

Current reservoir simulation models are based on an empirical extension of porous media single-phase flow, which is known to poorly represent flow behavior in a wide range of relevant operating conditions. Experiments and numerical simulations are proposed to study the detailed mechanics of immiscible two-phase flow in porous media, with the intent to explore the nonequilibrium mechanisms responsible for the breakdown of traditional continuum equations used for reservoir simulation. The experiments will be conducted with an index-matched visualization facility, which will permit both microscopic (pore scale) and mesoscopic measurements of the constituent phases and the local velocity field. The simulations will be conducted with a combination of simple pore network models and direct numerical simulation of the micropore dynamics. The outcomes of this research will enable the rational modeling extension of the traditional equilibrium relative permeabilties to account for the non-equilibrium conditions which occur for unstable displacement conditions.

2.	Approach

Short-Term Goals

The current funding represents an initiation seed program in anticipation of a fully funded project during Phase II. As such, the efforts are directed towards developing the computational tools, techniques, and test facility that will be needed for the successful completion of the project. We plan to complete the following short-term goals for the experimental work over the next six months:

- Determination of working fluids compatible with viscosity ratio and index of refraction requirements for the experimental technique

- Design and construction of the initial version of the test cell required for the experiments

- Development of the image processing routines required to determine the interface location and local fluid motion within the pore volumes

In addition to the above experimental program, a computational effort is underway in collaboration with Dr. Amir Riaz and Dr. Amir Shooshtari as part of a summer intern project for Mr. Mohamed Al Hebsi, visiting for 7 weeks from the Petroleum Institute. Mr. Hebsi will be implementing a pore-network simulation model developed by Dr. Riaz, with the goal of extending its functionality to a broad range of parametric space. The development of the pore-network model is a complementary tool to the pore-scale tests to be completed as part of the experimental program, as well as the direct numerical simulation tool. The short term goals for the numerical work include:

- Demonstration of the operation of the pore-network model to replicate simple known physics

- Extension of the pore-network model to include the effects of pore morphology.

- Development of iterative linear solvers for larger problems.

Long-Term Goals

Experimental work will be conducted to study the details of both the micro- and macroscopic behavior of the displacement process in the intermediate viscosity and capillary regime during the onset of fingering instabilities. Knowledge of the detailed pore-scale dynamics (interface configuration) and the resulting macroscopic evolution (relative phase saturation and velocity field) are needed in order to advance the current state of continuum modeling to cover a broader range of parametric space. Specifically, recent work has proposed generalized extensions to the standard relative permeability coefficients, which include permeability interaction terms to account for nonlinear phase interactions. To assess the development of these models, interaction of the capillary forces with the flow-induced viscous effects in the vicinity of the incipient finger need to be characterized.

Toward this goal, a laboratory scale, two-phase porous flow visualization facility will be constructed. The working fluids (aqueous salt solutions and various grade silicone oils) and porous media will be selected to generate an index-of-refraction matched system, which will allow for a clear view of the interior processes with minimal optical distortion. Separate fluorescent dyes will be used to mark both working fluids, which when combined with appropriate filters, will allow unambiguous measurements of each phase volume fraction, interface geometry, and the porosity of the media. Use of two different optical configurations will permit visualization of the microscale and macroscale behavior. These imaging systems will be mounted on a traversing stage to allow for a three-dimensional reconstruction of the fluid configuration from the sampled two-dimensional images. Lastly, the phases will also be seeded with neutrally buoyant micron-sized tracer particles, which will be used to measure the local velocity field of both phases. Our lab has expertise in developing and applying particle image velocimetry techniques to the study of multiphase systems, which can be leveraged to the proposed work.

The concurrent numerical work will produce a complementary set of results that will be used to obtain detailed flow field information difficult to access through the experiments. This includes the determination of phase saturation distribution, interfacial area, film thickness on solid surfaces, contact angle variation with capillary number, and viscosity ratio. Numerical simulations will also be used to explore a wider range of parameters and flow conditions than those possible with experiments.

Numerical simulations will be calibrated rigorously through a detailed comparison with experimental observations and the velocity field data obtained with particle image velocimetry. Together, numerical simulations and experiments will produce detailed flow field data that will be utilized to determine the averaged behavior of the flow process over various length scales containing different pore configurations. The average behavior of the flow statistics will determine the validity of the standard multi-phase flow models as well as suggest new averaging strategies for averaging of derivative based quantities such as pressure and temperature fields.

Numerical simulations will be based on the Volume of Fluid, finite element method. This method will be extended to take into account the discontinuous nature of the interface separating the fluids. The standard implementation is based on the introduction of a source term representing the interfacial forces into the momentum equations. This methodology gives rise to an interface that is not smooth in the gradient and hence does not accurately represent the interfacial curvature terms. The new implementation will use the level set function to model the interface. The interfacial conditions will then be determined from the exact interface representation to produce accurate flow conditions across the interface.

3.	Five-Year Schedule

Year 1:	Facility construction, regime identification, preliminary visualizations, development of image reconstruction routines;

Year 2:	Testing of initially selected conditions, development of PIV method for porous media application

Year 3:	Testing phase: influence of capillary number and viscosity ratio under various conditions; start construction on demonstration rig for PI; application of test results toward model development.

Year 4:	Continued testing at UM, shakedown and initial testing at PI; continued model development

Year 5:	Final testing based on feedback from earlier model assessment; final model development

Solar Cooling UM Investigators: Professor Reinhard Radermacher, Dr. Yunho Hwang GRA’s: Ali Al-Alili PI Investigator(s): Dr. Isoroku Kubo, Dr. Peter Rodgers Start Date: August 01, 2007 Report Date: July 08, 2008

# 1.	Objective/Abstract

The main objective of this project is to design, fabricate and test a solar cooling system with the highest possible cooling COP measured to date.  The approach involves combining a very efficient concentrating PV-T collector with separate sensible and latent cooling approach developed at CEEE. This solar cooling system is expected to operate under the UAE’s harsh climate conditions.

# 2.	Deliverables for the Completed Quarter

•	The following tasks were accomplished this quarter:

- Finish the literature review and publish a review paper on solar cooling technologies

- Model the solar sub-system in TRNSYS

- Model the best combination between the solar technologies and the thermal cooling technologies in TRNSYS.

# 3.	Summary of Project Activities for the Completed Quarter

The fundamentals of solar radiation, thermal collectors, PV and thermal cooling processes have been reviewed. A review paper on solar cooling technologies has been published. In addition, the solar thermal collector and the PV technology has been compared to the performance of the photovoltaic/thermal hybrid collector. The best combination between the solar technology and cooling technology has been modeled in TRNSYS.

# 3.1	Coupling the Solar and Cooling Technologies

A comparison of possible combinations is shown in Figure 1 based on the information gathered on the cooling processes and the various solar collectors.

Figure 1. Various combinations between solar and cooling processes

It can be seen that the highest possible overall cooling COP can be achieved by coupling the PV/thermal collector with two cooling processes. The reason for choosing these particular cooling cycles is to accommodate the latent load and the sensible load separately. A solid desiccant cycle, which is derived from the thermal output of the collector, is used to accommodate the latent load. A vapor compression cycle, which is powered by the electric output of the collector, is used to accommodate the sensible load.

The novelty of this combination is that minimal external energy source is needed since the collector is used to provide the electricity and thermal energy required to derive the two cooling cycles. The desiccant cycle lowers the vapor content of the inlet air, allowing the vapor compression cycle to operate at a higher evaporator temperature and pressure, which decreases the pressure ratio, hence increasing the compressor efficiency. The whole system might be configured as shown in Figure 2.

Figure 2. Possible system configuration

# 3.2	Modeling Methodology

This system is modeled based on Abu Dhabi weather data. Four cities in different US climate zones were also chosen for the investigation of the system performance in various climate conditions. The cities are shown in Figure 3 with their respective latitudes, longitudes and elevations.

Figure 3. The selected cities in different US climate zones

The modeling approach is shown in Figure 4. By calculating the electrical and thermal supply of the solar sub-system and the required heating and power by the cooling processes, one can calculate the solar fraction of each type of energy provided. For example, a thermal solar fraction and an electrical solar fraction can be calculated as shown below.

Thermal solar fraction = Qprovided / Qrequired

Electrical solar fraction = Eprovided / Erequired

Figure 4. Modeling Approach

The system is modeled with the well-known TRNSYS program. TNRSYS consists of many subroutines that model subsystem components. It is necessary to construct an information flow diagram for the system once all the components of the system have been identified. The information flow diagram for the whole system was created as shown in Figure 5. The purpose of the information flow diagram is to facilitate identification of the components and the flow of information between the various components.

Figure 5. System flow diagram

# 3.3	Solar Cooling System Modeling

The solar sub-system was modeled first. Its configuration is shown in Figure 6.

.

Figure 6: Solar sub-system components

Secondly, the vapor compression cycle (VCC) has been modeled in Engineering Equation Solver (EES). TRNSYS is capable of calling EES once the input information is available. The VCC uses R410a as a refrigerant and has a capacity of 15 kW. The T-s and the P-h diagrams of the VCC are shown in Figures 7 and 8, respectively.

Figure 7. VCC T-S diagram

Figure 8. VCC P-h diagram

The desiccant wheel cycle was then modeled in TNRYS. It consists of the desiccant wheel, the enthalpy wheel and two fans. After the two cooling processes were modeled, the conditioned space and the two sub-systems were coupled as shown in Figure 9.

Figure 9. The whole system in TRNSYS

A brief description of each component’s parameters and the TRNSYS module, TYPE, used to model each component, is shown in Table 1.

Table 1. TRNSYS Components

It should be mentioned that the purpose of the preliminary code is to insure that there are no errors in running the program and joining all the components together. Therefore, the values in the previous table will be modified once the whole system is sized. An example of the system performance under the UAE’s climate conditions for the first two weeks of July is shown in Figure 10.

Figure 10. Temperatures at different locations of the system

Orange ( Collector outlet temperature

Red ( Ambient temperature

Blue ( Temperature of water leaving the storage tank going to the collector

Pink ( Temperature of water leaving the storage tank going to the water-air heat exchanger

Green ( Condition space temperature

The two straight lines represent the comfort zone in the conditioned space.

The VCC COP is shown below in Figure 11.

Figure 11. VCC COP

The following main parameters were monitored during each simulation:

  - Mass flow rates

  - Temperatures

  - Humidity ratio

  - Electrical loads

  - Thermal loads

# 4.	Difficulties Encountered/Overcome

- Predicting the performance of the solar cooling system

- Sizing the different components in the system

- Optimizing the system performance

# 5.	Planned Project Activities for the Next Quarter

The following activities are to be conducted in the next quarter:

- Finalize the size of the whole system

- Investigate the main parameters’ sensitivity on the component, sub-system and whole system level

- Write a first draft of a paper on modeling the very efficient solar cooling system chosen using TRNSYS

# Appendix

Key References

- Stine, W.B., Geyer, W.B., 2001, Power from the sun, www.powerfromthesun.net.

- Threlkeld,.J, Kuehn, T., Ramsy, J.,1998, Thermal Environmental Engineering, Prentice-Hall, Inc, USA

- http://www.nrel.gov/rredc/solar_data.html

- http://rredc.nrel.gov/solar/old_data/nsrdb/tmy2/State.html

- Notton , G. , Poggi, P. , Cristofari, C., 2006, Predicting hourly solar irradiations on inclined surfaces based on the horizontal measurements: Performances of the association of well-known mathematical models, Energy Conversion and Management, 47 1816–1829

- http://rredc.nrel.gov/solar/old_data/nsrdb/1991-2005/siteonthefly.cgi?id=724060

- ASHRAE, 1999, Applications Handbook, CH.32

- Kreith, F. and Kreider, J.F., 1978, Principles of solar engineering, Hemisphere publishing corporation Washington USA

- Kalogirou, S., 2004, Solar thermal collectors and applications, Progress in Energy and Combustion Science  30 pp. 231–295

- Goswami, Y., Kreith, F. and Kreider, J.F., 2000, Principles of solar engineering, Taylor and Francis, PA, USA,

- Duffie, J.A., Beckman, W.A., 1991, Solar engineering of thermal processes, Second edition, John Wiley & Sons, Inc., New York, ISBN: 0-471-51056-4.

- Pasupathy, A., Velraj,  R., Seeniraj, R.V., 2008, Phase change material-based building architecture for thermal management in residential and commercial establishments, Renewable and Sustainable Energy Reviews, pp.39–64

- Dieng, A., Wang, R. , 2001 Literature Review on Solar Adsorption Technologies of Ice-making and Air Conditioning Purposes and Recent Developments in Solar Technology, Renewable and Sustainable Energy Reviews 5 pp.313–342

- Sumathy, K., Yeug, K, Yong, L., 2003, Technology Development in the Solar Adsorption Refrigeration Systems, Progress in Energy and Combustion Science 29 pp 301–327

- Roger, A. Messenger, J. V., 2005, Photovoltaic Systems Engineering, 2nd ed. Taylor & Francis

- http://www.nfpa.org/

- http://ieeexplore.ieee.org/iel5/7946/21930/01019771.pdf?arnumber=1019771

Waste Heat Utilization in the Petroleum Industry UM Investigators: Professor Reinhard Radermacher, Dr. Yunho Hwang GRA’s: Amir Mortazavi, Chris Somers PI Investigator(s): Dr. Saleh Al Hashimi, Dr. Peter Rodgers Research student: Sahil Popli Start Date: December 1, 2006 Report Date: June 26, 2008

# 1.	Objective/Abstract

The main objective of this project is to minimize overall energy consumption of gas or oil processing plants by utilizing waste heat and/or improving cycle design.  Consideration will include use of absorption chillers and two-phase expanders, among other options.

# 2.	Deliverables for the Completed Quarter

•	The following were modeled in ASPEN:

- GE MS6001 gas turbine

- Natural gas liquefaction and fractionation process

- Double effect water/LiBr absorption chiller

# 3.	Summary of Project Activities for the Completed Quarter

The GE MS6001 gas turbine was modeled as a potential waste heat source. This turbine was selected because it is currently used in the TAKREER refinery and could be used as a compressor driver in the ADGAS LNG plant.  The natural gas liquefaction and fractionation process was modeled to assess opportunities for cycle enhancements, heat integration and waste heat utilization. A potential use for waste heat is cooling, which is especially valuable in the Middle East. Absorption chillers are one of the best technologies for converting waste heat to cooling capacity because of their versatility and efficiency. To this end, a single- and double-effect water/lithium bromide chiller have been modeled.

# 3.1	Gas Turbine Modeling

The GE MS6001 gas turbine was modeled for:

- Quantifying the available of waste heat from one of the gas turbines at the TAKREER refinery.

- Driving the propane cycle.

The schematic diagram of the model is shown in Figure 1. In Table 1 the model results are compared with vendor data. It should be noted that the combustion process was considered in this model.

Table 1. The model results in comparison with vendor data

|  | Vender Data | Model | Discrepancy |
| --- | --- | --- | --- |
| Output Power [MW] | 43.53 | 42.84 | 1.58 % |
| Exhaust Temperature [°C] | 544 | 548 | 4 °C |
| Efficiency [%] | 33.3 | 34.4 | 3.22 % |
| Exhaust flow rate [kg/sec] | 140 | 140 | --- |

Figure 1. Schematic diagram of gas turbine model

# 3.2	Natural Gas Liquefaction and Fractionation Modeling

The APCI liquefaction process was selected for modeling because about 77% of LNG plants, including the  ADGAS plant, are utilizing this technology for natural gas liquefaction. The schematic diagram of process is shown in Figure 2.

Figure 2. Schematic diagram of APCI liquefaction process [3]

For the sake of simplicity, the gas-sweetening process and flash-gas utilization were not considered in the modeling. The schematic diagram of the model is shown in Figure 3.  The model is capable of modeling:

- Liquefaction and fractionation processes for different natural gas compositions

- The process for different product purity requirements

- Different vapor fractions at the LNG process

- The effect of ambient temperature on performance of the LNG plant

- The effect of new components on plant efficiency and capacity

- The effect of component-efficiency degradations on performance of the LNG plant.

As an example, modeling results for the natural gas composition specified in Table 2, with assumptions in Table 3, are summarized in Tables 4 and 5.

Figure 3. Schematic diagram of ASPEN model

Table 2. Assumed feed gas composition

| Gas composition after sweetening |
| --- |
| Component | Mole percent |
| Nitrogen | 0.1 |
| Carbon dioxide | 0.005 |
| Methane | 85.995 |
| Ethane | 7.5 |
| Propane | 3.5 |
| i-Butane | 1 |
| n- Butane | 1 |
| i-Pentane | 0.3 |
| n-Pentane | 0.2 |
| Hexane plus | 0.4 |
| Total | 100 |

# Table 3. Model assumptions

| Sea water temperature | 35 °C |
| --- | --- |
| Propane compressor efficiency | 83 % |
| Mixed refrigerant compressor efficiency | 86 % |
| Feed gas mass flow rate | 111.11 kg/s |

# Table 4. Product composition results				Table 5. Plant results

| Component | Mole fraction |
| --- | --- |
| Nitrogen | 0.00101821 |
| Carbon dioxide | 5.1739e-05 |
| Methane | 0.88945969 |
| Ethane | 0.07694433 |
| Propane | 0.02459356 |
| Iso- butane | 0.00417114 |
| N- Butane | 0.00322346 |
| N-Pentane | 0.00016162 |
| Iso-Pentane | 0.00033784 |
| N-Hexane | 9.1746e-06 |
| Iso-Hexane | 2.9206e-05 |

| Propane compressor power [MW] | 35.34 |
| --- | --- |
| Mixed refrigerant compressor power [MW] | 66.535 |
| Propane cycle cooling capacity [MW] | 115.466 |
| Mixed refrigerant cycle cooling capacity [MW] | 165.475 |
| Propane cycle COP | 3.267 |
| Mixed refrigerant Cycle COP | 2.487 |
| LNG Vapor fraction after the expander [%] | 0.05 |

# 3.3	Absorption Chiller Modeling

Absorption chillers were modeled as a means of utilizing waste heat. They were envisioned to take waste heat from a gas turbine and convert it into a cooling load to reduce the energy demands of the propane chiller cycle.

The model for a single-effect water/LiBr chiller was detailed in the last report. In this report, details of the double-effect model are described. The double-effect design will be useful when higher COPs are desired. There were some unique challenges involved in modeling the double-effect design. For one, the property method had to be checked at the higher temperatures and pressures needed for double-effect cycles. Additionally, there was added complexity in component modeling.

As with any model, this model has an associated error, which is summarized below. Heat duties of various components were compared to published values in the textbook by Drs. Herold and Radermacher titled “Absorption chillers and heat pumps” (1996), which are based on EES models. Note that the components associated with pure water have very low errors (less than 0.4%), while the components with solution have a larger error (~3%). This is a result of the property method chosen. It is believed that this error could be improved using a data regression analysis in ASPEN, which takes known experimental data to improve property parameters. Now that both single and double effect cycles have been modeled, this technique will be investigated.

Table 6. Water/LiBr model comparison

|  | Units | EES | ASPEN | Error | % Error |
| --- | --- | --- | --- | --- | --- |
| Absorber | kW | 436.18 | 421.155 | 15.025 | 3.44% |
| Upper condenser | kW | 192.78 | 193.447 | 0.667 | 0.35% |
| Lower condenser | kW | 185.7 | 185.579 | 0.121 | 0.07% |
| Evaporator | kW | 354.37 | 354.737 | 0.367 | 0.10% |
| Desorber | kW | 267.49 | 259.335 | 8.155 | 3.05% |
| COP | - | 1.325 | 1.368 | 0.043 | 3.24% |

The temperatures at various state points in the cycle were also compared, with a maximum error of 1.6 ºC and an average error of 0.36 ºC.

The process flow diagram of the model in ASPEN Plus is shown below.

Figure 4. Water/LiBr double-effect chiller process flow diagram

# 4.	Difficulties Encountered/Overcome

- Assessing LNG plant parameters and gas compositions

- Assessing parameters of specific gas turbines (GE MS6001) for modeling

- Finding suitable property methods in ASPEN for Water/LiBr absorption chiller modeling

# 5.	Planned Project Activities for the Next Quarter

The following activities are to be conducted in the next quarter:

- Modeling LNG refrigeration cryogenic cycles

- Designing and modeling upgrades for the current LNG plant

- Continued modeling of different absorption chiller designs

- Investigating use of gas turbine as compressor drivers for reducing steam consumption and increasing availability and reliability of steam production

# Appendix

Justification and Background

Waste heat utilization opportunities are abundant in the oil and gas industry. Proper use of waste heat could result in improved cycle efficiency, reduced energy usage, reduction in CO2 emissions, and increased production capacity.

CEEE at the University of Maryland has extensive experience in the design and implementation of integrated combined cooling, heating, and power (CCHP) projects. The faculty at PI has experience in the design and operation of petroleum processing plants. Jointly the team is well equipped to address the challenge posed by this project.

Approach

- Assess waste heat (WH) sources (PI)

- Assess WH conversion processes (UM)

- Assess utility requirements (PI)

- Match WH sources/processes and utility requirements (PI, UM)

- Develop/implement of software for system analysis (PI, UM)

- Rank and propose implementation of 1 or 2 preferred systems (PI, UM)

- Define additional R&D as needed (PI, UM)

Two-Year Schedule

June 1, 2007	Report assessing WH sources and utility requirements

June 1, 2007	WH conversion options report

Oct. 1, 2007	Useful version of software

Apr. 31, 2008	Ranking of systems and selection

Nov. 31, 2008	Report recommended steps forward

Key References

- Alefeld, G., Radermacher, R., 1994, “Heat conversion systems”, CRC Press, Boca Raton.

- Al-Hamdan, Q.Z., Ebaid, M.S.Y., 2006, “Modeling and simulation of a gas turbine engine for power generation”, ASME Journal of Engineering for Gas Turbines and Power, Vol. 128, pp. 302-311.

- LNG technology selection,   http://www.fwc.com/publications/tech_papers/files/TariqLNG.pdf, Last access, June, 2008

- Haring, H., 2008, “ Industrial Gas Processing”, Wiley-VCH, Weinheim

- ASHRAE, 2002, “ASHRAE Refrigeration Handbook”, American Society of Heating, Refrigeration and Air-Conditioning Engineers, Atlanta, GA, USA.

- ASHRAE, 2005, “ASHRAE Fundamentals Handbook”, American Society of Heating, Refrigeration and Air-Conditioning Engineers, Atlanta, GA, USA.

- Brant, B., Brueske, S., Erickson, D.C., Papar, R., 1998, “New waste-heat refrigeration unit cuts flaring, reduces pollution”, Oil & Gas Journal, May 18, pp.61-64.

- Brooks, F.,J., 2000 “GE gas turbine performance characteristics”, GE Power Systems Schenectady, NY, GER-3567H.

- Cohen, H., Rogers, G.F.C., Saravanamuttoo, H.I.H., 1996, “Gas turbine theory”, 4th edition, Longman Scientific & Technical, Singapore.

- Erickson, D.C., 2000 “LPG recovery from reformer treat gas”, US Patent 6,158,241.

- Erickson, D.C., Anand, G., Papar, R.A., Tang, J., 1998, “Refinery waste heat powered absorption refrigeration – cycle specification and design”, Proceeding of the ASME Advanced Energy System Division, AES-Vol. 38, pp.391-402.

- Erickson, D.C., Kelly, F., 1998, “LPG recovery from refinery by waste heat powered absorption refrigeration”, IECEC-98-079, 33rd Intersociety Engineering Conference on Energy Conversion, Colorado Springs, CO.

- Giampaolo, T., 2003, “The gas turbine handbook: principles and practices”, 2nd edition, The Fairmont Press, Lilburn, GA.

- Herold, K.E.; Radermacher, R., Klein, S, 1996, “Absorption chillers and heat pumps”, CRC Press, Boca Raton.

- Kim, T.S., Hwang, S.H., 2006, “Part load performance analysis of recuperated gas turbine considering engine configuration and operation strategy”, Energy, Vol. 31, pp., 260-277.

- Klein, S.A., 2005, “Engineering Equation Solver” F-Chart Software.

- Kurz, R., 2005, “Gas turbine performance”, 44th Turbomachinery Symposium, pp.131-146.

- Kurzke, J., 2003, “Model based gas turbine parameter corrections”, GT2003-38234, Proceedings of 2003 ASME TURBO EXPO: Power for Land, Sea, & Air, Atlanta, GA, USA.

- Li, Y.G., Pilidis, P., Newby, M.A., 2006, “An adaptation approach for gas turbine design-point performance simulation”, Journal of Engineering for Gas Turbines and Power, Vol. 128, pp. 789-795.

- Orlando, J.,A., 1996, “Cogeneration design guide”, American Society of Heating, Refrigeration and Air-Conditioning Engineers, Atlanta, GA.

- Pande, M., 1996, “Tools for fractionator design in ammonia-water absorption machines”, Master Thesis, University of Maryland, College Park.

- Walsh, P.P., Fletcher, P., 1998, “Gas turbine performance”, Blackwell Science, Oxford.

Energy Efficient Transport Process Projects

Thermally Enhanced Polymer Heat Exchanger for Seawater Applications UM Investigator(s): Prof. Avram Bar-Cohen, Prof. S.K. Gupta GRA(s): Juan Cevallos, Patrick Luckow PI Investigator(s): Dr. Peter Rodgers, Dr. Ahmed Abdala Start Date: October 2006 Report Date: 07 July 2008

1.	Objective/Abstract

The proposed two-year study will address the fundamental thermal performance issues associated with the use of thermal high-conductivity polymer materials, addressing their advantages and limitations and defining the heat exchanger configurations that optimize the unique characteristics of high conductivity polymer materials.

To achieve optimum thermal performance, a clear understanding of the thermal engineering characteristics of fiber-enhanced polymer tubes/channels and the fundamental thermo-fluid predictive relations that underpin heat exchange in such configurations will be developed.

Successful completion of this effort will provide fundamental thermofluid modeling relations for thermally enhanced polymer tubes and channels; it will also provide the basis for determining the environmental, weight, and cost advantages resulting from future applications of this technology to seawater heat exchangers for shipboard heat exchangers and for the petroleum and power industries.

2.	Deliverables

- Build the laboratory scale test apparatus, calibrate and begin data collection.

- Summarize least-material optimization work for a draft paper.

- Patrick Luckow will work at the PI from June 2 to July 5 to assist in reviewing ADGAS heat exchanger data for designing a prototype polymeric heat exchanger.

- Complete review paper on polymer heat exchangers.

- Complete Moldflow filling parametric analysis and create response surface models.

- Complete experimental verification of Moldflow filling simulation.

- Complete experimental verification of fiber orientation Moldflow prediction.

3.	Summary of Project Activities for the Completed Quarter

- Build the laboratory scale test apparatus, calibrate and begin data collection.

  - Crossflow heat exchanger and manifolds were built with Stratasys Dimension FDM equipment, using FDM-grade ABS plastic.

  - A second heat exchanger, made of thermally-enhanced thermoplastic material-filled Nylon 12 from PolyOne, was injection-molded in small pieces and assembled with epoxy. Figure 1 below shows pictures of the individual parts of the PolyOne material, as well as the assembled heat exchanger.

| (a) Injection Molded Parts | (b) Assembled heat exchanger |
| --- | --- |
| Figure 1. Cross-flow heat exchanger made with thermally enhanced Nylon 12 |

  - Test equipment was purchased and installed, as shown schematically in Figure 2. Labview code was written to collect and process thermocouple and fluid flow data measurements. Initial calibration was done using built-in calibration functions in the thermocouple DAQ module, and refined calibrations were done using ice baths and boiling water.

Figure 2. Polymer heat exchanger test apparatus

  - Data was collected for the unfilled polymer heat exchanger, and results are presented in Figure 3. Error analysis revealed an overall 15.7% uncertainty, reflected in the figure.

Figure 3. Experimental temperature drop over unfilled polymer heat exchanger, compared to predicted results

- Summarize least-material optimization work for a draft paper.

  - Results of least-material studies were summarized in a draft paper for submittal to 2009 Tunisia conference on Convective Heat and Mass Transfer in Sustainable Energy, and initial revisions were completed.

- Patrick Luckow will work at the PI from June 2 to July 5 to assist in reviewing ADGAS heat exchanger data for designing a prototype polymeric heat exchanger.

Patrick was at the PI from June 5 to June 30, where he completed the following tasks:

  - Assessment of UM HX test facility

    - Analyzed experimental data obtained, and compared with predictions.

    - Completed a sensitivity analysis of HX air side temperature drop as function of thermal conductivity and heat transfer coefficient.

    - Assessed the potential effects of using methane as opposed to air in the experiment.

    - Reviewed Nusselt number correlations for both laminar and turbulent flow, which included simultaneously developing and fully developed flows, and assessed the sensitivity of the predicted HX air side temperature drop to the specific Nu number correlation used.

    - Completed a parametric study of heat exchanger outlet temperature as a function of fin spacing and thermal conductivity, for 2 flowrates and 2 fin thicknesses.

    - Completed experimental error analysis.

  - Studied and summarized design specifications of a shell-and-tube heat exchanger used for natural gas liquefaction at Das Island.

  - Revised draft paper on heat exchangers least-material optimization for future submission.

- Complete review paper on polymer heat exchangers.

The first draft of the paper is underway and will be delivered by Juan Cevallos on July 10th, 2008.

- Complete Moldflow filling parametric analysis and create response surface models.

Mahmoud Adi, a senior undergraduate at The Petroleum Institute, is currently completing his summer internship at UM. He is running Moldflow simulations as part of a two-level factorial design experiment. Multi-level design will be considered once the two-level analysis is finished. Six variables are being considered:

1.     Melt Temperature  (TM)

2.     Fin Spacing  (S)

3.     Fin Height (H)

4.     Fin Thickness (t)

5.     Base Thickness (tb)

- Base Surface Area (Ab)

The total number of runs is 64. For each run, the cycle time (filling, packing, and cooling) and the number of gates required for filling is recorded. A single simulation may vary in running time from one to fifteen hours, depending on the part’s dimensions and the analysis type. Twenty-six simulations have been completed so far.

.

- Complete experimental verification of Moldflow filling simulation.

  - A spiral aluminum mold was machined using CNC equipment. The cross-section of the spiral is 2.286 mm wide by 1.27 mm tall.

  - The spiral mold was used to conduct filling experiments using the Babyplast injection machine to create parts with PolyOne’s thermally enhanced Nylon 12 (NJ 6000 TC). The parts were injected at two different pressures: 150 MPa and 180 MPa, with a melt temperature of 270 C. The measured length of the spirals was compared with the length predicted by Moldflow under similar conditions. Figure 4 below shows a plot comparing the experimental results to those predicted by Moldflow. Moldflow predictions are approximately within 15% of the experimental measurements

Figure 4. Experimental verification of Moldflow filling predictions

- Experimental verification of fiber orientation Moldflow prediction.

The verification of the Moldflow fiber orientation prediction has been superseded by measurement of the thermal conductivity of the thermally-enhanced Nylon 12 provided by PolyOne. The purpose of this experiment is to measure the actual in-plane and out-of-plane conductivities and compare them with the nominal value given by the vendor.

The out-plane conductivity has been measured using the laser flash method and the results are shown in Table 1 below:

Table 1.  Thermal conductivity measurements using laser flash method for out-of-plane samples

| Sample | ρ (g/cm3) | α (cm2/s) | Cp (J/Kg.K) | k (W/m.K) |
| --- | --- | --- | --- | --- |
| 1 | 1.513 | 0.02398 | 1.030 | 3.737 |
| 2 | 1.500 | 0.02196 | 1.100 | 3.625 |
| 3 | 1.503 | 0.02404 | 1.155 | 4.172 |

- Difficulties Encountered/Overcome

None to report.

5.	Planned Project Activities for the Next Quarter

- Data collection on thermally enhanced PolyOne polymer heat exchanger.

- Complete revisions on least-material optimization paper.

- Patrick Luckow, Juan Cevallos, Avram Bar-Cohen and Peter Rodgers are scheduled to attend the 2008 Energy Sustainability Conference August 10-14 to present their paper, “Energy Efficient Polymers for Gas-Liquid Heat Exchangers.”

- Submit Polymer Heat Exchangers review paper to a professional publication.

- Measure in-plane thermal conductivity of PolyOne thermally-enhanced Nylon 12, and complete experimental verification of fiber orientation Moldflow prediction.

- Complete Moldflow filling parametric analysis and create response surface models.

- Juan Cevallos will complete a first draft of his Master’s thesis.

Appendix

Justification and Background

High thermal-conductivity polymer heat exchangers could play an important role in seawater-based cooling systems for the power industry, naval applications, and coastal petroleum refineries. Such advanced heat exchangers could facilitate the more direct use of seawater in these applications, while providing reduced weight, greater resistance to corrosion and fouling, reduced energy consumption, and greater geometric flexibility and ease of manufacturing, relative to the technology in use today.

While conventional metal heat exchangers are generally incapable of providing reliable long-term service with salt water (and other corrosive fluids), to date the cost, complexity, and the restricted availability of exotic corrosion-resistant materials have limited the design and application of seawater heat exchangers.

Compact, high performance heat exchangers fabricated of high thermal-conductivity polymers offer a promising alternative to these exotic materials in refineries and power plants located along the coast, where seawater is the primary coolant.

Approach

1.	Review the available compact liquid-liquid heat exchanger concepts, e.g., shell-in-tube and plate-coil, and identify their strengths and weaknesses.

2.	Define the relevant heat exchange metrics, e.g., kW/m3 and COP (kW heat/kW pumping), and rank the concepts by these metrics.

3.	Review and tabulate the thermal, chemical, and mechanical properties of thermally enhanced polymer materials suitable for use in liquid-to-liquid heat exchangers.

4.	Apply the selected metrics to conventional polymer and thermally enhanced polymer heat exchangers, and re-rank the heat exchanger concepts.

5.	Develop new polymer nanocomposite materials and compare their thermal, chemical, and mechanical properties to the best-known thermally enhanced polymeric materials.

6.	Select the most promising polymer materials and configuration(s) for seawater heat exchange and determine the theoretical performance limits for these configurations/materials.

7.	Fabricate and test polymer tube/channel heat exchanger “building blocks” to determine the pressure drop and heat transfer coefficients achievable.

8.	Correlate baseline thermofluid data for “building block” tube/channels and compare to theoretical predictions.

9.	Develop a test loop for testing of pilot scale polymer heat exchangers, representative of industrial applications.

10.	Develop recommendations for seawater-cooled, thermally enhanced polymer heat exchangers for specific applications, such as in the power industries, refineries, and aboard ships.

Two-Year Schedule

Year 1:

  - Conduct literature review on: (i) the strengths and weaknesses of various commercially available heat exchanger designs and (ii) current usage of polymer heat exchangers.

  - Assess the thermal, chemical, and mechanical properties of thermally-enhanced polymer materials suitable for use in liquid-to-liquid heat exchangers.

  - Assess theoretical performance limit of polymer candidate materials and configuration(s).

  - Construct laboratory-scale test apparatus for thermal characterization of polymer heat exchanger “building block” tube/channels.

  - Fabricate polymer nanocomposite materials suitable for polymer heat exchangers.

  - Characterize thermal properties of polymer “building block” tube/channel heat exchanger test vehicles.

  - Correlate baseline thermofluid data for “building block” tube/channel with theoretical predictions.

Year 2:

- Construct a test loop for thermal characterization of pilot scale polymer heat exchangers representative of industrial applications.

- Characterize thermal properties of pilot-scale polymer heat exchangers.

- Recommend seawater-cooled, thermally enhanced polymer heat exchangers for specific applications.

Key References

- Zaheed, L., and Jachuck, R.J.J., 2004, “Review of polymer compact heat exchangers, with special emphasis on a polymer film unit,” Applied Thermal Engineering, Vol. 24, No. 16, pp. 2323-2358.

- Bahadur, R., and Bar-Cohen, A., 2005, “Thermal Design and Optimization of Polymer-Based Pin Fin Natural Convection Heat Sinks,” IEEE Transactions on Components and Packaging Technologies, Volume 28, Issue 2, pp 238-246.

- Zweben, C., 2003, “Emerging High-Volume Commercial Applications for Thermally Conductive Carbon Fibers,” Sixth International Business Conference on The Global Outlook for Carbon Fiber, San Diego, California, USA, November 5 – 7.

- Shah, R.K., 2006, “Advances in science and technology of compact heat exchangers,” Heat Transfer Engineering, vol. 27, no. 5, pp. 3-12.

- Pugh, S. J., et al, 2005, “Fouling During the Use of Seawater as Coolant—the Development of a User Guide,” Heat Transfer Engineering, vol. 26, no. 1, pp. 35-43.

- Zweben, C., 2004, “Emerging High-Volume Commercial Applications for Advanced Thermally Conductive Materials,” SAMPE 49th International Symposium and Exhibition, Long Beach, California.

- Bahadur, R., and Bar-Cohen, A., 2005, “Thermal Design and Optimization of Polymer-Based Pin Fin Natural Convection Heat Sinks,” IEEE Transactions on Components and Packaging Technologies, Volume 28, Issue 2, pp 238-246.

- Suzuki, T. and Takahashi, J., 2005, “Prediction of energy intensity of carbon fiber reinforced plastics for mass-produced passenger cars,” 9th Japan International SAMPE Symposium JISSE-9, Tokyo, Japan, 29 November–2 December, 2005.

- Wang, L., and Sundén, B., and Manglik, R.M., 2007, “Plate Heat Exchangers: Design, Applications and Performance,” WIT Press, Volume Billerica, MA.

- Kampe, S.L., 2001, “Incorporating Green Engineering in Materials Selection and Design,” 2001 Green Engineering Conference, Roanoke, Virginia, July 29-31 2001.

- Osswald, T.A., and Hernández-Ortiz, J.P., 2006, “Polymer Processing: Modeling and Simulation,” Hanser Gardner, Cincinnati, OH.

An EHD-Enhanced Gas-Liquid Separator UM Investigators: Dr. Serguei Dessiatoun, Dr. Amir Shooshtari GRA’s: Mohamed Alshehhi PI Investigator(s): Dr. Michael Ohadi, Dr. Afshin Goharzadeh Start Date: October 2006 Report Date: 15 July 2008

1.	Objective/Abstract

To study hybrid inertia-EHD gas-liquid separation phenomena for electrically conductive and nonconductive liquid particles suspended in a moving gaseous medium. This is useful in a variety of applications including petrochemical and process industries, refrigeration and cryogenics, and micron/sub micron air filtration and clean room applications.

2.	Milestones/Deliverables

- Air-oil separation

- Journal paper highlighting numerical modeling work

- Trip to ADNOC companies to develop research opportunities

3.	Summary of Project Activities for the Completed Quarter

- Air-Oil Separation

The experimental test setup for the air-oil separation was slightly modified to enable safe operation and environmental conditions for the Aerodynamic Particle Siezer (APS). The following modifications were

- A bypass T-section, installed before the separator to enable conducting tests with different air flow rater.

- Two T-sections tubes, installed before and after the test section (EHD oil separator) to examine the efficiency of the separator.

- A conventional oil separator (Emerson model), installed before the test section (EHD oil separator) to promote cleaner air, since the APS is very sensitive to small particles.

Figure (1) shows the experimental test setup after the modifications.

Figure 1. Air-oil separator test setup

The oil separator geometry is a wire-cylinder separator. The diameter of the wire and cylinder are 0.08 mm and 50 mm, respectively. The length of the cylinder is 100 mm.

The experiments allowed the air to pass through the oil reservoir, where the oil droplets were injected in the airflow. Then the air-oil droplet mixture passed into the conventional oil separator at the first stage of the separation to clean the air of the big oil droplets and other particulates of matter. After the first stage of the separation, the mixture passed into the EHD oil separator to remove the finer oil droplets.

The tests focused on inspecting the behavior of the droplets under voltage variations. Figure 2 and Figure 3 show the effect of applied voltage on particle concentration at different flow rates.

Figure 2. Particle concentration and mean diameter vs. applied voltage at air flow rate = 70 L/min and oil injection rate = 0.1 g/min

Figure 3. Particle concentration and mean diameter vs. applied voltage at air flow rate = 30 L/min and oil injection rate = 0.15 g/min

Particles behaved the same in the two tests, with an error percentage within 5 %. Particles began to break up as the applied voltage increased. This is because the charge on droplets overcame the surface tension, which is known as Rayleigh’s limit.

The efficiency was calculated based on the particle concentration of oil droplets (Number/cm3) before and after the EHD separator.  The aerodynamic particle sizer was used to obtain the particle concentration. The formula used to calculate the efficiency is

Since the way that efficiency is calculated depends on the number of particles, then in the first case this equation could be applied since the number leaving the separator is larger. For the second case, the efficiency was about 70% at 20 kV.

- Journal Paper

A journal paper is being prepared for submission to the journal Aerosol Science and Technology. The paper highlights the numerical modeling findings.

- Visit to ADNOC Companies

Two field trips were taken in the last quarter to find academic research opportunities.

- FLUOR visit (Apr 6-9 2008)

This visit was initiated by GASCO to become familiar with the ongoing project between the two companies. The project is called Sour Gas Development (SGD), which involves purifying gas from sulfur.

- UAE visit (May 4-9 2008)

The purpose of this trip was to visit some of ADNOC’s on/off shore fields. The fields visited were the Habshan plant (GASCO) and Das Island (ADGAS). Also, the visit involved many successful meetings with both companies and PI. Many applications for the separation work have been identified and discussed.

Follow-up work will include a short proposal to these companies to win their support for research in gas production.

4.	Difficulties Encountered/Overcome

Some challenges in the design of gas-and-conductive liquid separator are

- Preventing charge leakages and/or shortages due to the conductive nature of fluid

- Designing power supply and control mechanisms

5.	Planned Project Activities for the Next Quarter

- Test air-oil separator with different electrode geometries

- Conduct numerical modeling studies with turbulent flow

- Finish a journal paper highlighting the numerical modeling to be submitted to Aerosol Science and Technology journal

Appendix

Justification and Background

Separation comprises a significant part of the oil and natural gas production process.  In many stages of this process, electrostatic separation significantly increases the efficiency and often decreases the cost of production. Most of the oil producers, including ADNOC, operate where the climate is hot and therefore use refrigeration and air-conditioning equipment.  The efficiency and reliability of this equipment appreciably suffers due to mal-distribution of lubricant oil in the system. Electrostatic separation can correct this mal-distribution and improve the efficiency of this refrigeration and air-conditioning equipment.   Similarly, vapor compression equipment with lubricant circulation is also used in oil refinery processes. This circulation can be significantly improved using EHD separators to increase heat-pumping efficiency. UM has already developed a working prototype for gas-and-non-conductive droplet separation. However, the fundamentals of this separation mechanism must be better understood to enable optimization of the working design. There is also a need to explore the feasibility of separation of gas-and-conductive liquid mixtures, which poses additional challenges.

Conventional gas/liquid separators are based on inertial and gravitational forces. They have poor efficiency when separating micron-size particles in the flow due to low gravitational and inertial forces acting on small particles. In contrast, electro-hydrodynamic (EHD) forces strongly affect particles of such size. The combination of a conventional separator with EHD allows us to create the most effective and lowest pressure-drop particle separator, with potential applications to separation of electrically conductive and non-conductive liquid particles. The separation of electrically conductive particles like water-air mixtures (fog) imposes significant design constraints on separator electrode design and high-voltage power supply selection.

Approach

Detailed analysis and identification of the phenomena and the design challenges involved in effective implementation of the mechanism. Parametric study of existing and improved separators. Design iterations, including numerical flow and field simulations, fabrication, and testing. Creation of database and engineering design correlations.

Two-Year Schedule

Year 1:

- Conduct literature review to study current technologies for separation of solid or liquid particles from gas flows by electrostatic and electro-hydrodynamic (EHD) forces.

- Evaluate existing technologies and assess their applicability to flow separation of gas-and-liquid-droplet mixtures.

- Evaluate and optimize current designs of UM EHD separators for non-conductive liquid particles in gas flow.

- Design and fabricate a two-phase gas-liquid droplet separator capable of operating with conductive fluids. Conduct a parametric study of separators for different conductive fluids, concentrations, and gas flow rates.

Year 2:

- Continue optimization and numerical study of hybrid gas-and-non-conductive liquid droplet separator. Continue parametric experimental study of gas-and conductive separator.

- Design iterations and implementation.

- Experiment on different designs.

- Present the best design to ADNOC group of companies.

- Develop design correlation.

- Prepare report.

Key References

- Mo, B., Ohadi, M.M., and Dessiatoun, S.V., "Liquid vapor separation and thermal management in an EHD-enhanced capillary pumped loop," Heat Transfer 1998, Proceeding of 11th International Heat Transfer Conference, Vol. 2, Taylor & Francis Inc., Levittown, PA, pp.63-68.

- Ohadi, M. M., Ivenkenko, I., and Dessiatoun, S., “Electrohydrodynamic Liquid-Vapor Separator,” USA Pat.# 6,582,500

- Schrage, D.S., Shoemaker, J.M., and McQuillen, J., 1998, “Passive two-phase fluid separation,” AIAA 36th Aerospace Sciences Meeting & Exhibit, Reno, NV, Jan. 1998, AIAA-98-0731

- Balachandran, W., Machowski, W., Ahmad, C.N. “Electrostatic atomization of conducting liquids using AC superimposed on DC fields,” Industry Applications, IEEE Transactions on Volume 30, Issue 4, July-Aug. 1994 Page(s):850 - 855 Digital Object Identifier 10.1109/28.297899

Study of Condensing Flows in a Micro-scale Channel with a Micro-element Array and Visual Techniques UM Investigators: Dr. S. Dessiatoun, Dr. A Shooshtari GRA’s: Ebrahim Al-Hajri PI Investigator(s): Dr. M. Ohadi, Dr. A. Goharzadeh Start Date: December 2006 Report Date: 15 July 2008

1.	Objective/Abstract

The proposed two-year study will investigate, by different experimental techniques, the fundamentals of the two-phase condensing flow phenomenon in a sub-millimeter microchannel. In order to understand the mechanism of the flow, local measurements of heat flux, temperature and flow velocities are necessary. The present project intends to use an optimum flow-visualization technique to measure heat flux distribution and local fluid- and vapor-phase velocities, respectively.

2.	Deliverables for the Completed Quarter

- Completed constant-quality pressure drop testing of condensation in microchannels with R-134a and R245fa.

- Designed a visualization microchannel condenser and ordered a high-speed camera.

3.	Summary of Project Activities for the Completed Quarter

Constant-quality tests for pressure drop study in microchannel for refrigerants R134a and R245fa have been completed. The tests were carried out to study the effects of mass flux, saturation temperature and quality on pressure drop. The table below shows the test matrix for this investigation.

The results for both refrigerants are shown in Figures 1-8. The results were consistent and repeatable. Both refrigerants show similar trends in each of the studies, which increases our confidence in the outcome. The study of the effect of saturation temperature shows that for a constant mass flux, increasing vapor quality decreases both vapor density and vapor viscosity, causing an increase in the velocity, which therefore increases pressure drop. For example, at 30 oC saturation temperature, vapor density and vapor viscosity decrease 7 times and 15 times, respectively, when increasing vapor quality from 0.1 to 0.9; thus, the pressure drop increases. On the other hand, surface tension has a negative effect on pressure drop; however, the effect of vapor density and vapor viscosity is dominant.

Our study of mass flux revealed that as mass flux is increased, pressure drop increases, as shown in Figures 2 and 6. This can also be seen in Figures 3 and 7, where the pressure drops of two different testing conditions are relatively close.

System instability prevented some tests using R245fa from being completed.

Table 1. Parametric Test Table for Constant Quality Test for Pressure Drop

Table 2. Liquid and Vapor Properties of R134a

| Tsat (oC) | lv | l (kg/m3) | v (kg/m3) | lv | l (kg/m-s) | v (kg/m-s) | (N/m) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 7.032 | 292.2 | 41.55 | 14.99 | 0.0001827 | 0.00001219 | 0.007418 |
| 40 | 6.492 | 359.5 | 55.38 | 12.71 | 0.0001612 | 0.00001268 | 0.006127 |
| 50 | 5.879 | 430 | 73.15 | 10.7 | 0.0001416 | 0.00001324 | 0.004891 |

Figure 1. Effect of saturation temperature on local pressure drop for R134a at mass flux = 300 kg/m2s

Figure 2. Effect of mass flux on local pressure drop for R134a at Tsat = 50 oC

Figure 3. Comparison of two local pressure drop curves at different conditions

Figure 4. All the results for R134a

Figure 5. Effect of saturation temperature on local pressure drop for R245fa at mass flux = 300 kg/m2s

Figure 6. Effect of mass flux on local pressure drop for R245fa at Tsat = 50 oC

Figure 7. Comparison of two local pressure drop curves at different conditions

Figure 8. All the results for R245fa

4.	Difficulties Encountered/Overcome

None.

5.	Planned Project Activities for the Next Quarter

- Conduct visualization experiments in the microchannel

- Conference paper and/or article.

Appendix

Justification and Background

With the development of new manufacturing technologies and fluid maintenance techniques, miniaturization of heat transfer systems has proven to be possible and to afford great economic benefits.  Two orders of magnitude of reduction in system weight and volume with significant reductions in cost have become feasible. Sufficient data and advanced modeling are available to characterize boiling processes in microchannels. However, such data are lacking for condensing flows in micro-scale passages and are necessary for development of predictive models and correlations in the future.

This project will be conducted in two parts. To investigate local heat transfer with precision, the first part will use the micro-fabricated element-array technique to measure local heat flux and temperature profiles.  This will enable understanding of the flow and condensation process in greater detail than traditional methods have presently allowed. In the second part, flow visualization at the micro-scale will be used to complement the heat transfer experiments to provide data on velocity profiles and flow dynamics that are unobtainable by heat transfer measurements. This combined data set will be used in future predictive models and correlations, which will pave the way for optimization of two-phase, high-performance heat transfer systems.

In the present age of miniaturization, there is a need to understand flow phenomena in compact phase-change-type micro-fluidic systems. In recent years, work has characterized the boiling phenomenon using high-speed optics, micro-heater arrays for local wall temperatures, and heat flux measurements and Particle Image Velocimetry (PIV) techniques. Those techniques significantly improve the understanding of boiling phenomenon. Similar experiments in condensation, particularly micro-array heat flux and temperature experiments combined with PIV studies can provide extremely valuable information for the understanding of the condensation phenomenon in microchannels.

Approach

UM-side participation

(a) Conduct an extensive literature survey for experimental studies on condensation of refrigerants in microchannels of hydraulic diameter 1 mm or less, and extract useful data for heat transfer and pressure drops. (b) Conduct a survey of literature for analytical/numerical models in microchannel condensing flows and study them. Understand inputs typically needed for predictive models. (c)  Work with PI to conduct a survey of literature and vendors for flow visualization of two-phase micro-fluidic systems.

Based on above literature study, design prototype of a microchannel with a platinum micro-resistors array and experimental loop.

Develop the processes for micro-array fabrication and microchannel fabrication and make necessary design changes to accommodate technical issues. Finalize experimental prototype design.

Fabricate prototype and complete instrumentation. Fabricate experimental loop.

Test experimental loop for various mass flow rates of a suitable refrigerant fluid at different two-phase qualities. Collect test data on local heat fluxes on channel walls, overall pressure drop, and high-speed digital video evidence.

Work with PI to fabricate the recommended flow-visualization prototype and associated experimental loop parts.

PI-side participation

- Work with UM to conduct an extended literature survey on the flow visualization on micro-fluidic systems focusing on multi-phase flow.

- Develop the optimum flow visualization system for multi-phase flow inside a microchannel.

- Work with UM to recommend a design suitable for the optimum visualization technique. Develop requirements and recommendations for a flow-visualization test section that will be fabricated by UM.

- Conduct flow visualization measurements inside the microchannel prototype designed and fabricated at UM.

5.	Compare flow-visualization data with UM micro-array data.

Two-Year Schedule

UM-side participation

Year 1.

Literature review and summary.

Design of micro-array prototype.

Investigation of micro-array fabrication.

Fabrication of experimental setup.

Year 2.

Final fabrication of micro-array prototype.

Final fabrication of visualization prototype and loop.

Experimentation on micro-array.

Final report.

PI-side participation

Year 1.

Literature review and summary.

Development of optimum visualization setup.

Year 2.

Experimentation on visualization setup designed and fabricated in UM.

Final report.

Key References

- Kim, J., Benton, J., McQuillen and J, Vickerman, M., 2001,”Subcooled Pool Boiling in Microgravity and Hi-g,” Journal of Heat Transfer, vol. 123, iss. 4, pp. 620.

- Lee, J., Kim, J. and Kiger, K. T., 2000, “Time and Space Resolved Heat Transfer Characteristics of Single Droplet Cooling Using Microscale Heater Arrays,” International Journal of Heat and Fluid Flow, Vol. 22, pp. 188.

- Begg, E., Khustalev, and D., Faghri, 1999, “Complete Condensation of Forced Convection Two-Phase Flow in a Miniature Tube,” Journal of Heat Transfer, Vol. 121, pp. 904.

- Garimella, S., 2004, “Condensation Flow Mechanisms in Microchannels: Basis for Pressure Drop and Heat Transfer Models,” Heat Transfer Engineering, vol. 25, iss. 3, pp. 204.

- Yang, C.Y. and R.L. Webb, 1996, “Friction Pressure Drop of R-12 in Small Hydraulic Diameter Extruded Aluminum Tubes with and without Micro-Fins,” Int. J. Heat Mass Transfer, vol. 39, iss. 4, pp. 801.

- C. D. Meinhart, S. T. Wereley, J. G. Santiago, 1999, “PIV measurements of a microchannel flow” Exp. In Fluids, vol. 27, pp 414.

Energy System Management Projects

Robust Optimization of Petrochemical Systems UM Investigator: Dr. Shapour Azarm PI Investigators: Dr. Saleh Al Hashimi and Dr. Tareq Al Ameri UM’s GRA: Mr. Weiwei Hu PI’s GRA: Ms. Naveen Al Qasas Acknowledgement: Dr. Mian Li Start Date: 16 April 2008 Report Date: July 1 2008

1.	Objective/Abstract

The objective of our study continues to be the development of a framework for robust optimization of petrochemical systems based on the net profit and/or performance effects. In this reporting cycle, we have tried to address some of the problems associated with the computational costs with our previously developed robust optimization approach. As a result, we proceeded with our investigations and developed a faster robust optimization approach. We are pleased to report that we now have some encouraging preliminary results for such an approach. Moreover, since our last quarterly report, the prototype simulation model for the distillation column has been further extended by our collaborators at PI to include a coupled reactor-distillation simulation model. Our research effort will continue to further refine this coupled simulation model and the corresponding optimization approach for this model.  The simulation model (or case study) for the reactor-distillation system will be used to demonstrate the applicability of the proposed robust optimization approach.

2.	Deliverables for the Completed Quarter

- A preliminary decomposed bi-subsystem multi-objective optimization model, i.e., reactor-distillation simulation model, for a petrochemical system has been under development.

- A multi-objective, multi-disciplinary optimization problem has been set up for the reactor-distillation model, and the convergence of the entire system has been tested.

- Some preliminary Pareto solutions to the reactor-distillation system optimization problem in the deterministic case have been obtained.

- A new and more efficient single-objective, single-level robust optimization method that considers feasibility robustness has been proposed by UM and is under development to address the computational difficulties experienced in the previously proposed robust optimization approach.

- The proposed single-level robust optimization method is under testing using a single-objective distillation column optimization problem in addition to a couple of other numerical/engineering examples. Our preliminary results indicate that the computational efficiency of this new robust optimization is significantly better than our previous method.

- An abstract for a conference paper was submitted by PI on behalf of the PI-UM work to the International Conference on Modeling, Simulation, and Applied Optimization (ICMSAO) in Sharjah 2009. We have just been informed that this abstract has been accepted and we will submit a full paper for this conference by September 2008.

- Two PI-UM joint papers are under development: one paper is in the area of combining robust optimization and sensitivity analysis, and the other is on the new single-level robust optimization approach for single-objective optimization problems.

3.	Summary of Project Activities for the Completed Quarter

- UM and PI had three teleconferences on April 29th, May 20th and June 18th. A summary of the minutes from these meetings is given below:

- UM presented the previously developed bi-subsystem (reactor-distillation) deterministic optimization problem and its corresponding results using an "all-at-once" optimization approach. PI commented that ni (an input to the reactor model) should be kept fixed and perhaps should be used in the future as part of the robust optimization effort (i.e., let ni have uncertainty). PI also proposed a revised/new model for the reactor-distillation system. This model was expected to have multiple subsystems, with each subsystem to have multiple objectives. Once this model is developed by PI, UM is expected to solve it using its decomposition based optimization techniques and report back the results to PI for further considerations and extensions.

- PI presented slides on "The Production of Phthalic Anhydride from O-Xylene." These slides essentially summarized three subsystems, which involved a reactor and two distillation towers. The modeling for these subsystems was recently completed by PI and submitted to UM for further development as an optimization problem, as a decomposed or undecomposed case study.

- UM presented a new robust optimization approach. The purpose of this new approach was to make the previously developed outer-inner robust optimization approach more efficient.

- PI updated their reactor-distillation model. PI discussed the details of this new reaction-distillation system that they were working on. This model included one reactor and two distillation towers. This model was used for a multi-product reaction-distillation process. PI reported that a decomposed model for this process was in place; PI is in the process of finalizing the model and sending it to UM.

- UM and PI are planning for three papers based on their joint work. The first paper is a conference paper whose abstract was just accepted (see Deliverables). The other two papers are journal articles. A draft of one of these two papers was prepared a while back. This paper was in the area of combining robust optimization with sensitivity analysis. The other journal paper is focused on the newly developed robust optimization method.

- The originally (or previously) developed reactor-distillation (bi-subsystem) model consisting of a reactor model and a distillation model was completed by PI and submitted to UM for the optimization study. Based on this model, the interaction between the two subsystems is defined through a two-way coupling as shown in Figure 1. The first coupling, which is a mixture of propane and propylene after the reaction procedure, derives from the reactor model. The mixture is then fed to the distillation column where the first stage separation is made. The second coupling is from the distillation column to the reactor. It is assumed that un-reacted propane (a constituent of the bottom) leaves the distillation column and is fed back to the reactor, where it is mixed with fresh feed and run through the reaction process again. To conduct the design optimization for this reactor-distillation (bi-subsystem) problem, the coupling was broken up by adding a target value for the corresponding coupling and by enforcing the requirement that the coupling variable must converge to its target. In this problem, as shown in Figure 2, the RUP generated from the distillation column and fed back to the reactor, called RUPDist., could be artificially broken up via a target variable called  RUPRct..

Figure 1. Couplings between two subsystems in the reactor-distillation model

- Figure 2 shows how this convergence requirement worked for the bi-subsystem model. We used the target variable RUPRct. as part of the inputs to the reactor to start the simulation of the reactor model. The value of RUPDist. is available when the simulations of those two subsystems are finished. If the value of RUPDist is equal to the value of RUPRct that we used, the two subsystems are said to be consistent. In our optimization problem, we searched for alternatives (i.e., design variables [see below] plus the target RUPRct) that are able to satisfy the convergence condition.

Figure 2. Convergence condition of the reactor-distillation model

- The objectives of the originally developed reactor-distillation optimization problem were to maximize the purity of the distillation stream and maximize the overall profit. We formulated this problem as a multi-disciplinary optimization problem in an all-at-once fashion. Because there are two subsystems in the reactor-distillation model, they must be consistent in such a way that the difference between the coupling variable and the target variable is as small as possible, as formulated in Figure 3. The optimization model has six variables, two for the reactor subsystem and four for the distillation column.

Figure 3. Formulation of reactor-distillation system

- The Pareto optimum solutions using two different threshold  values are shown in Figure 4, i.e. and

Figure 4. Bi-subsystem optimization results

- In our previously reported bi-level robust optimization approach, the robustness of each design alternative had to be evaluated by an inner optimization problem for all possible uncertain parameters, which led to a significant increase in the computational effort for the robust optimization approach. To overcome this burden, we have proposed a new robust optimization approach that has a single-level (instead of outer-inner or bi-level) optimization structure. As shown in Figure 5 (see also Figure 6), we consider a relaxed problem with more constraints than the deterministic optimization problem. The relaxed problem becomes equivalent to the robust optimization problem when we consider every possible uncertain parameter value in the constraints of the relaxed problem. However, it is possible that we could use a certain number (subset), i.e., K, of uncertain parameter values to represent all possible uncertain parameter values. In this regard, it is possible that the relaxed problem is computationally less expensive than our previous bi-level (outer-inner) optimization approach if K is relatively small. To compare, among the three types of optimization problems under consideration (Figure 5), the deterministic problem involves the least computational cost, while the robust optimization is the most expensive to carry out since it has essentially an infinite number of constraints.

Figure 5. Comparison of computational cost for three types of optimization problems

- In the proposed new robust optimization approach, we can approach the feasibly robust optimum solutions by gradually cutting the feasible domain of the relaxed optimization problem. Essentially, the optimum solution of a relaxed robust optimization will converge to the optimum solution of the robust optimization problem by gradually adding new constraints to the relaxed problem using some "outstanding" uncertain parameter values (see the next bullet). The three ellipses in Figure 6 represent the feasible domain of the deterministic, relaxed and robust optimization problems. With some additional constraints, it can be shown that the feasible domain of the relaxed problem will approach that of the robust problem.

Figure 6. Relationship of feasible domains in the design space

- The flow chart of the newly proposed, single-level, feasibility-based robust optimization algorithm is shown in Figure 7. The algorithm starts from the relaxed problem, which is the same as the deterministic problem when the iteration counter i = 0. After we obtain the optimum x(i), we can reduce the feasible domain of the relaxed problem by finding the “outstanding” parameter value ∆p(i) with respect to x(i) and adding a set of new constraints (i.e., J constraints) back to the relaxed problem using this ∆p(i) value. The outstanding ∆p(i) is the one which leads to the largest violation in constraint functions, given x(i). The stopping criteria will be applied to test the robustness of the current optimum x(i) by using an optimization problem. This optimization problem is used not only to test the satisfaction of x(i) by all J constraints with respect to all possible uncertain parameter values, but also to find the outstanding ∆p(i) value. Consequently, if x(i) is satisfied by all J constraints, it is a feasibly robust solution, and the algorithm will end. We have some preliminary results that show that the obtained results from this algorithm are both feasibly robust and optimum for single-objective optimization problems with interval uncertainty.

Figure 7. Algorithm of an efficient approach to robust optimization

- We demonstrate this single-level robust optimization approach using the distillation column design problem. The objective is to maximize the overall profit of the distillation process. There are two parameters, F and X, which have uncontrollable variations. Among the four variables in the optimization model, two of them (N1 and N2) can take only integer values, and the other two take continuous variables. The formulation of this optimization problem is shown in Figure 8. As mentioned before, in this problem, we assume that the uncertainty does not affect the objective function, and robustness is considered only with respect to the constraints, i.e., feasibility robustness.

Figure 8. Formulation of the robust optimization problem of the distillation column

- The feasibly robust and optimum solutions of this problem are obtained in two iterations (Figure 9(a)) by the new single-level approach. The computation cost and accuracy of this new approach is attractive compared to our previous approach. Figure 9(b) shows that the solution using the new approach (in the red triangle) agrees with the ones from our previous bi-level approach (in the black circle). We can also show that the proposed approach is significantly less computation-intensive than our previous bi-level approach.

(a)

(b)

Figure 9. Result of the single-level robust optimization

4.	Difficulties Encountered/Overcome

Based on the reactor-distillation model developed by PI earlier in April, UM was able to successfully set up and solve the optimization problem using the all-at-once format and by using two different threshold values in the convergence. However, through the follow-up conference meetings with PI, the compatibility issue between the two subsystems was questioned. PI then decided to update the reactor-distillation model by using a new model. A prototype of this new model was developed by PI and was recently submitted to UM for testing. UM will continue working on this new version of the reactor-distillation model and perform the optimization on it. Previous concerns with the computational cost of robust optimization are expected to be addressed by using the single-level robust optimization approach. However, the new robust optimization approach is only capable of handling the problems having a single-objective function. This robust optimization approach will be extended to handle multi-objective optimization problems as well. These and other related issues will be further investigated.

5.	Planned Project Activities for the Next Quarter

- Continue working on the updated reactor-distillation model that UM received from PI.

- Set up the convergence and compatibility requirements between the reactor and distillation models and obtain optimum solutions first using an all-at-once formulation.

- Perform sensitivity analysis in the model when parameters have both reducible and irreducible uncertainty.

- Extend the new single-objective robust optimization approach to handle multi-objective robust optimization problems.

- Finalize the joint paper on robust optimization and sensitivity analysis.

- Continue working on the joint paper on the new single-level robust optimization approach.

- Develop multi-disciplinary robust design optimization and sensitivity analysis approach for the integrated distillation-reactor model.

Appendix

Justification and Background

Optimization-based design of distillation tower with other subsystems (e.g., reactor, condenser, etc.) needs to be better understood, particularly when significant uncertainty exists during the operation of these systems in a refinery plant.

A preliminary review of the literature has revealed that previous methods in design and/or operation of petrochemical systems have been mainly based on either engineering decisions or business decisions.  The literature is sparse for the cases when these two types of decisions are integrated sequentially. However, given that operating decisions are based on engineering and business considerations simultaneously, these methods should be further developed and tuned to actual conditions of real plants to increase profitability.

Approach

There are two main tasks in the proposed approach. Both tasks will begin after a literature review in the respective domain is performed.

Task 1 (PI):

Develop and implement engineering analysis models for a petrochemical system:

- Task 1.1: Develop a MATLAB-based multi-input, multi-output analysis model for a distillation column.

- Task 1.2: Extend the above analysis model for the distillation column to include: (i) additional complexity, (ii) subsystem details; or, expand the model to include other subsystems in a refinery plant. The ultimate goal is to develop an integrated multi-subsystem petrochemical analysis model for a plant or a group of units in the plant.

Task 2 (UM):

Develop and implement a robust optimization approach:

- Task 2.1: Develop and implement a MATLAB-based multi-objective and robust optimization approach for the above analysis models.

- Task 2.2: Extend the robust optimization approach to consider the case when: (i) the upper and lower bounds for the known range of inputs include quantifiable variability, (ii) for a subset of uncertain inputs, their probability distribution is available, while for the remaining inputs the range is given.

Two-Year Schedule

Tasks 1 and 2 will begin in the first year. Tasks 1.1 and 2.1 are expected to be completed by the end of the first year. Tasks 1.2 and 2.2 will begin toward the end of the first year and are expected to be completed by the end of the second year.

Key References

- Forbes, R.J., Short History of the Art of Distillation, E.J. Brill, Leiden, 1948.

- Grossmann, I. E., Sargent, R. W. H., “Optimum Design of Chemical Plants with Uncertain Parameters,” AIChE Journal, 24(6): 1021-1028, 1978.

- Halemane K. P., Grossmann I. E., “Optimal Process Design under Uncertainty,” AIChE Journal, 29 (3): 425-433, 1983.

- Li, M., S. Azarm, “Multi-objective Collaborative Robust Optimization (McRO) with Interval Uncertainty and Interdisciplinary Uncertainty Propagation,” Trans. ASME, Journal of Mechanical Design (forthcoming)

- Inamdar, S. V.; Gupta, Santosh K.; Saraf, D. N, “Multi-Objective Optimization of an Industrial Crude Distillation Unit Using the Elitist Non-Dominated Sorting Genetic Algorithm,” Chemical Engineering Research and Design, 82(5): 611-623, 2004.

- Janak, S. L., Lin, X., Floudas, C. A., “A New Robust Optimization Approach for Scheduling Under Uncertainty: II. Uncertainty with Known Probability Distribution,” Computers and Chemical Engineering, 31, 171-195, 2007.

- Li, M., S. Azarm, and A. Boyars, “A New Deterministic Approach using Sensitivity Region Measures for Multi-Objective and Feasibility Robust Design Optimization,” Trans. ASME, Journal of Mechanical Design, 128 (4), 874-883, 2006.

- Lin, X., Janak, S. L., Floudas, C. A., “A New Robust Optimization Approach for Scheduling Under Uncertainty: I. Bounded Uncertainty,” Computers and Chemical Engineering, 24, 1069-1085, 2004.

- Du, X.P., A. Sudjianto, and B.Q. Huang, Reliability-based design with the mixture of random and interval variables. Journal of Mechanical Design, 2005. 127(6): p. 1068-1076.

- Douglas, J.M. Conceptual Design of Chemical Processes, McGraw-Hill Science, 1998.

Dynamics and Control of Drill Strings on Fixed and Floating Platforms UM Investigators: B. Balachandran GRA’s: Chien-Min Liao (started in SPRING 2007) PI Investigator(s): Mansour Karkoub and Youssef Abdelmagid Start Date: 12/01/2006 Report Date: 30 June 2008

1.	Objective/Abstract

Research objectives are the following: i) develop and analytically and numerically study control-oriented models for the drill strings, ii) investigate the control of an under-actuated nonlinear system (drill string) with complex interactions with the environment, and iii) build drill-string test-beds at  PI & UM to validate  the analytical findings and suggest possible strategies to mitigate drill-string failures.

2.	Milestones/Deliverables

On the modeling, analysis, and simulation front, the following have been addressed:

- Modification of the reduced order models and equilibrium point analysis

- Additional numerical studies with both the four degree-of-freedom and the five degree-of-freedom reduced-order models

On the experimental front, the following have been addressed:

- Experimental design and construction, data collection tests

- Contact between the drill string bottom and the outer shell

3.	Summary of Project Activities for the Completed Quarter

Accomplishments:

- Fixed-point analysis and calibration of reduced-order models.

- Numerical investigations to determine how the motions are organized around the equilibrium position. These simulations should help guide the experiments.

- Preliminary experiments to visualize rolling and bumping motions for different torque inputs

- A conference paper entitled “Drill-String Dynamics” authored by C. M. Liao, B. Balachandran, M. Karkoub, and Y. Abdelmagid has been presented at the Twelfth Nonlinear Vibrations, Dynamics, and Multibody Systems on June 1st in Blacksburg, VA.

- A journal article is under preparation for submission to the ASME Journal of Vibration and Acoustics.

In the following sections, the project progress is briefly detailed over three sections.  In the first section, the modified models and fixed-point analysis are presented.  In the second section, numerical results are discussed, and in the third section, a brief description of the experiments underway and observations of the rolling motions of the rotor along the outer shell and bumping motions between the rotor and outer shell are presented.

3.1: Examination of the Four Degree-of-Freedom Model

Since the previous report, errors were discovered in the equations derived initially.  The equations have been re-derived as discussed in the prior reports, and the corrected equations are presented here.

(1)

(2)

(3)

(4)

where

(5)

The main differences between this modified model and that of Melakhessou et al. (2003) are as follows: i) the unbalanced mass  is not relatively small compared  to the section mass , and ii) there is an additional term related to the torsion stiffness in Eq. (2).

Disregarding all the external force terms, the system is determined to have one fixed or equilibrium point, and this fixed point is given by

(6)

(7), (8)

The radial position of the equilibrium point depends on the initial radial displacement and the radial stiffness and contact stiffness.  Also, this point can be determined for either λ=0 or λ=1.   For the system parameter values given in the work of Melakhessou et al. (2003) and studied in our prior work, the eigenvalues were determined from the Jacobian Matrix, but this equilibrium point was found to be unstable.

Next, free oscillation results obtained through numerical integration are presented for different initial positions of Section II relative to Section I in Figures 3.1.1 to 3.1.3.   When there is contact between the outer shell and Section II, the oscillations have characteristics similar to those observed in the case of forced oscillations.   This is evident when the results of the present report are compared to those presented in previous reports.

Case I:  Initial position close to the center of the stator

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 3.1.1. Phase portraits:  a) radial displacement of Section II, b) rotation angle of Section I, c)  bending angle of Section II, and d) rotation angle of Section II.

Case II:  Initial position close to the outer shell

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 3.1.2. Phase portraits:  a) radial displacement of Section II, b) rotation angle of Section I, c) bending angle of Section II, and d) rotation angle of Section II.

Case III:  Initial position corresponds to contact with the outer shell

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 3.1.3: Phase portraits:  a) radial displacement of Section II, b) rotation angle of Section I, c) bending angle of Section II, and d) rotation angle of Section II.

3.2: Examination of the Five Degree- of-Freedom Model

The corrected system with five degrees of freedom is presented next.  With the additional tilt angle, the equations read as

(9)

(10)

(11)

(12)

(13)

where  as in Eq. (5).   Again, for free oscillations of the system, the equilibrium points of the system are determined.  The system is found to have one equilibrium or fixed point, which is given by

(14)

with the additional condition that the tilt angle

Again, as with the four degree-of-freedom model, the free oscillations of the system were studied for different initial conditions and the results are presented in Figures 3.2.1 and 3.2.2.   As in the system with the four degrees of freedom, the oscillatory characteristics are different in cases with contact and without contact.  The inclusion of the tilt angle does include some oscillatory characteristics other than those observed previously.

Case IV:  Initial position close to the center of the stator

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 3.2.1. Phase portraits:  a) radial displacement of Section II, b) rotation angle of Section I, c) bending angle of Section II, and d) rotation angle of Section II.

Case V:  Initial position corresponds to contact with the outer shell

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Figure 3.2.2. Phase portraits:  a) radial displacement of Section II, b) rotation angle of Section I, c) bending angle of Section II, and d) rotation angle of Section II.

3.3: Experimental Arrangement and Observations

In Figures 3.3.1 and 3.3.2, experimental observations of rolling motions and bumping motions made in the arrangement at the University of Maryland are shown.  The first case corresponds to the higher rotation speed, while the second one corresponds to a lower rotation speed.  With a heavier unbalance mass, it is expected that one would observe rolling motions.  These characteristics have been predicted previously in forced oscillations of four degree-of-freedom and five degree-of-freedom systems.

Figure 3.3.1. Rotor in rolling mode (order from left to right, up to down).

Figure 3.3.2. Rotor in bumping mode (order from left to right, up to down).

In Figure 3.3, the wave simulating robot being studied at the Petroleum Institute to simulate off-shore excitations on a drilling platform is shown:

- Difficulties Encountered/Overcome

Experimental calibration of absolute encoders and fabrication and construction of the experimental arrangement at the University of Maryland has taken longer than anticipated.   It was found that one of the encoders received was defective.  This encoder has been replaced.

- Planned Project Activities for the Next Quarter

Numerical and Analytical Investigations

The numerical investigations will be continued with the reduced-order models discussed in the previous report, and different nonlinear oscillatory behaviors and instabilities will be studied. Through the analyses, different types of solutions will be investigated.  If feasible, analyses will be conducted along the lines of Leine and Nijmeijer (2004) and Long, Lin, and Balachandran (2007) to study bifurcations in systems with discontinuities.  Through interactions with the experimental investigations, the reduced-order models will also be extended and/or refined.  Attention will also be paid to possible nonlinear coupling between bending vibrations and torsion vibrations and other modes of vibrations.  Parametric studies will be conducted to understand the influence of the unbalanced mass and parameters such as contact stiffness and contact damping.

Experimental Investigations

The experiments of Mihajlović et al. (2004, 2007) will continue to serve as a reference for the proposed experiments. These experiments will be conducted with a focus on the following: i) drill-string performance on the bottom end section, ii) interaction between the rotating disk and stick-slip phenomena,  iii) rotating system subjected to an axial force, iv) the contact stiffness associated with stick-slip interactions, and v) validation and refinement of reduced-order models.

Appendix

Justification and Background

Drill-string dynamics need to be better understood to understand drill-string failures, control drill- string motions, and steer them to their appropriate locations in oil wells.   Although a considerable amount of work has been carried out on oil-well rotary drilling (for example, Spanos et al., 2003), the nonlinear dynamics of this system is not well understood given that the drill string can undergo axial, torsional, and lateral vibrations, and operational difficulties include sticking, buckling, and fatiguing of strings.   In addition, the prior models focus on either bending or torsion or axial motions.

Approach

A combined analytical, numerical, and experimental approach is being pursued at the University of Maryland (UM) and Petroleum Institute (PI). Specifically, the drill string is being modeled as a nonlinear dynamical system consisting of interconnected structural components with joints. Appropriate attention is also to be paid to the soil conditions. Finite element methods are to be used for developing computational models, as appropriate. The experiments at UM and PI will be tailored to address specific aspects of the drill-string dynamics as well as complement each other.  Actuator and sensor choices will also be explored to determine how best to control the system dynamics. The studies will be initiated with drill strings located on fixed platforms and later extended to systems located on floating platforms.

Interactions

During the Blacksburg conference, a meeting was held with Professor A. Berlioz from France. He was the co-advisor of Mr. H. Melakhessou.  Professor Berlioz shared some of the experimental data obtained in the work of Melakhessou with the authors.  He also stressed the importance of taking stick-slip interactions into account, as in the present effort.

Two-Year Schedule

January 1, 2007 to July 31, 2007:  Modeling of drill-string dynamics, computational models; analytical and numerical studies; identification of appropriate oil-well model

August 1, 2007 to October 31, 2007:  Analytical and experimental studies and initiation of experimental studies

November 1, 2007 to January 31, 2008:  Experimental arrangement and calibration experiments and simulations of reduced-order models

February 1, 2008 to July 31, 2008:  Continuation of experimental studies, studies on actuator and sensor configurations for control of drill-string dynamics, and investigations into the need for vibration isolation schemes

August 1, 2008 to October 31, 2008: Studies on drill-string systems located on floating platforms

Key References

- Leine, R. I., van Campen, D. H., and Keultjes, W. J. G. (2002). “Stick-Slip Whirl Interaction in Drill String Dynamics,” ASME Journal of Vibration and Acoustics, Vol. 124 (2), pp. 209-220.

- Melakhessou, H., Berlioz, A., and Ferraris, G. (2003). “A Nonlinear Well-Drillstring Interaction Model,” ASME Journal of Vibration and Acoustics, Vol. 125 pp. 46-52.

- Nayfeh, A. H. and Balachandran, B. (1995). Applied Nonlinear Dynamics: Analytical, Computational, and Experimental Methods, Wiley, New York.

- Spanos, P. D., Chevallier, A. M., Politis, N. P., and Payne, M. L. (2003). “Oil and Gas Well Drilling: A Vibrations Perspective,” Shock and Vibration Digest Vol. 35(2), pp. 85-103.

- Mihajlović, N., van Veggel, A. A., van de Wouw, N., and Nijmeijer, H. (2004)  “Analysis of Friction-Induced Limit Cycling in an Experimental Drill-String System,”  ASME Journal of Dynamic Systems, 	Measurement, and Control, Vol. 126(4), pp. 709-720.

- Mihajlović, N., van de Wouw, N., Rosielle, P.C.J.N., and Nijmeijer, H. (2007) “Interaction between torsional and lateral vibrations in flexible rotor systems with discontinuous friction,” Nonlinear Dynamics, published online.

Developing Corporate Dashboards for Multi-Unit Firms: An Agent-Based Approach UM Investigator: Dr. P. K. Kannan PI Investigator: Dr. Tareq Al Ameri UM’s GRA: Mr. Phillipe Kamaha UM High-School Student: Mr. Wendell Shirley Start Date: 15 May 2008 Report Date: July 15 2008

1.	Objective/Abstract

Multi-unit enterprises are defined as systems that are interconnected through complementary product/service categories and the markets they serve and through a common ownership of the enterprises that renders the problem of overseeing/managing these enterprises as a whole a complex task (see Figure 1 below). These units might be plants within a firm or firms within a multi-organizational setting.

Figure 1. Multi-unit oversight dashboard concept

Our project focuses on developing measurement systems that will incorporate the interconnectedness among the units and provide clear guidelines at the multi-unit level through dashboards that will enable the management of such complex systems and improve the understanding of such systems. The project will also enable managers to understand the implications of their various policies and decisions at the multi-unit level through the use of agent-based models.

Given that the task of oversight is a complex one, our research focuses on (1) identifying the key performance variables that the management would benefit most from of in understanding the impact of the market forces and their own policies and decisions across units, (2) designing the measurement schemes across the multiple units that will encompass the areas of marketing metrics, new products/services, financial measures and key engineering performance measures, and (3) designing simulation studies to test the robustness of these measures under different market and product-market (ranging from substitute markets to complement markets for the firms) scenarios, and the sensitivity of these measures to policy changes and actions.

2.	Deliverables for the Completed Quarter

- The project was started in mid-May 2008 after the allocation of seed money by EERC. The initial research ideas were developed and are presented later in the report, along with the timetable for completion.

- A framework for a multi-plant problem within a refinery setting has been developed to tie the research more closely with PI’s research contexts.

3.	Summary of Project Activities for the Completed Quarter

- UM and PI interacted through teleconference on May 20, 2008, during which the initial research ideas were presented to the PI team. The original research plan as presented later in this section was reviewed, and it was suggested that the problem might be modified to one of multi-plant problem within a firm to make the scope manageable.

- UM hired engineering student Phillipe Herve Kamaha to work on the project for the summer as well as for Fall 2008 and a high-school student, Wendell Shirley, for the summer 2008.

- Initial research activities focused on the first objective of the project as follows: determining key performance indicators (KPIs) across firms and understanding how they are impacted by market forces and interactions. Based on secondary research and refinement of the questions, the first phase of the two-phase project was developed as focusing on the skeletal design of the corporate dashboard. The specific areas we focused on were: (1) What should be measured and why? (2) Key measures and their interrelationships, (3) Integration of commonly used measures in marketing, finance, engineering and (4) Specifying the insides of the dashboard.

- Based on secondary research, the following areas of initial focus were identified:

Interrelationship Between Firms

- Focus on manufacturing and manufacturing-based relatedness, synergy, and coordination

- Focus on primary value activities of each firm

- Incoming logistics, operations, outbound logistics, market and sales, and service

- Supporting functions: technology development, procurement, human resources management, and administration

- Interrelationships based on the above value chain

The interrelationships in the manufacturing related activities will include (1) raw materials – that is, the types of and processes for acquiring raw materials; (2) product and process science/technology – specifically, the theoretical principles underlying the design and manufacture of products, and (3) resource conversion - the equipment, processes, and procedures used to apply the technical and scientific principles to the conversion of raw materials into end products. From the marketing and market related activities the interrelationships will focus on (1) marketing – the processes and methodologies used to market the products, and (2) market interrelationships – the degree to which customers are common for the firms, substitutability and complementarity of the products of firms, etc.

Focus on Specific Measures

The following measures were examined as candidates for the key performance indicators (KPIs) focusing on manufacturing and marketing/sales activities. These measures are used by each firm’s management as well as by managements interested in multi-firm oversight across all firms. (These measures can also be tailored to the problem of multi-plant oversight within a firm, in which case these measures will be defined at the plant level and across plants).

Cost Drivers

  - Economies of scale – factories, equipment and logistics scale

  - Capacity utilization – factory/plant utilization

  - Linkages – with suppliers and distributors

  - Integration – backward into supplies, forward into distribution

  - Timing of new capacity, new facility, and new technology investments

  - Location of plants, warehouses

  - Discretionary policies that affect costs

Uniqueness drivers

  - Capacity or inventory available to provide delivery as requested

  - Quality specifications and tolerances

  - New product-process development processes

  - System-wide flexibility and responsiveness to design changes

- Revised Problem Formulation and Research Design: Given the discussion with PI and with the objective of making the problem more manageable and focused, the problem context was changed to a multi-plant environment. A sample framework has been developed as follows:

  - The problem considers production at an industrial chemical multi-plant facility. The initial focus is on determining production rates and schedules of multiple products in the multi-plant facility to meet customer orders and inventory targets. The plant process requirements and quality requirements are also considered.

  - We consider four plants to start with – two plants of Type 1 and two plants of Type 2. Type 1 plants can produce multiple products – one at a time. Type 2 plants produces products which require input of final products from the Type 1 plants. The schematic can be shown as follows:

Figure 2. Schematic of the multi-plant firm

  - There are interdependencies between the plants as shown because of the intermediate products and shared resources. The problem we consider is one of planning and scheduling the products so that the customer demands are met and stock-outs are minimized. If the demand and constraints are known deterministically, this problem can be solved using optimization methods. However, we incorporate uncertainties and interactions among markets and consumers, so they cannot be solved easily using optimization techniques. (For example, the products could be substitutes/complements, in which case, if there is a stock-out of one, some consumers may choose to use another one instead of going away from the market). We will formulate the deterministic problem (using expected values of the uncertain distributions) as an optimization problem so that it can be used as a benchmark.

  - The focus in this problem is on performance metrics. Given the above problem setup, we will determine a list of recommended performance metrics, submetrics, and sub-submetrics, both at the plant level and the overall firm level. These metrics could be related to the set of metrics identified in the previous bullet points. We will examine several questions at this stage: (1) which of the above metrics are used by different stakeholders (e.g., plant managers, firm level managers), and how do they relate? How often should these metrics be monitored: per month, per quarter, or in real time? (For example, at the strategic level they could be measured less often). Which metrics are sufficient? When do the metrics enter a “danger zone” as in a dashboard that require managerial action?

  - The next step is the design of agent-based simulation model that would explain how the performance metrics react to environmental and managerial control factors. In addition to these, interaction among customers in the market will be taken into account. This simulation will be carried out in stages, starting from a simple model with few variables to gradually building a more sophisticated model with many variables and interactions.

  - Based on the results of the simulation, we will perform sensitivity analysis, optimization and robustness analysis of the metrics simulation model. Sensitivity analysis, in addition to validating the simulation model, will provide insights into how the performance metrics help and will identify the critical performance metrics and the critical control factors. We will also examine the robustness of the performance metrics. Based on the analysis, the overall objective of this step is to identify the best set of performance metrics that should go into the dashboard of the upper management to optimally control the multi-plant setup.

- The UM team has already started examining the simulation test bed – NetLogo environment – so that the multi-plant setup can be modeled. Currently, the team is modeling simple setups of the problem with 4 plants and a closed market of customers, and examining the impact of various control variables on meeting customer demand and on stock-outs.

5.	Planned Project Activities for the Next Quarter

- The UM team will continue specifying the multi-plant problem further with the help of interaction with PI team. Specifically, attention will be focused on determining the appropriate and relevant metrics to examine.

- UM will also formulate the optimization problem that will serve as a benchmark based on the above metrics.

- The UM team will continue developing the NetLogo simulation model and present the developments to the PI team on a continual basis.

- The UM PI, P. K. Kannan, will plan a visit to meet with PI faculty to further interact with them on the problem and refine the problem based on face-to-face discussions. This trip is being planned for the end of October currently, but will be coordinated with the PI team to suit their availability.

Appendix

Justification and Background

In managing a multiple-unit firm (for example, a firm with multiple plants or a firm with multiple Strategic Business Units), the upper level management has to have a set of performance metrics which will act as a dashboard to indicate to the managers how the different units are performing on key dimensions. Given the interaction between the different units and the interaction across customers they serve, designing such a dashboard is not an easy task. The dashboard cannot just contain those metrics and measures that are used at the unit level because they might ignore such interactions. The problem of finding the right set of measures for dashboard-based oversight of the multiple units is therefore a complex problem. Our objective in this project is to find such a smallest set of metrics that are appropriately sensitive to the changes in the phenomenon that managers are interested in measuring while at the same time robust to the noises in the environment, so that managers are able to “steer” the multiple units successfully in a turbulent environment.

Approach

The research team will start focusing on the multi-plant level problem with the following stages during the seed funding stage of the project:

- Stage 1: Design of KPIs for multi-plant oversight.  Plant level measures are being developed currently and will be shared with the PI team in the next meeting. These KPIs will enable the management of multiple plants at the corporate level using the developed dashboard.

- Stage 2: Understanding robustness of corporate dashboard measures and specification for multi-plant oversight

- Stage 3: Agent-based simulations to understand the impact of market forces for the plants and firm

- Stage 4: Decision-support system for multi-plant oversight

Key References

- Jackson, Jennifer R, Jeanna Hoffman, John Wassick, and Ignacio E. Grossman, “A Nonlinear Multiperiod Process Optimization Model for Production Planning in Multi-Plant Facilities,” Working paper, Carnegie Mellon University. 2002.

- Kleijnen, Jack PC and Martin T Smits, “Performance Metrics in Supply Chain Management,” Journal of the Operational Research Society, 2003.

- Gargeya, Vidyaranya B, “Plant Level Performance Measurement: An Exploratory Case Study of a Pharmaceutical Encapsulation Company,” Technovation, Vol. 25, Issue 12, 2005, p. 1457-1467.

- Kaplan, Robert S. and David P. Norton, “Using the Balanced Scorecard as a Strategic Management System,” Harvard Business Review, Jan-Feb, 1996, p. 75-85.

- Birkinshaw, Julian and Mats Lingblad, “ Intrafirm Competition and Charter Evolution in the Multibusiness Firm,” Organization Science, Vol. 16, No. 6, Nov-Dec, 2005.

- Robins, James and Margarethe F. Wiersema, “A Resource-Based Approach to the Multibusiness Firm: Empirical Analysis of Portfolio Interrelationships and Corporate Financial Performance,” Strategic Management Journal, Vol. 16, No. 4 (May) 1995, p. 277-299.

- NetLogo, http://ccl.northwestern.edu/netlogo/

Development of a Probabilistic Model for Degradation Effects of Corrosion-Fatigue-Cracking in Oil and Gas Pipelines UM Investigator: Prof. Mohammad Modarres GRA: Mohamed Chookah Faculty Research Assistant: Mohammad Nuhi PI Investigator(s): Prof. Abdennour Seibi Start Date: October 2006 Report Date: 15 July 2008

# 1.	Objective

This study involves developing and applying an engineering-based (mechanistic) probabilistic model for health management of oil pipelines in process plants. The study involves two interrelated projects. The first project, which is the topic for a PhD dissertation, focuses on model development and demonstration. The second project involves developing a degradation acceleration lab at PI and performing experiments to further validate the proposed models of the first project. The funds made available by the Petroleum Institute would facilitate building the experimental set-up. Mr. Mohamed Chookah is working on the first project. Mr. M. Nuhi, a Faculty Research Assistant, supports the mechanistic failure part of the research and will be responsible for experimental and data development.

The overall objective of this study is to propose and validate a probabilistic mechanistic model based on the underlying degradation phenomena whose parameters are estimated from the observed field data and experimental investigations. Uncertainties about the structure of the model itself and parameters of the model will also be characterized.  The proposed model should be able to capture wider ranges of pipelines rather than only the process ones.  The proposed model will assess pipeline health and can account for material and size variability.  The existing probabilistic models sufficiently address the corrosion and fatigue mechanisms individually, but are inadequate to capture mechanisms that synergistically interact.  Admitting the fact that capturing all degradation mechanisms will be a challenging task, the new model will address pitting corrosion followed by corrosion-enhanced fatigue-crack growth.

# 2.	Deliverables

- Interim report on corrosion-fatigue models (submitted 8/31/2007).

- Data analysis of field data (on-going, delayed due to difficulties with updating the model structure and collecting data. New deadline: 30 August 2008).

- Interim report on application example (on-going).

- Design, construction, and commissioning of test rig (design completed on 12/31/2007, construction and installation is on-going, and expected testing equipment assembly completion date is 8/25/2008).

- Interim report on model validation based on conditioned progress in obtaining experimental results (on-going).

- Conference and Archival Papers:

  - Final paper submitted to the conference committee titled “Probabilistic Safety Assessment & Analysis (PSA) 2008” conference to be held in Knoxville, Tennessee, 7-11 Sep 2008.

  - M. Modarres attended a panel discussion on corrosion at the Reliability and Maintainability Symposium (RAMS) held 28-31 January 2008 in Las Vegas, Nevada. PI research was presented and discussed under the title “Consideration of Corrosion Induced Degradation in Design and Operation of Equipments: Example of Corrosion-Fatigue Cracking Degradation Modeling.”

  - M. Modarres and M. Chookah participated in the first Energy Education and Research Collaboration (EERC) Workshop held at the PI in Abu Dhabi from 4-5 January, 2008.

  - Submitted a paper to Reliability Engineering and System Safety Journal: S. Chamberlain, M. Chookah and M. Modarres, Development of a Probabilistic Physics of Failure Model for Reliability Assessment of Compressed Natural Gas Vehicle Cylinders.

  - Submitted paper accepted by the ASME conference committee to appear in the Proceedings of the ASME 2008 International Design Engineering Technical Conferences & Computers and Information in Engineering Conference, Development of a Probabilistic Model for Assessment of Degradation of Pipelines Due to Corrosion-Fatigue Cracking. Authors: Chookah, Nuhi, Modarres and Seibi

- Final Report (Due 12/31/2008)

# 3.	Summary of Project Activities for the Completed Quarter

Background (reported previously in the 3rd quarter report):

# The following is a summary of our adopted models.

# Pitting Corrosion Model

To assess the influence of concurrent pitting corrosion, a simplified model for pit growth proposed by Harlow and Wei was used [9].  The model is patterned after that proposed by Kondo [10] and assumes a pit of hemispherical shape growing at constant volumetric rate in accordance with Faraday’s law from an initial radius aο.  The rate of pit growth (with volume V = (2/3)πa3) is given as follows:

But assuming ρ is constant,

From Faraday’s Law,

Hence by substitution,

where

;

and a is the pit radius at time t; M is the molecular weight of metal; Ip is the pitting current; Ipo is the pitting current coefficient; η is the metal’s valence; ρ is the density of the metal; F = 96,514 C/mole is Faraday’s constant; Ea is the activation energy; R = 8.314 J/mole-K is the universal gas constant; and T is the absolute temperature.

# Corrosion Fatigue Crack Growth Model

# Electrochemical Model

For the electrochemical reaction contribution, the surface coverage θ is identified with the ratio of the amount of charge transferred during each loading cycle (q) to that required to completely “repassivate” the bared surface (qs), or, more conveniently,

For this purpose, a simplified model for the reaction is used: for example, it is assumed that the underlying electrochemical reaction consists of a single step and is represented by thermally activated, first-order kinetics [1, 11].  The bare surface reaction current and charge densities are represented in simple exponential forms:

where io is the peak current density (initial rate of reaction on the clean, bare surface), and k is the reaction rate constant in Arrhenius form.  Thus,

where

.

# Mechanistic Model

For mechanistic understanding of the problem, the following mechanistic model for fatigue crack growth was chosen. It is assumed that both parts of the above superposition equation can be modeled by the power law (Paris-Erdogan relationship) [12] of the form

where

with Δσ being the far field stress range, and β a geometric parameter.

The coefficients Cr and Cc reflect material properties, and the exponents nr and nc, reflect the functional dependence of crack growth-rate on the driving force, ΔK.

Incorporating the electrochemical and mechanical relations yields a simple differential equation in that the variables a and N can be separated.  Estimation of parameters nr and nc may require numerical integration [1].

# Superposition Model

A superposition model proposed by Wei [13] was adopted.  In the most general form the fatigue crack growth rate is given by [7]:

with a cycle–dependent rate and a time–dependent rate. Within each of these rates, the mechanical (deformation) and environmental contributions as being from independent parallel processes are treated.

# The corrosion fatigue model becomes

From the solution of this equation, we can estimate the N as follows:

where af and atr are the final and initial crack sizes, respectively.

atr could be calculated iteratively using the criterion set earlier,

which reflects equality between the pitting and cracking rates at the onset of crack growth,

The corrosion-fatigue life NF is the sum of the number of loading cycles over which pitting and fatigue cracking dominates at a given stress level [7] and is given by

Generic data (from the related papers) were used to build and run the computer routine Matlab for corrosion fatigue according to Wei’s superposition model.

Table 1.  Deterministic parameters for X70 steel used in life estimation [1]

Universal gas constant R = 8.314 J/mol-K

Activation energy Ea = 35 KJ/mol

Fatigue exponent nr = 2

Corrosion fatigue exponent nc = 2

Frequency ν = 0.1 - 10 Hz

Applied stress range Δσ = 100 - 500 Mpa

Temperature T = 293 - 723 K

Final crack size af = 25 mm

Shape Factor β = 1.24

Faraday’s constant F = 96,514 C/mole

Molecular weight M = 55 g/mole

Valence η = 3

Density ρ = 7.87 g/cm3

Table 2.  Random variable distribution (Weibull) for X70 steel used in life estimation [1]

Random α β γ Variable (shape factor) (scale factor)

Cr 12 4.0 × 10-11(m/cyc)(MPa√m)-2 0

Cc 8 2.0 × 10-10(m/cyc)(MPa√m)-2 0

κο 10 3.0 × 105 (s-1) 0

An exponential distribution is assumed for the current density (Ip) using the data in [14].  The pdf of Ip is

The flowchart shown in Figure 1 outlines the steps followed in assessing the required variables in our proposed model:

# Figure 1.  Algorithm of the computational method applied in the research

We developed simple empirical parametric models estimated from curve fitting of data obtained from the computer simulation, as shown below.

# Figure 2.  Results of the simulation

# Through an extensive trial and error process, a simplified general parametric empirical model is proposed as follows:

This model was checked against Wei’s model, which has consistently shown a reasonable match as shown for one such case in Figure 3.

# Figure 3.  Graph of the simulation (Wei’s model) and the proposed empirical model

Technical Progress Since the 5th Quarter

Assuming frequency, temperature, and cyclic stress are independent, the above general model is modified to the following form, which explicitly describes the environmental factors of stress, frequency and temperature,

where,

Based on the uncertainties of the three random variables (Cc, Cr, ko) used in this simulation,  best estimates of the constant parameters A and B are presented as two parameter Weibull distributions:

β = 3.32				            β = 1.7

A					B

α = 4.01*10-7				α = 2.48*10-22

Similarly, this modified model has been verified against Wei’s model, where once again a good match is secured as shown below.

# Figure 4.  Graph of the simulation (Wei’s model) and the proposed empirical model

Estimation of model parameters “A and B” Including uncertainties

Here we have verified the distribution of A and B parameters of the proposed empirical model structure against the variable environmental conditions.  Utilizing ReliaSoft-Weibull++ 5.32 program to analyze the distribution of each parameter, respectively, it was possible to obtain the following,

# Figure 5.  CDF (Weibull) of parameter “A” distribution

# Figure 6.  CDF (Weibull) of parameter “B” distribution

The environmental conditions used to run the simulation to build the above distributions are shown in Table 3.

# Table 3.  Randomly selected environmental conditions to run the Monte Carlo simulation to obtain A & B distributions

| Data set | T, K | σ, MPa | ν, Hz | Ip, A |
| --- | --- | --- | --- | --- |
| 1 | 373 | 10 | 10 | 1×10-5 |
| 2 | 673 | 20 | 7 | 1×10-6 |
| 3 | 473 | 30 | 5 | 1×10-5 |
| 4 | 273 | 40 | 4 | 1×10-6 |
| 5 | 573 | 50 | 3 | 1×10-5 |

The most noticeable evidence from Figures 5 & 6 is the negligible impact of environmental condition variations on the A and B distributions.  This evidence implies the independency of A and B variability from the pipeline’s surrounding environmental conditions, allowing us to focus on its source of variability mainly from the material property.

##### Corrosion Model

- Corrosive species in the pipeline flow streams play an important role in the overall degradation mechanism.  Among all of the possible corrodents, the modeling shall only concentrate on two significant corrosive species in the oil refinery fields [15-28],

- Corrosion due to  chloride concentration [Cl-]

- Corrosion due to H2S concentration [H2S].

Chloride corrosion

Most chloride salts in the crude oil are inorganic (sodium, magnesium, or calcium chlorides) and are effectively removed by the desalter. The non-extractable chlorides are not removed in the desalter, but can break down from downstream heating and processing to form hydrochloric acid (HCl). They cause corrosion and fouling problems. The forms of these chlorides are still being investigated and it is possible that they could be organic.  Even with as little as 1% of the non-extractable chlorides, a major increase in the atmospheric tower overhead HCl and chloride levels can occur and cause severe corrosion and fouling problems [29].

Attempts to model the effects of chloride concentration have been well documented in literature.  Table 3 lists some of the most promising models.

Table 4.  Chloride concentration effect models

| Proposed Model | Respective References |
| --- | --- |
| Ip = A exp ( -B Epit ) Icorr=E exp (-F x [pH] ) CR= G exp (H x [pH] ) | [30],[31],[34] [33],[37] [33] |
| Epit = - C log [Cl- ] + D Ecorr = - R [ pH] (+,-) S | [31],[32],[33],[34],[35],[36] [33],[36],[37] |
| pH = - P ln [ Cl- ] + Q | pH decreases with increasing chloride concentration.[30],[32] |
| Ip = M exp ( N log [Cl- ] ) | The current density increases with increasing chloride concentration [30],[31],[34],[37] |

The coefficients A, B, C, D, E, F, G, H, M, N, P, Q, R, and S are constant values.

The effect of [Cl-] on Epit follows the following relation [38, 39]:

Epit(T) = Epit°(T)  + B(T) log [Cl-]

where, Epit° is the pitting potential at 1M chloride concentration, and B(T) is the slope of Epit dependence on  [Cl-], with  T, the absolute  temperature.

Similar to chloride [Cl-], increasing the temperature generally results in decreasing Epit values.

Examining the pitting behavior of carbon steel in bicarbonate solutions containing chloride, the following relations were found for Epit° (mV) and B(T)  as a function of temperature [38]:

Epit° (T) = -584.8 + 3.92 T

B(T) = -24.5 – 1.1 T

The general dependency

Ip = A exp (-B Epit)

Epit = - C  log [Cl- ] + D

we can combine with Ipvalues related to Epit and get

Ip = A* exp(B* log [Cl-])

H2S corrosion

Sulphur is one of the foremost corrodents which cause problems in the refinery industry. It occurs in crude petroleum at various concentrations and forms a variety of chemical compounds, including hydrogen sulphide, mercaptans, sulphides, polysulphides, thiophenes, and elemental sulphur.  Because of great influence of hydrogen sulphide on the corrosion behaviors of the steels, two forms of sulphide corrosion are distinguished [29, 40]: without hydrogen present and with hydrogen present.

Sulphide corrosion without hydrogen present

Sulphur contained in hydrocarbon fractions in atmospheric and vacuum distillation units, catalytic cracking units, and hydro-treating and hydro-cracking units upstream of the hydrogen injection line destroys steel structures. Heat exchanger tubes, furnace tubes and piping are generally made of carbon steel.  Although the data given by respondents were incomplete and scattered considerably, they were combined with earlier reported corrosion rates and presented as the original McConomy curves [29, 40].

Figure 7. Modified McConomy curves showing the influence of temperature on sulphide corrosion rates of steels (without hydrogen present) [29, 40].

Estimating from these curves the corrosion rate for carbon steel in case of corrosion without hydrogen present, we get a relation for corrosion rate dependent on temperature:

The above model represents a case of 6 wt% sulfur content.

Sulphide corrosion with hydrogen present

The basic information for material selection for refinery hydrogen units is provided by the so-called Couper-Gorman curves [29, 40].

Figure 8.  Effect of temperature and hydrogen sulfide content on high-temperature H2S/H2 corrosion of carbon steel (naphtha desulpharizers)

1 mil/yr = 0.025 mm/yr [29, 40].

Table 5.  Corrosion data of carbon steel in naphtha

| H2S [ mol% ] | Corrosion rate(CR) in [mm/yr] Icorr [ uA ] |
| --- | --- |
| 0.1 | 6E-5 exp (0.0134 T[K] ) (2.5979E-2)exp(0.0134 T[K]) |
| 0.2 | 2E-5 exp (0.0155 T[K] ) (0.8660E-2)exp(0.0155 T[K]) |
| ... | ... ..... |
| 1.0 | 1E-5 exp ( 0.0170 T[K] ) (0.4330E-2)exp(0.0170 T[K]) |
| ... | ... |
| 10.0 | 8 E-6 exp ( 0.0179 T[K] ) (0.3464E-2)exp(0.0179 T[K]) |

Using the data in Table 4, the general relation for the corrosion of carbon steel will be

for different H2S concentrations.

H2S concentration effect on the corrosion current is affected by temperature, partial pressure, and cyclic load conditions.

Temperature

As is shown above, temperature is the most important degrading agent, and nearly all investigators report a rapid increase of corrosion rate with rising temperature. The majority of the data indicates that a temperature rise of 38ºC (311 K) can be expected to approximately double the rate of attack.  This relationship is illustrated by exponential curves by M. W. Kellogg Co. by G. Sorell et al. [41-45], which can be given by the following equation:

Corrosion rate [in/yr] = K * exp (A T[K] )

where K is a constant (~ 0.0014   ) and  A is  a constant ( ~ 0.0062 ) and  T is the temperature in Kelvin. Although a notable exception to this trend has been described by Backensto et.al. [46], where the rates go through a maximum above 1000 ºF (811 K).  The maximum corrosion rates result in the range from 672 K to 755 K.  According to this literature, the collected data show without exception that under constant temperature the corrosion rate increases with higher hydrogen sulfide contents.  This explanation strengthens our suggestion that the corrosion rate increases exponentially with the hydrogen sulfide concentration, and this tendency, like the chloride corrosion, can be given in the following form:

Corrosion rate [in / yr] = 0.2138 exp (0.0348* [H2S (vol. %)])

The corrosion rate and the current in [m A/ cm2] conversion are given in the literature.  Another interesting fact in this literature [41] is that in attempting to relate the rate of attack to some measure of hydrogen sulfide content, it becomes apparent that the often-used measures like weight volume or mole percent do not correlate as well as the partial pressure of the hydrogen sulfide in the gas mixture. They illustrate the synergetic effects of the hydrogen sulfide content, hydrogen sulfide partial pressure, and total pressure on each other and their effects on the corrosion rate, where the following relation for corrosion rate can be derived:

ln ( CR[in/yr.] ) = -5.73895 + 0.00665 T [K] + 0.0174 [H2S]

and

[H2S] =0.0909 * (p)

where p= partial pressure of hydrogen sulfide.

Pressure

The total pressure appears to be an important corrosion variable only in as much as it determines the partial pressure of the hydrogen sulfide in a given gas mixture.

Cyclic conditions

Cyclic conditions accelerate the corrosion rate because they tend to deteriorate the sulfide scale, which is at least partially protective. Different types of cyclic conditions of greatest interest are cyclic heating and cooling, alternate reducing and oxidizing atmospheres, and the cyclic loading from the pumps.

Proposed model for combination of chloride and hydrogen sulfide corrosion

In a sour gas (H2S) and chlorinated environments, the synergetic effect of chloride concentration and hydrogen sulfide concentration together can increase the corrosion rate. Chloride in the presence of hydrogen sulfide has the tendency to make a localized attack, causing localized corrosion, and synergistically, they affect the corrosion rate in a sour gas environment in an additive [47-49] form.  So, we can say that the total corrosion rate would be the sum of the contribution of the chloride and the hydrogen sulfide concentration,

CR = CR (Cl-) + CR (H2S)

This means, in other words, that

The general form of the additive total corrosion rate  is

IP(t) =  IP([Cl-])  +  IP([H2S])

IP(t) =  {A exp ( B x log ([Cl-])  }   +  {  C exp ( D x  [H2S] ) }

or,

IP(t) =  {A exp ( B (24.5 + 1.1 T) log ([Cl-])  }x exp [(-3.92 E) T ]   +

C exp(D * ( -5.73895 + 0.00665 T [K]  +  0..174 [H2S]  )

Probabilistic Estimation of the Parameters

An actual failed pipeline from the Ruwais Refinery in Abu Dhabi, UAE, was investigated, and the following conditions were gathered:

- Pipeline material: carbon steel

- Medium flow: heavy vacuum gas oil

- Operating temperature (T): 443 K

- Operating pressure (σ): 1.547 MPa

- Loading frequency (ν): 4.76×10-7 Hz

- Wall thickness (af): 0.00635 meters

- Service life (N): 375.2784 cycles

- A & B Weibull distribution parameters given in Equation 17.

The updated model was used to run the simulation and obtain the crack size “ai” values, which were then fitted to Weibull, as shown in  Figure 9.

Figure 9.  The pdf of the crack size “a”

- Parameters for “ai” Weibull distribution: α= 0.00189;  β=1.3337

- The CDF value for a crack size of 0.00635 m is 0.99348

From the simulation results it was concluded that the probability of a crack reaching the surface of the pipeline for complete fracture is 0.652%.  This very low probability is consistent with the field data observed, given the fact that the observed pipe failure in the Ruwais Refinery constitutes a small fraction of the pipes exposed to this degradation process.  Further statistical tests of significance will be performed in the future to formally measure the consistency of the estimation and observation. The corrosion fatigue phenomenon does occur over a long period of time, and eventually, if the crack goes undetected, it will completely crack through. However, over the past 25 years this has occurred only rarely, and our model outcome is consistent with the industry’s historical experience.  This model’s findings should support the introduction of new inspection cycles, which will enhance the maintenance program.

Project Progress Since the 5th Quarter

- The Cortest offer has been technically reviewed and accepted by PI.  The purchase order has been received by Cortest.  The expected completion date for equipment assembly at Cortest is 8/25/2008.

# Figure 10.  Proposed corrosion-fatigue testing equipment from Cortest Corp.

- The following papers have been submitted:

    - "Development of a Probabilistic Physics of Failure Model of Compressed Natural Gas Bus Cylinder" for publication in the "Reliability Engineering & Systems Safety Journal."  (Under review)

    - "Development of a Probabilistic Model for Mechanistic Evaluation of Reliability of Oil Pipelines Subject to Corrosion-Fatigue Cracking" for presentation & publication in the ASME DAC 2008 conference to be held in New York, NY in the period 3-6 Aug 2008. (Final paper submitted & accepted)

    - "Development of a Probabilistic Model for Mechanistic Evaluation of Reliability of Oil Pipelines Subject to Corrosion-Fatigue Cracking" for presentation in the "Probabilistic Safety Assessment & Analysis (PSA) 2008" conference to be held in Knoxville, Tennessee in the period 7-11 Sep 2008. (Final paper submitted)

    - A poster is planned to be exhibited at the PHM-International Conference on Prognostics and Health Management (affiliated with the IEEE Reliability Society) to be held in Denver, CO, in October 2008. (Awaiting conference committee announcement for submission)

- The corrosion model structure for the chloride and hydrogen sulphide concentration effects has been proposed.

- Several companies, laboratories, and academic institutions have been contacted for experimental corrosion-fatigue data availability.  Requests were declined due to data confidentiality.

- Several testing laboratories have been contacted for the possibility of conducting corrosion-fatigue testing. (On-going)

# 4.	Difficulties Encountered/Overcome

- Initial budget allocated for the testing facility was not enough to purchase the customized equipment. This matter was solved by mid-February and Cortest Corp has received the purchase order.

- Collection of useful field data proved to be very difficult for the following reasons:

  - The busy environment of the refinery was a great communication obstacle.

  - The collected data were in many pieces and required a substantial effort to gather.

  - The confidentiality of the data could not be compromised, preventing a smooth data collection.

  - A lack of online monitoring devices made it impossible to obtain crack growth trends.

- The study will therefore heavily rely on test data to validate the models developed as opposed to using field data.

- The difficulty with data collection has led to a slight delay in our probabilistic (Bayesian)  estimation of the parameters of the proposed empirical model using the collected data. This task was supposed to end 31 December 2007, but we now estimate that this should be completed by 31 August 2008.

# 5.	Deliverables for the Next Quarter

- Application of the collected field data to validate the proposed corrosion-fatigue empirical model.

- Estimation of the distribution of the parameters of the proposed parametric models.

- Application of Markov Chain Monte Carlo (MCMC) Bayesian analysis to update the estimated model parameters of the parametric model.

- Uncertainty analysis to characterize the limitations of the data collected.

- Sensitivity analysis for the proposed empirical model.

- Procurement and installation planning of the lab equipment at PI.

- Submission of a poster to be exhibited at the PHM-International Conference on Prognostics and Health Management (affiliated with the IEEE Reliability Society) to be held in Denver, CO, in October 2008.

- Addressing reviewer comments received for the paper titled “Development of a Probabilistic Physics of Failure Model of Compressed Natural Gas Bus Cylinder” submitted for publication in the Reliability Engineering & Systems Safety Journal.

# Appendix

# Justification and Background

Oil pipelines are susceptible to degradation over the span of their service life. Corrosion is one of the most common degradation mechanisms, but other critical mechanisms such as fatigue and creep cannot be overlooked.  The rate of degradation is influenced by factors such as pipeline materials, process conditions, geometry, and location.  Based on these factors, a best estimate of the pipeline’s service life (reliability) is calculated.  This estimate serves as a target that guides maintenance and replacement practices. After a long period of service, however, this estimate requires reevaluation due to new evidence observed from monitoring the conditions of the pipeline.

A number of deterministic models have been proposed to estimate reliability of pipelines.  Among these models is the ASME B31G code [50], which is the most widely accepted method for the assessment of corroded pipelines [51].  However, these models are highly conservative and lack the ability to estimate the true life and health of the pipeline. It is necessary, therefore, to develop a best-estimate assessment of the life of these pipelines and integrate the uncertainties surrounding this estimate.  In addition to the limitations embedded in these deterministic models are the problems with inspection techniques and tools that may be inadequate and susceptible to errors and imprecision.  The proposed probabilistic models would be capable of addressing the limitations of these models (by accounting for model uncertainties), inspection data (characterizing limited and uncertain evidences) and subjective proactive maintenance (involving decision making process under uncertainty).

# Approach

The researchers will attempt to identify a focal point in one of ADNOC’s operating companies, such as TAKREER, which will champion this project and provide data pertinent to the core activities of this research study.  The study consists of two interrelated projects that will run over a period of two years and a half.  The first phase of Project 1 will focus on the development of a PhD thesis proposal, which encompasses the latest technological development and ongoing research activities and outlines the subject of the research project.  The second phase will concentrate on the development of a probabilistic model for piping in process plants followed by model validation through collected experimental and field data.  The second project, which will run a year later, will focus on the design, construction and commissioning of the corrosion-fatigue test cell.  The test rig will be designed and built by the research team at the University of Maryland (UM) with the assistance of Dr. Abdennour Seibi from the Petroleum Institute (PI).  The third phase of this study will deal with model application to ADNOC process facilities in order to predict their remaining service life.

The test rig, which will be built at PI, will be used by Mr. Nuhi to conduct an experimental study reflecting field conditions for model validation developed in project 1.  The equipment needed would include corrosion test cells, autoclaves, multiphase flow loops, and testing machines for slow strain rate and crack growth testing. This activity also requires a complete line of monitoring equipment for evaluation of corrosion, scaling, and chemical treatment for field and laboratory.  This test rig, once built, will be a useful tool for teaching, research, and possibly training field engineers from operating companies.  See “Two-Year Schedule” for a summary of the major tasks and the corresponding timeline.

# Overview of the Original Two-Year Schedule

# Project 1:

- PhD thesis proposal, which will include a literature search (9/1/2006 - 6/30/2007)

- Data collection from ADNOC process plants (1/1/2007 - 8/30/2007)

- Prof. Modarres visit to PI to review progress and plan for accelerated lab development (3/2007).

- Dr. Seibi visit to UM to advise PhD student in his thesis work and assist in designing the accelerated Testing Facility (11 – 21 May/2007).

- Empirical/Engineering-Based Model Development (9/1/2006 – 6/30/2007)

  - Streamlining of the model to pipeline/pressure vessel application.

  - Collection of appropriate data (data availability is at the discretion of ADNOC operating companies).

  - Actual model development.

- Probabilistic estimation of model parameters (9/1/2007 – 08/31/2008)

- Application example (11/1/2007 – 08/31/2008)

- Dr. Seibi visit to UM for thesis proposal defense and thesis defense (dates to be announced).

# Project 2:

- Design, construction, and commissioning of Accelerated Degradation Lab at PI.  UM research team will design the test facility with the assistance of Dr. A. Seibi from PI (06/01/2007 - 09/30/2008).

- Test planning (09/30/2008 – 12/31/2008).  Dr. Seibi will visit UM for two weeks during this period to jointly develop the test plan with UM researchers.

- Experimental test for model testing/validation (01/01/2009 - 04/31/2009)

- Examples of model applications (01/01/2008 – 04/31/2008)

- Conference and archival paper development (Dates of delivery depend on availability of results).

# Key References

- Harlow, D. G., and Wei, R. P. (1993).  A Mechanistically Based Approach to Probability Modeling for Corrosion Fatigue Crack Growth.  Engineering Fracture Mechanics, 45, 1, 79-88.

- Wei, R. P., and Harlow, D. G. (2005).  Mechanistically Based Probability Modeling, Life Prediction and Reliability Assessment.  Modeling Simulation Material Science Engineering, 13, R33-R51.

- Harlow, D. G., and Wei, R. P. (2001).  Probability Modeling and Statistical Analysis of Damage in the Lower Wing Skins of Two Retired B-707 Aircraft.  Fatigue Fracture Engineering Material Structure, 24, 523-535.

- Wei, R. P., Masser, D., Liu, H., and Harlow, D. G. (1994).  Probabilistic Considerations of Creep Crack Growth.  Material Science and Engineering, A189, 69-76.

- Wei, R. P. (2001).  A Model for Particle Induced Pit Growth in Aluminum Alloys.  Scripta Materialia, 44, 2647-2652.

- Dolley, E. J., Lee, B., and Wei, R. P. (2000).  The Effect of Pitting Corrosion on Fatigue Life.  Fatigue Fracture Engineering Material Structure, 23, 555-560.

- Wei, R. P. (2002).  Environmental Considerations for Fatigue Cracking.  Fatigue & Fracture of Engineering Materials & Structures, 25, 8/9, 845-854.

- Trethewey, K. R., and Chamberlain, J. (1995).  Corrosion for Science and Engineering.  Longman, England.

- Harlow, D. G., and Wei, R. P. (1994).  Probability Approach for Prediction of Corrosion and Corrosion Fatigue Life.  AIAA Journal, 32, 10, 2073-2079.

- Kondo, Y. (1989).  Prediction of Fatigue Crack Initiation Life Based on Pit Growth.  Corrosion, 45, 7-11.

- Atkins, P. W. (1994).  Physical Chemistry.  W. H. Freeman and Company, NY.

- Dowling, N. E. (1993).  Mechanical Behavior of Materials.  Prentice Hall, NJ.

- Wei, R. P., and Gao, M. (1983).  Reconsideration of the Superposition Model for Environmentally Assited Fatigue Crack Growth.  Scripta Metallurgica, 17, 959-962.

- State Structures Research Laboratory, and State Materials Office – Corrosion Research Laboratory (2002).  Galvanic Testing of Stressed Strands Inside Carbon Steel Pipe – Final Report.  Florida Department of Transportation.

- H.N. Chen, L.S. Chen, Q.H. Lin and X. Long, Corrosion 55 (1999), p. 626.

- A. Pardo, E. Otero, M.C. Merino, M.D. López, M.V. Utrilla and F. Moreno, Corrosion 56 (2000), p. 411.

- M. Romero, Z. Duque, O. Rincón, O. Pérez, I. Araujo and A. Martinez, Corrosion 56 (2000), p. 867.

- I.B. Singh, Corrosion 57 (2001), p. 483.

- T. Laitinen, Corros. Sci. 42 (2000), p. 421.

- G. Gabetta, Corrosion 53 (1997), p. 516.

- K. Yamakawa and R. Nishimura, Corrosion 55 (1999), p. 24.

- R.C. Sierra, E. Sosa, M.T. Oropeza and I. González, Electrochim. Acta 47 (2002), p. 2149.

- R.A. Carneiro, R.C. Ratnapuli and V.F.C. Lins, Mater. Sci. Eng. A 357 (2003), p. 104.

- G.M. Omweg, G.S. Frankel, W.A. Bruce, J.E. Ramirez and G. Koch, Corrosion 59 (2003), p. 640.

- F.D. Moraes, F.L. Bastina and J.A. Ponciano, Corros. Sci. 47 (2005), p. 1325.

- C. Ren, D. Liu, Z. Bai and T. Li, Mater. Chem. Phys. 93 (2005), p. 305.

- A.N. Kuzyukov, Y.Y. Nikhayenko, V.A. Levchenko, V.A. Borisenko and V.G. Moisa, Int. J. Hydrogen Energy 27 (2005), p. 813.

- Y.Y. Chen, Y.M. Liou, H.C. Shih., Stress corrosion cracking of type 321 stainless steels in simulated etrochemical process environments containing hydrogen sulfide and chloride, Materials Science and Engineering A 407 (2005) 114–126.

- Gutzeit, J. ,et ,al.  Corrosion in Petroleum Refining and Petrochemical Operations.  Metals Handbook, 9th Ed., Vol 13, Corrosion,Metals Park , Ohio 44073.

- Gutzeit, J. (2000).  Effect of Organic Chloridecontamination of Crude Oil on Refinery Corrosion.  Corrosion, Paper  No. 00694.

- www.nace.org/nacestore/assets/ConferencePapers/2000/00694.pdf

- Lin, C. J., et,al. Scanning Micoelectrode Studies of Early Pitting Corrosion of 18/8 Stainless Steel,Corrosion, Vol 54, No.4, pp.265-270.

- Chapter 9. Pitting Corrosion, KAIST, http://corrosion.kaist.ac.kr

- Andijani, I., ,et.al. (1999). Studies on corrosion of carbon steel in deaerated saline solutions in presence of scale inhibitor.  Presented at the WSTA IV Golf Conference, Bahrain.

- Petek, A., et.al. (2007). Localized Dissolution Kinetics of Low Carbon Steel.   Acta Chim Slov. 54, pp 725-729.

- Huisert, M. Electrochemical Characterisation of Filiform. Corrosion on Aluminium Rolled Products.  www.iospress.nl/html/9789040722363.php

- Joseph, C., Farmer, et.al. (1997)  Crevice Corrosion & pitting of High-Level Waste Containers:  Integration  of  Deterministic  &  Probabilistic  Models, UCRL_JC_127980 Part 1.

- Sardisco, J. B., ,et.al. (1965).  Corrosion of iron in an H2S-CO2-H2O system composition and protectiveness of the ssulfide film as a function of pH.  Corrosion, Vol 21, pp 350-354.

- Brossia, C. S., and  Cragnolino,  G. A.  (2000). Effect  of  Environmental Variables on localized Corrosion of Carbon Steel.  Corrosion, Vol 56, No 5, pp 505-514.

- Mack, L. P., ,et.al. (1984). Effect of Bromide Ions on the Electrochemical Behavior of Iron.  Corrosion, Vol 40, No 5.

- Sorell, G., and Hoyt, W. B., (1956).  Collection and Correlation of High Temperature Hydrogen Sulfide Corrosion Data.  The 12th Annual NACE Conference.  The M. W. Kellogg Co., New York, N. Y.

- Corrosion Doctors (2008).  Corrosion Rate Conversion.  http://corrosion-doctors.org/Principles/Conversion.htm

- Shannon, D. W., and Boggs, J. E. (1958).  Factors Affecting the Corrosion of Steel By Oil-Brine-Hydrogen Sulfide Mixtures.  NACE, Vol. 15, pp. 299t-302t.

- Shannon, D. W., and Boggs, J. E. (1958).  An Analytical Procedure for Testing the Effectiveness of Hydrogen Sulfide Corrosion Inhibitors.  NACE, Vol. 15, pp. 303t.

- Carroll, J. J. (1998).  Software for Phase Equilibria in Natural Gas-Water Systems, A Discussion of the Effect of pH on the Solubility of Hydrogen Sulfide.  AQUAlibrium, http://www.telusplanet.net/public/jcarroll/ION.HTM.

- Backnesto, E. B., Drew, R. E., and Stapleford, C. C.  (1956).  High Temperature Hydrogen Sulfide Corrosion.  Corrosion, Vol. 12, No. 1, pp. 22-31.

- Ma, H.Y., Cheng, X.L., Chen, S.H., Li, Chen, G.Q., X., Lei, S.B., and Yang, H.Q.  (1998).  Theoretical Interpretation on Impedance Spectra for Anodic Iron Dissolution in Acidic Solutions Containing Hydrogen Sulfide.  Corrosion–Vol. 54, No. 8.

- Lauvstad, G.  Ø.  (2007).  Breakdown in Passivity of Austenitic Stainless Steels in Cl- and H2s – Modeling and Characterization of the Pit Initiation Process.  NACE Corrosion.  Paper No.07660.

- Wei, S., and Nesic S.  (2007).  A Mechanistic Model of H2S Corrosion of Mild Steel.  NACE Corrosion.  Paper No. 07655.

- ASME-B31G (1991).  Manual for Determining the Remaining Strength of Corroded Pipelines: A Supplement to ASME B31G Code For Pressure Piping.  New York: American Society of Mechanical Engineers.

- Lee, O. S., Kim, D. H. and Choi, S. S. (2006).  Reliability of Buried Pipeline Using a Theory of Probability of Failure. Solid State Phenomena, 110, 221-230.

# Text boxes

O2

HO2

O2

H

O

O

H

O

OH

M

SH

H

O2

HS2

SH

H

O

S

SH

HSO

HOSO

SO2

SO

S

S2

HS2

H2S

Alkaline solution tank

Sulfur-capture tank

Water trap

Thermocouple

To gas chromatograph

Flow controllers power switch

Temperature display

Ignition switch

Temperature display power switch

Ceramic-coated electrodes

CH4

Wirebond on second side

Outlet Thermocouple

Inlet Thermocouple

O2

Flame Igniter

Facility control board

Flow meters/ controllers

Gas conditioning and sampling system

Test rig

DC power sources

Flame Igniter, 100 kV

Heater

°C

H2S reactor

CH4 reactor

CH4

Power Supply

Epoxy Glue

Thermocouples

Data Acquisition Card

O2

H2S

H2S

To concentration sampling, sulfur capture, and exhaust

Figure 3.3.3. Wave excitation arrangement.

encoder

programmable controller

battery

Amplifier

Outlet reservoir

Zero Temperature Bath

Inlet Reservoir

Power Supply connection

Air Direction

Inlet air flow

Protection Cover

Outlet Thermocouple

Fixing Spring

Sample

Inlet Thermocouple

Conventional oil separator

Oil reservoir

Flow meter

EHD oil separator

Aerodynamic Particle Sizer

Test Sample

Pressure Line

Wirebond on first side

Inlet Pipe

Outlet Pipe

Red dots are the (Ntr, atr) values

High voltage power supply